SECTION 07 18 00

TRAFFIC COATINGS

Display hidden notes to specifier. (Don't know how? Click Here)

Copyright 2024 - 2024 ARCAT, Inc. - All rights reserved

** NOTE TO SPECIFIER ** Barrett Company ; hot fluid-applied rubberized asphalt waterproofing.
This section is based on the products of Barrett Company , which is located at:
2926 Chester Ave. 
Cleveland, OH 44114
Toll Free Tel: 800-647-0100
Tel: 908-647-0100
Fax: 908-647-0278
Email: request info (info@barrettroofs.com)
Web: http://www.barrettroofs.com  
 [ Click Here ] for additional information.
For over 10 decades the Barrett Company has had hands-on experience, professionally engineered products, and systems in the high-performance roofing and waterproofing markets.

- GENERAL

  - SECTION INCLUDES

** NOTE TO SPECIFIER ** Delete items below not required for project.

    - Hybrid polyurea and polyurethane trafficable deck coating.

    - Two-component solvenated epoxy-polyamine primer.

  - RELATED SECTIONS

** NOTE TO SPECIFIER ** Delete any sections below not relevant to this project; add others as required.

    - Section 03 30 00 - Cast-in-Place Concrete.

    - Section 04 20 00 - Unit Masonry.

    - Section 06 10 00 - Rough Carpentry.

    - Section 07 14 16 - Cold Fluid-Applied Waterproofing.

    - Section  - .

    - Section 07 21 19 - Foamed-In-Place Insulation.

    - Section 07 62 00 - Sheet Metal Flashing and Trim.

    - Section 07 72 13 - Manufactured Curbs.

    - Section 07 91 23 - Backer Rods.

  - REFERENCES

** NOTE TO SPECIFIER ** Delete references from the list below that are not actually required by the text of the edited section.

    - ASTM International (ASTM):

      - ASTM C579 - Standard Test Methods for Compressive Strength of Chemical-Resistant Mortars, Grouts, Monolithic Surfacings, and Polymer Concretes.

      - ASTM C836 - Standard Specification for High Solids Content, Cold Liquid-Applied Elastomeric Waterproofing Membrane for Use with Separate Wearing Course.

      - ASTM C957 - Standard Specification for High-Solids Content, Cold Liquid-Applied Elastomeric Waterproofing Membrane With Integral Wearing Surface.

      - ASTM D412 - Standard Test Methods for Vulcanized Rubber and Thermoplastic Elastomers - Tension.

      - ASTM D470 - Standard Test Methods for Crosslinked Insulations and Jackets for Wire and Cable.

      - ASTM D624 - Standard Test Method for Tear Strength of Conventional Vulcanized Rubber and Thermoplastic Elastomers.

      - ASTM D2240 - Standard Test Method for Rubber Property - Durometer Hardness.

      - ASTM D2369 - Standard Test Method for Volatile Content of Coatings.

      - ASTM D2697 - Standard Test Method for Volume Nonvolatile Matter in Clear or Pigmented Coatings.

      - ASTM E96 - Standard Test Methods for Gravimetric Determination of Water Vapor Transmission Rate of Materials.

    - Miami Dade County, Florida.

    - South Coast Air Quality Management District (SCAQMD).

    - United States Department of Agriculture (USDA).

  - SUBMITTALS

    - Submit under provisions of Section 01 30 00 - Administrative Requirements.

    - Product Data:

      - Manufacturer's data sheets on each product to be used.

      - Preparation instructions and recommendations.

      - Storage and handling requirements and recommendations.

      - Typical installation methods.

** NOTE TO SPECIFIER ** Delete if not applicable to product type.

    - Verification Samples: Two representative units of each type, size, pattern and color.

    - Shop Drawings: Include details of materials, construction and finish. Include relationship with adjacent construction.

  - QUALITY ASSURANCE

    - Manufacturer Qualifications: Company specializing in manufacturing products specified in this section with a minimum five years documented experience.

    - Installer Qualifications: Company specializing in performing Work of this section with minimum two years documented experience with projects of similar scope and complexity.

    - Source Limitations: Provide each type of product from a single manufacturing source to ensure uniformity.

** NOTE TO SPECIFIER ** Include mock-up if the project size or quality warrant the expense. The following is one example of how a mock-up on might be specified. When deciding on the extent of the mock-up, consider all the major different types of work on the project.

    - Mock-Up: Construct a mock-up with actual materials in sufficient time for Architect's review and to not delay construction progress. Locate mock-up as acceptable to Architect and provide temporary foundations and support.

      - Intent of mock-up is to demonstrate quality of workmanship and visual appearance.

      - If mock-up is not acceptable, rebuild mock-up until satisfactory results are achieved.

      - Retain mock-up during construction as a standard for comparison with completed work.

      - Do not alter or remove mock-up until work is completed or removal is authorized.

  - PRE-INSTALLATION CONFERENCE

    - Convene a conference approximately two weeks before scheduled commencement of the Work. Attendees shall include Architect, Contractor and trades involved. Agenda shall include schedule, responsibilities, critical path items and approvals.

  - DELIVERY, STORAGE, AND HANDLING

    - Store and handle in strict compliance with manufacturer's written instructions and recommendations.

    - Protect from damage due to weather, excessive temperature, and construction operations.

  - PROJECT CONDITIONS

    - Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's recommended limits.

  - WARRANTY

    - Manufacturer's standard limited warranty unless indicated otherwise.

- PRODUCTS

  - MANUFACTURERS

    - Barrett Company, which is located at: 2926 Chester Ave.; Cleveland, OH 44114; ASD Toll Free: 800-647-0100; Phone: 908-647-0100; Email: ________; Web: www.barrettroofs.com.

** NOTE TO SPECIFIER ** Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

    - Substitutions: Not permitted.

    - Requests for substitutions will be considered in accordance with provisions of Section 01 60 00 - Product Requirements.

** NOTE TO SPECIFIER ** Delete articles not required.

  - HYBRID POLYUREA AND POLYURETHANE TRAFFICABLE DECK COATING

    - Performance Requirements:

      - Compliance:

        - ASTM C836.

        - ASTM E96.

        - SMAQMD VOC requirements.

      - Solids by Volume: 95 percent.

      - Pot Life at 75 degrees F (24 degrees C) and 50 percent RH: 9 minutes.

      - Tack Free Time: 3 to 4 hours.

      - Hardness, ASTM D2240, Shore A: 80 plus or minus 3.

      - Tensile Strength, ASTM D412: 2500 psi (17,200 kPa) plus or minus 100 psi (689 kPa).

      - Elongation, ASTM D412: 800 percent plus or minus 100 percent.

      - Tear, ASTM D624: 300 pli (52,500 N/m) plus or minus 25 pli (9100 N/m).

      - Split Tear, ASTM D470: 100 pli (17,500 N/m) plus or minus 10 pli (1750 N/m).

      - VOC Content, ASTM D2369: 0.49 lb/gal (59 g/L).

      - Minimum Application Temperature: 20 degrees F (minus 6.7 degrees C).

    - Basis of Design: HyppoCoat100; as manufactured by Barrett Company.

      - Description: An aliphatic two component, fast-setting, rapid-curing, solvent-free, high-performance, and high-solids polyurea/urethane polymer waterproof coating that can be utilized suitably for heavy-duty wearing surface applications on prepared interior or exterior concrete, plywood and metal surfaces.

** NOTE TO SPECIFIER ** Delete dry film thickness options not required.

      - Dry Film Thickness: 36 mil (0.91 mm). Light pedestrian.

      - Dry Film Thickness: 48 mil (1.2 mm). Heavy pedestrian.

      - Dry Film Thickness: 55 mil (0.91 mm). Vehicular.

      - Dry Film Thickness: 65 mil (1.2 mm). Heavy vehicular traffic.

      - Dry Film Thickness: _____.

      - Features:

        - Applied at any thickness in one application.

        - Excellent weathering.

        - Seamless.

        - Non-gassing.

        - Fast curing.

        - Resists dirt attraction.

        - Good thermal stability.

        - Highly flexible over extreme temperatures.

        - Excellent low temperature flexibility.

        - No odor.

        - Recoatable.

        - Meets SCAQMD VOC Requirements.

  - TWO-COMPONENT SOLVENATED EPOXY-POLYAMINE PRIMER

    - Performance Requirements:

      - Compliance:

        - ASTM C579.

        - ASTM C957.

        - Miami Dade County approved.

        - Meets USDA criteria.

      - Pot Life at 75 degrees F (24 degrees C) and 50 percent RH: 75 minutes plus or minus 15 minutes.

      - Relative Density, Part A: 1.27 plus or minus 0.1.

      - Relative Density, Part B: 1.85 plus or minus 0.1.

      - Solids by Volume, ASTM D2369: 90 percent plus or minus 2 percent.

      - Solids by Weight, ASTM D2697: 84 percent plus or minus 2 percent.

      - VOC Content, ASTM D2369: 0.75 lb/gal (90 g/L).

** NOTE TO SPECIFIER ** Delete basis of design options not required.

    - Basis of Design: HyppoCoat PC; as manufactured by Barrett Company.

      - Performance Requirements:

        - Viscosity at 75 degrees F (24 degrees C): 600 plus or minus 50.

      - Description: A two component, solvenated, epoxy-polyamine liquid-applied primer with unique penetrating characteristics.

      - Dry Film Thickness: 4 mil (0.10 mm) plus or minus 1 mil (0.025 mm).

      - Features:

        - Excellent adhesion.

        - Low viscosity.

        - Seals concrete.

- EXECUTION

  - EXAMINATION

    - Do not begin installation until substrates have been properly constructed and prepared.

    - If substrate preparation is the responsibility of another installer, notify Architect in writing of unsatisfactory preparation before proceeding.

  - PREPARATION

    - Clean surfaces thoroughly prior to installation.

    - Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

  - INSTALLATION

    - Install in accordance with manufacturer's instructions, approved submittals, and in proper relationship with adjacent construction.

  - FIELD QUALITY CONTROL

    - Flood Test: Each contiguous area shall be water tested with 2 inches (51 mm) of standing water for a 48 hour period.

      - Provide for overflow in the event of rain.

      - Flood tests shall be witnessed and approved by Architect and Manufacturer.

      - An electric field vector mapping may be used in lieu of the flood test.

    - Correct any deficiencies in the membrane, if any, as prescribed by material Manufacturer and approved by the Architect.

  - CLEANING AND PROTECTION

    - Clean products in accordance with the manufacturers recommendations.

    - Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION