SECTION 09 77 26

SHOP-APPLIED SURFACING FILMS.

Display hidden notes to specifier. (Don't know how? Click Here)

Copyright 2025 - 2025 ARCAT, Inc. - All rights reserved

** NOTE TO SPECIFIER ** American Renolit Corp.; shop applied surfacing films.
This section is based on the products of American Renolit Corp., which is located at:
1207 E. Lincolnway
LaPorte, IN 46350
Tel: 219-324-6886
Fax: 219-324-5332
Email: request info ()
Web: https://www.renolit.com/en/company/market-units/exterior-solutions/renolit-united-states-canada  
 [ Click Here ] for additional information.
RENOLIT is a family-owned business that offers high-quality plastic films and products serving the automotive, healthcare, home and building, maritime, packaging, and visual communication sectors. RENOLIT Exofol PFX is their premium exterior product which includes anti-graffiti properties. Exofol PFX is applied over many types of exterior building materials such as railings, soffits, and cladding.

- GENERAL

  - SECTION INCLUDES

** NOTE TO SPECIFIER ** Delete items below not required for project.

    - Shop-applied high performance decorative surfacing film applied to window profiles.

  - RELATED SECTIONS

** NOTE TO SPECIFIER ** Delete any sections below not relevant to this project; add others as required.

    - Section 08 52 00 - Wood Windows.

    - Section 08 53 0- Plastic Windows.

  - REFERENCE STANDARDS

    - AWI - Architectural Woodwork Institute Standards.

    - Woodwork Institute - NAAWS - North American Architectural Woodwork Standards; Edition 2, with Errata.

  - SUBMITTALS

    - Submit under provisions of Section 01 30 00 - Administrative Requirements.

    - Samples: Two complete sets of color chips representing manufacturer's full range of available colors and patterns.

    - Statement of Applicator Qualifications.

    - Warranty:

      - Refer to Section 01 78 00 Project Closeout.

      - Complete forms with Owner's name and register with manufacturer.

  - QUALITY ASSURANCE

    - Applicator Qualifications: Company specializing in performing Work of this section with minimum three years experience with projects of similar scope and complexity.

  - DELIVERY, STORAGE, AND HANDLING

    - Protect film from damage during handling and transportation.

    - Store film protected from exposure to harmful weather conditions and at temperature conditions recommended by manufacturer.

    - Avoid contact with materials that might cause staining, scratching, or other surface damage.

  - WARRANTY

    - Manufacturer's standard 5 year warranty for color retention.

- PRODUCTS

  - MANUFACTURERS

    - Acceptable Manufacturer: American Renolit Corp., which is located at:
1207 E. Lincolnway
LaPorte, IN 46350
Tel: 219-324-6886
Fax: 219-324-5332
Email: request info ();Web: https://www.renolit.com/en/company/market-units/exterior-solutions/renolit-united-states-canada

    - Manufacturer Tel: 1-219-324-6886; Web: www.com. Web: .RENOLIT EXOFOL PFX (US).

** NOTE TO SPECIFIER ** Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

    - Substitutions: Not permitted.

    - Requests for substitutions will be considered in accordance with the provisions of Section 01 25 00.

  - SHOP-APPLIED, MULTILAYER, HIGH-PERFORMANCE DECORATIVE FILM

    - Thickness: 0.0067 inch (0.17 mm) to 0.0071 inch (0.18 mm).

    - Layers:

      - Manufacturer's standard primer.

      - Unplasticized, pigmented PVC base film with SST.

      - Manufacturer's standard ink layer.

      - Transparent polymethyl methacrylate (PMMA) film.

      - Transparent polyvinylidene fluoride (PVDF) film.

    - Finish:

** NOTE TO SPECIFIER ** Delete one of the following two paragraphs.

      - Color: As indicated on drawings.

      - Color: As selected by Architect from manufacturers standard range of color selections.

      - Pattern: Woodgrain.

      - Sheen: Super-Matt.

- EXECUTION

  - EXAMINATION

    - Verify substrate condition. Determine conditions are acceptable for film application in accordance with manufacturer's instructions.

    - If substrate preparation is responsibility of another party, notify Architect of unsatisfactory preparation before proceeding.

    - Notify Architect in writing of conditions detrimental to proper and timely completion of work. Do not proceed without correcting unsatisfactory conditions.

  - PREPARATION

    - Surface Preparation: Clean and prepare substrates in accordance with film manufacturer's instructions.

  - APPLICATION

    - Apply film coating in accordance with manufacturer's written instructions on manufacturer approved lamination machine.

    - Allow to cure prior to shipping.

  - PROTECTION

    - Protect installed film from damage by subsequent shipping, installation, and construction operations.

END OF SECTION