SECTION 06 60 00

CELLULAR PVC FABRICATIONS

Display hidden notes to specifier. (Don't know how? Click Here) 
 Copyright 2016 -  2020 ARCAT, Inc. - All rights reserved

PART 1    GENERAL
1.1	SECTION INCLUDES
A.	Cellular PVC fabrications including the following:
1.	Trim.
2.	Mouldings.
3.	Decking.
4.	Porch flooring.
5.	Railings.
6.	Pavers.
1.2	RELATED SECTIONS
A.	Section 06 10 00 - Rough Carpentry.
B.	Section 06 20 00 - Finish Carpentry.
1.3	REFERENCES
A.	ASTM International (ASTM): ASTM E84 - Standard Test Method for Surface Burning Characteristics of Building Materials.
1.4	SUBMITTALS
A.	Submit under provisions of Section 01 30 00 - Administrative Requirements.
B.	Product Data: Manufacturer's data sheets on each product to be used, including:
1.	Preparation instructions and recommendations.
2.	Storage and handling requirements and recommendations.
3.	Installation methods.
C.	Verification Samples: For each finish product specified, two samples, minimum size 6 inches (150 mm) square representing actual product, color, and patterns.
1.5	QUALITY ASSURANCE
A.	Regulatory Requirements: Comply with requirements of authorities having jurisdiction and applicable codes at the location of the project.
B.	Manufacturer Qualifications: Minimum 5 years experience manufacturing similar products.
C.	Installer Qualifications: Minimum 2 years experience installing similar products.
D.	Mock-Ups: Provide a mock-up for evaluation of surface preparation techniques and application workmanship.
1.	Construct area designated by Architect.
2.	Do not proceed with remaining work until workmanship is accepted by Architect.
3.	Remodel mock-up area as required to produce acceptable work.
1.6	DELIVERY, STORAGE, AND HANDLING
A.	Deliver and store products in manufacturer's unopened packaging bearing the brand name and manufacturer's identification until ready for installation.
B.	Comply with manufacturer's recommendations. Handle materials to avoid damage.
1.7	PROJECT CONDITIONS
A.	Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's recommended limits.
1.8	WARRANTY
A.	Provide manufacturer's standard limited warranty for products, stating that components will be free from defects in material that occur as a direct result of the manufacturing process, occur under normal use and service, occur during the warranty period and result in blistering, peeling, flaking, cracking, splitting, cupping, rotting or structural defects from termites or fungal decay. 
1.	AZEK Trim Warranty Period: 25 years.
2.	AZEK Moulding Warranty Period: 25 years.
3.	AZEK Decking Warranty: 30 years for single-family residential applications.
4.	AZEK Porch Floor Warranty:
a.	Lifetime for single-family residential applications.
b.	20 years for applications other than single-family residential.
5.	AZEK Rail Warranty:
a.	25 years for single-family residential applications.
b.	10 years for applications other than single-family residential.
6.	AZEK Cable Rail Warranty: 10 years.
7.	AZEK Rail Accessories Warranty: 5 years.
8.	AZEK Pavers Warranty Period: 10 years for single-family residential applications.
PART 2    PRODUCTS
2.1	MANUFACTURERS
A.	Acceptable Manufacturer: AZEK Building Products, Inc., which is located at: 894 Prairie Ave.; Wilmington, OH 45177; ASD Toll Free Tel: 877-ASK-AZEK; Email: request info; Web: https://www.azek.com; https://timbertech.com
B.	Substitutions: Not permitted.
C.	Requests for substitutions will be considered in accordance with provisions of Section 01 60 00.
2.2	TRIM
A.	Fire Performance Characteristics: Provide products complying with the following:
1.	Flame Spread Index: Less than 25, ASTM E 84.
B.	PVC Trim: Material shall have the following characteristics:
1.	Material: Solid Cellular PVC.
2.	Style: Traditional.
3.	Style: Frontier.
4.	Trim Size, 5/8 Thickness:
a.	5/8 inches x 3-1/2 inches x 12 feet actual dimension.
b.	5/8 inches x 3-1/2 inches x 18 feet actual dimension.
c.	5/8 inches x 5-1/2 inches x 12 feet actual dimension.
d.	5/8 inches x 5-1/2 inches x 18 feet actual dimension.
e.	5/8 inches x 7-1/4 inches x 12 feet actual dimension.
f.	5/8 inches x 7-1/4 inches x 18 feet actual dimension.
g.	5/8 inches x 9-1/4 inches x 12 feet actual dimension.
h.	5/8 inches x 9-1/4 inches x 18 feet actual dimension.
i.	5/8 inches x 11-1/4 inches x 12 feet actual dimension
j.	5/8 inches x 11-1/4 inches x 18 feet actual dimension.
k.	5/8 inches x 15-1/4 inches x 12 feet actual dimension.
l.	5/8 inches x 15-1/4 inches x 18 feet actual dimension.
5.	Trim Size, 4/4 Thickness:
a.	1 x 2 x 18 feet nominal, 3/4 inches x 1-1/2 inches by 18 feet actual dimension.
b.	1 x 4 x 12 feet nominal, 3/4 inches x 3-1/2 inches by 12 feet actual dimension.
c.	1 x 4 x 18 feet nominal, 3/4 inches x 3-1/2 inches by 18 feet actual dimension.
d.	1 x 5 x 12 feet nominal, 3/4 inches x 4-1/2 inches by 12 feet actual dimension.
e.	1 x 5 x 18 feet nominal, 3/4 inches x 4-1/2 inches by 18 feet actual dimension.
f.	1 x 6 x 12 feet nominal, 3/4 inches x 5-1/2 inches by 12 feet actual dimension.
g.	1 x 6 x 18 feet nominal, 3/4 inches x 5-1/2 inches by 18 feet actual dimension.
h.	1 x 8 x 12 feet nominal, 3/4 inches x 7-1/4 inches by 12 feet actual dimension.
i.	1 x 8 x 18 feet nominal, 3/4 inches x 7-1/4 inches by 18 feet actual dimension.
j.	1 x 10 x 12 feet nominal, 3/4 inches x 9-1/4 inches by 12 feet actual dimension.
k.	1 x 10 x 18 feet nominal, 3/4 inches x 9-1/4 inches by 18 feet actual dimension.
l.	1 x 12 x 12 feet nominal, 3/4 inches x 11-1/4 inches by 12 feet actual dimension.
m.	1 x 12 x 18 feet nominal, 3/4 inches x 11-1/4 inches by 18 feet actual dimension.
n.	1 x 16 x 12 feet nominal, 3/4 inches x 15-1/4 inches by 12 feet actual dimension.
o.	1 x 16 x 18 feet nominal, 3/4 inches x 15-1/4 inches by 18 feet actual dimension.
6.	Trim Size, 5/4 Thickness:
a.	5/4 x 4 x 12 feet nominal, 1 inches x 3-1/2 inches by 12 feet actual dimension.
b.	5/4 x 4 x 18 feet nominal, 1 inches x 3-1/2 inches by 18 feet actual dimension.
c.	5/4 x 4 x 20 feet nominal, 1 inches x 3-1/2 inches by 20 feet actual dimension.
d.	5/4 x 5 x 12 feet nominal, 1 inches x 4-1/2 inches by 12 feet actual dimension.
e.	5/4 x 5 x 18 feet nominal, 1 inches x 4-1/2 inches by 18 feet actual dimension.
f.	5/4 x 5 x 20 feet nominal, 1 inches x 4-1/2 inches by 20 feet actual dimension.
g.	5/4 x 6 x 12 feet nominal, 1 inches x 5-1/2 inches by 12 feet actual dimension.
h.	5/4 x 6 x 18 feet nominal, 1 inches x 5-1/2 inches by 18 feet actual dimension.
i.	5/4 x 6 x 20 feet nominal, 1 inches x 5-1/2 inches by 20 feet actual dimension.
j.	5/4 x 8 x 12 feet nominal, 1 inches x 7-1/4 inches by 12 feet actual dimension.
k.	5/4 x 8 x 18 feet nominal, 1 inches x 7-1/4 inches by 18 feet actual dimension.
l.	5/4 x 8 x 20 feet nominal, 1 inches x 7-1/4 inches by 20 feet actual dimension.
m.	5/4 x 10 x 12 feet nominal, 1 inches x 9-1/4 inches by 12 feet actual dimension.
n.	5/4 x 10 x 18 feet nominal, 1 inches x 9-1/4 inches by 18 feet actual dimension.
o.	5/4 x 10 x 20 feet nominal, 1 inches x 9-1/4 inches by 20 feet actual dimension.
p.	5/4 x 12 x 12 feet nominal, 1 inches x 11-1/4 inches by 12 feet actual dimension.
q.	5/4 x 12 x 18 feet nominal, 1 inches x 11-1/4 inches by 18 feet actual dimension.
r.	5/4 x 12 x 20 feet nominal, 1 inches x 11-1/4 inches by 20 feet actual dimension.
s.	5/4 x 16 x 12 feet nominal, 1 inches x 15-1/4 inches by 12 feet actual dimension.
t.	5/4 x 16 x 18 feet nominal, 1 inches x 15-1/4 inches by 18 feet actual dimension.
u.	5/4 x 16 x 20 feet nominal, 1 inches x 15-1/4 inches by 20 feet actual dimension.
7.	Trim Size, 6/4 Thickness:
a.	6/4 x 4 x 20 feet nominal, 1-1/4 inches x 3-1/2 inches by 20 feet actual dimension.
b.	6/4 x 6 x 20 feet nominal, 1-1/4 inches x 5-1/2 inches by 20 feet actual dimension.
c.	6/4 x 8 x 20 feet nominal, 1-1/4 inches x 7-1/4 inches by 20 feet actual dimension.
d.	6/4 x 10 x 20 feet nominal, 1-1/4 inches x 9-1/4 inches by 20 feet actual dimension.
e.	6/4 x 12 x 20 feet nominal, 1-1/4 inches x 11-1/4 inches by 20 feet actual dimension.
8.	AZEK Rabbeted Trim:
a.	5/4 x 4 x 18 feet nominal, 1 inches x 3-1/2 inches by 18 feet actual dimension.
b.	5/4 x 6 x 18 nominal, 1 inches x 5-1/2 inches by 18 feet actual dimension.
c.	5/4 x 8 x 18 feet nominal, 1 inches x 7-1/4 inches by 18 feet actual dimension.
C.	PVC Cornerboards: Material shall have the following characteristics:
1.	Material: Solid Cellular PVC.
2.	Style: Traditional.
3.	Style: Frontier.
4.	Cornerboards with Straight Corners:
a.	5/4 x 4 x 4 x 10 feet nominal, 1 inches x 3-1/2 inches x 3-1/2 inches by 10 feet actual dimension.
b.	5/4 x 4 x 4 x 20 feet nominal, 1 inches x 3-1/2 inches x 3-1/2 inches by 20 feet actual dimension.
c.	5/4 x 6 x 6 x 10 feet nominal, 1 inches x 5-1/2 inches x 5-1/2 inches by 10 feet actual dimension.
d.	5/4 x 6 x 6 x 20 feet nominal, 1 inches x 5-1/2 inches x 5-1/2 inches by 20 feet actual dimension.
e.	6/4 x 4 x 4 x 10 feet nominal, 1-1/4 inches x 3-1/2 inches x 3-1/2 inches by 10 feet actual dimension.
f.	6/4 x 6 x 6 x 10 feet nominal, 1-1/4 inches x 5-1/2 inches x 5-1/2 inches by 10 feet actual dimension.
5.	Cornerboards with Rabbeted Corners:
a.	5/4 x 4 x 4 x 10 feet nominal, 1 inches x 3-1/2 inches x 3-1/2 inches by 10 feet actual dimension.
b.	5/4 x 4 x 4 x 20 feet nominal, 1 inches x 3-1/2 inches x 3-1/2 inches by 20 feet actual dimension.
c.	5/4 x 6 x 6 x 10 feet nominal, 1 inches x 5-1/2 inches x 5-1/2 inches by 10 feet actual dimension.
d.	5/4 x 6 x 6 x 20 feet nominal, 1 inches x 5-1/2 inches x 5-1/2 inches by 20 feet actual dimension.
e.	5/4 x 8 x 8 x 10 feet nominal, 1 inches x 7-1/4 inches x 7-1/4 inches by 10 feet actual dimension.
f.	5/4 x 8 x 8 x 20 feet nominal, 1 inches x 7-1/4 inches x 7-1/4 inches by 20 feet actual dimension.
6.	Quick-Corner: With 13/16 J-Channel:
a.	6 x 6 x 20 feet nominal, 1 inches x 5-1/2 inches x 5-1/2 inches by 20 feet actual dimension.
D.	PVC Sheet: Material shall have the following characteristics:
1.	Material: Solid Cellular PVC.
2.	Style: Traditional.
3.	Sheet Size:
a.	3/8 inches x 4 feet x 8 feet actual dimension.
b.	3/8 inches x 4 feet x 10 feet actual dimension.
c.	1/2 inches x 4 feet x 8 feet actual dimension.
d.	1/2 inches x 4 feet x 10 feet actual dimension.
e.	5/8 inches x 4 feet x 8 feet actual dimension.
f.	5/8 inches x 4 feet x 10 feet actual dimension.
g.	5/8 inches x 4 feet x 18 feet actual dimension.
h.	3/4 inches x 4 feet x 8 feet actual dimension.
i.	3/4 inches x 4 feet x 10 feet actual dimension.
j.	3/4 inches x 4 feet x 12 feet actual dimension.
k.	3/4 inches x 4 feet x 18 feet actual dimension.
l.	1 inches x 4 feet x 8 feet actual dimension.
m.	1 inches x 4 feet x 10 feet actual dimension.
n.	1 inches x 4 feet x 12 feet actual dimension.
o.	1 inches x 4 feet x 20 feet actual dimension.
E.	PVC Skirt Board: Two-piece skirt board including universal siding interface. Material shall have the following characteristics:
1.	Material: Solid Cellular PVC.
2.	Style: Traditional.
3.	Style: Frontier.
4.	Skirt Board Trimboard Size:
a.	5/4 x 6 x 18 feet nominal, 1 inches x 5-1/2 inches by 18 feet actual dimension.
b.	5/4 x 8 x 18 feet nominal, 1 inches x 7-1/4 inches by 18 feet actual dimension.
c.	5/4 x 10 x 18 feet nominal, 1 inches x 9-1/4 inches by 18 feet actual dimension. 
5.	Nailing Flange Length: 1-1/2 inches.
6.	Drip Edge Overhang: 1/4 inches.
F.	AZEK To Mill (ATM): Material shall have the following characteristics:
1.	Material: Solid Cellular PVC.
2.	Board Size:
a.	1-1/4 inches x 9-1/4 inches x 18 feet actual dimension.
b.	1-1/4 inches x 48 inches x 8 feet actual dimension.
G.	Integrated Drip Edge Board: Two-piece skirt board including drip edge. Material shall have the following characteristics:
1.	Material: Solid Cellular PVC.
2.	Style: Traditional.
3.	Style: Frontier.
4.	Skirt Board Trimboard Size:
a.	5/4 x 4 x 18 feet nominal, 1 inches x 3-1/2 inches by 18 feet actual dimension.
b.	5/4 x 6 x 18 feet nominal, 1 inches x 5-1/2 inches by 18 feet actual dimension.
5.	Nailing Flange Length: 1-1/4 inches.
6.	Drip Edge Overhang: 1/8 inches.
H.	Finish Grade Trim: Two-piece, hidden fastener trim system with base plate for fastening and cover trim with nailing flange. Material shall have the following characteristics:
1.	Material: Solid Cellular PVC.
2.	Style: Traditional.
3.	Finish Grade Trim Size:
a.	6/4 inches x 4 inches by 18 feet actual dimension.
b.	6/4 inches x 6 inches by 18 feet actual dimension.
4.	Miter Corner Reinforcement: 3" x 3".
I.	Column Wrap: Composed of three connected panels and a fourth panel that locks into place to form a tight and secure enclosure. Material shall have the following characteristics:
1.	Material: Solid Cellular PVC.
2.	Style: Traditional.
3.	Column Wrap Size (Inner Dimensions):
a.	4 x 4 x 10 feet nominal, 3-3/4 inches x 3-3/4 inches by 10 feet actual dimension.
b.	6 x 6 x 10 feet nominal, 5-3/4 inches x 5-3/4 inches by 10 feet actual dimension. 
c.	8 x 8 x 10 feet nominal, 7-3/4 inches x 7-3/4 inches by 10 feet actual dimension.
2.3	MOULDINGS
A.	Crown Profiles: Material shall have the following characteristics:
1.	Material: Solid Cellular PVC.
2.	Crown Moulding Profile:
a.	3 inch Crown Moulding:  9/16 inches x 2-3/4 inches x 16 feet, AZM-52.
b.	4 inch Crown Moulding:  9/16 inches x 3 5/8 inches x 16 feet, AZM-49.
c.	5 inch Crown Moulding:  11/16 inches x 4 5/8 inches x 16 feet, AZM-47.
d.	6 inch Crown Moulding:  11/16 inches x 5-1/4 inches x 16 feet, AZM-45.
e.	8 inch Crown Moulding:  7-1/2 inches x 1 inches, AZM-43.
f.	3-1/2 inch Bed Moulding:  13/16 inches x 3-1/2 inches x 16 feet, AZM-28. 
g.	Bed Moulding: 9/16 inches x 1-3/4 inches x 16 feet, AZM-75.
h.	Cove Moulding: 9/16 inches x 2-3/4 inches x 16 feet, AZM-52. 
i.	Imperial Rake Crown: 1 3/8 inches x 2-3/4 inches x 16 feet, AZM-6937.
j.	Rams Crown: 1 13/32 inches x 2 1/16 inches x 16 feet, AZM-6934.
B.	Detail Profiles: Material shall have the following characteristics:
1.	Material: Solid Cellular PVC.
2.	Detail Profile:
a.	Historic Sill: 1-3/4 inches x 2 1/32 inches x 16 feet, AZM-6930.
b.	Sub Sill Nose: 1 17/32 inches x 1-1/2 inches x 16 feet, AZM-6933. 
c.	Water Table: 2-3/4 inches x 2 inch x 18 feet, AZM-6935.
d.	Quarter Round: -3/4 inches x-3/4 inches x 16 feet, AZM-105.
e.	Scotia: -3/4 inches x-3/4 inches x 16 inches, AZM-93.
f.	Drip Cap: 1 5/8 inches x 11/16 inches, AZM-197. 
C.	Casing Profiles: Material shall have the following characteristics:
1.	Material: Solid Cellular PVC.
2.	Casing Profile:
a.	Adams Casing: 1 1/16 inches x 3-1/2 inches x 16 feet, AZM-97.
b.	Back Band: 1 11/32 inches x 1 3/16 inches x 16 feet, AZM-6931. 
c.	Back Moulding: 11/16 inches x 1 5/8 inches x 16 feet, AZM-217.
d.	Base Cap: 11/16 inches x 1 1/8 inches x 16 feet, AZM-164.
e.	Brick Mould: 1-1/4 inches x 2 inch x 17 feet, AZM-180.
f.	Brick Mould: 1-1/4 inches x 2 inch x 18 feet, AZM-180.
g.	Colonial Base Cap: -3/4 inches x 5-1/4 inches x 16 feet, AZM-163. 
h.	Crosshead Pediment: 2 13/32 inches x 7 1/8 inches x 18 feet, AZM-6216.
i.	Rake Moulding: 1 1/16 inches x 2 inch x 16 feet, AZM-287. 
j.	Shingle Mould: 11/16 inches x 1 5/8 inches x 16 feet, AZM-210.
k.	Square Profile Moulding: 1-1/2 inches x 1-1/2 inches x 12 feet, AZM-236.
l.	Wainscot Cap: 1 inches x 2-1/4 inches x 16 inches, AZM-284.
m.	Fluted/Reeded: 5-1/4 inches x 15/16 inches, AZM-606. 
n.	Garage Door Thermostop: 2 inch x 3/8 inches, AZM-6936. 
2.4	DECKING
A.	Thermal Characteristics: Provide products complying with the following:
1.	Flame Spread Index: Less than 200, ASTM E 84.
B.	Arbor Collection: Tropical hardwood look. Material shall have the following characteristics:
1.	Material: Solid Cellular PVC.
2.	Dimensions: 1 inches x 5-1/2 inches.
3.	Color: Silver Oak.
4.	Color: Mountain Redwood.
5.	Color: NEW Morado.
6.	Color: NEW Acacia.
7.	Color: Hazelwood.
8.	Color: Brazilian Walnut.
9.	Color: To be selected by Architect.
10.	Profile: Grooved, for hidden fastening.
11.	Profile: Square shouldered.
12.	Board Length: 12 feet.
13.	Board Length: 16 feet.
14.	Board Length: 20 feet.
15.	Fastening System: FUSIONLoc.
16.	Fastening System: Cortex.
17.	Trim: Fascia trim.
C.	Harvest Collection: Material shall have the following characteristics:
1.	Material: Solid Cellular PVC.
2.	Dimensions: 1 inches x 5-1/2 inches.
3.	Color: Brownstone.
4.	Color: Slate Gray.
5.	Color: NEW Kona.
6.	Color: Island Oak.
7.	Color: Autumn Chestnut.
8.	Color: To be selected by Architect.
9.	Profile: Grooved, for hidden fastening.
10.	Profile: Square shouldered.
11.	Board Length: 12 feet.
12.	Board Length: 16 feet.
13.	Board Length: 20 feet.
14.	Fastening System: FUSIONLoc.
15.	Fastening System: Cortex.
16.	Trim: Fascia trim.
D.	Vintage Collection: Realistic wood appearance and texture. Material shall have the following characteristics:
1.	Material: Capped Cellular PVC.
2.	Dimensions: 1 inches x 5-1/2 inches.
3.	Color: Mahogany.
4.	Color: Cypress.
5.	Color: Dark Hickory.
6.	Color: To be selected by Architect.
7.	Profile: Grooved, for hidden fastening.
8.	Profile: Square shouldered.
9.	Board Length: 12 feet.
10.	Board Length: 16 feet.
11.	Board Length: 20 feet.
12.	Fastening System: FUSIONLoc.
13.	Fastening System: Cortex.
14.	Trim: Fascia trim.
2.5	PORCH FLOORING
A.	Thermal Characteristics: Provide products complying with the following:
1.	Flame Spread Index: Less than 200, ASTM E 84.
B.	Porch Flooring: Material shall have the following characteristics:
1.	Material: Capped Cellular PVC.
2.	Surface Texture: Smooth.
3.	Edge Profile: Tongue and groove.
4.	Color: Brownstone.
5.	Color: Slate Gray.
6.	Color: Morado.
7.	Color: Silver Oak.
8.	Color: Oyster.
9.	Color: To be selected by Architect.
10.	Fastening System: FUSIONLoc.
11.	Fastening System: Cortex.
12.	Trim: Fascia trim.
13.	Storage: AZEK In-Deck Storage Kit.
14.	Bench & Planter: AZEK Bench & Planter Kit.
2.6	RAILINGS
A.	Thermal Characteristics: Provide products complying with the following:
1.	Flame Spread Index: Less than 200, ASTM E 84.
B.	Premier Rail: Wood look railing system. Material shall have the following characteristics:
1.	Material: Solid Cellular PVC.
2.	Profile: Classic Victorian profile.
3.	Color: White.
4.	Color: Black.
5.	Color: Kona.
6.	Color: Brownstone.
7.	Color: Slate Gray.
8.	Color: To be selected by Architect.
9.	Infill: As indicated on Drawings.
10.	Infill: Composite.
11.	Infill: Aluminum balusters, round.
12.	Infill: Aluminum balusters, square.
13.	Infill: Cable.
14.	Infill: Glass.
15.	Length: 6 feet.
16.	Length: 8 feet.
17.	Length: 10 feet.
18.	Hidden fastener system.
C.	Reserve Rail: Material shall have the following characteristics:
1.	Material: Solid Cellular PVC.
2.	Color: White.
3.	Infill: As indicated on Drawings.
4.	Infill: Composite.
5.	Infill: Aluminum balusters, round.
6.	Infill: Aluminum balusters, square.
7.	Infill: Cable.
8.	Infill: Glass.
9.	Length: 6 feet.
10.	Length: 8 feet.
11.	Length: 10 feet.
12.	Length: 12 feet, over the post.
13.	Length: 16 feet, over the post.
14.	Hidden fastener system.
D.	Trademark Rail: Material shall have the following characteristics:
1.	Material: Solid Cellular PVC.
2.	Profile: Colonial.
3.	Color: White.
4.	Infill: As indicated on Drawings.
5.	Infill: Composite.
6.	Infill: Aluminum balusters, round.
7.	Infill: Aluminum balusters, square.
8.	Infill: Cable.
9.	Infill: Glass.
10.	Length: 6 feet.
11.	Length: 8 feet.
12.	Length: 10 feet.
13.	Hidden fastener system.
E.	Rail Lighting: LED lights.
1.	Type: Lighted Island Cap.
2.	Type: Post Cap Light.
3.	Type: Accent Light.
4.	Type: Under Rail Light.
5.	Type: In-Deck Light.
6.	Type: Riser Light.
F.	Gate Kit: Designed to work with AZEK Rail. Material shall have the following characteristics:
1.	Height: 36 inches.
2.	Single Gate Opening: 48 inches.
G.	ADA Rail: Handrail designed to work with AZEK Rail. Material shall have the following characteristics:
1.	Compliant with IRC and IBC handrail test requirements.
2.	Color: Black.
3.	Color: White.
4.	Color: To be selected by Architect.
2.7	PAVERS
A.	Standard Pavers: Material shall have the following characteristics:
1.	Material: Solid Composite.
2.	Recycled Content: Up to 95 percent post-consumer.
3.	Color: Redwood.
4.	Color: Boardwalk.
5.	Color: Olive.
6.	Color: Village.
7.	Color: Waterwheel.
8.	Color: To be selected by Architect.
9.	Size: As indicated on Drawings.
10.	Size: 4 inches x 8 inches.
11.	Size: 4 inches x 4 inches.
12.	Size: 8 inches x 8 inches.
13.	Special Shape: Soldier Course Wedge, 4 inches x 8 inches, Redwood.
14.	Special Shape: Soldier Course Wedge, 4 inches x 8 inches, Waterwheel.
15.	Special Shape: Soldier Course Full, 4 inches x 8 inches, Redwood.
16.	Special Shape: Soldier Course Full, 4 inches x 8 inches, Waterwheel.
17.	Paver Grid: 16 inches x 16 inches.
18.	Combined Height of Paver and Grid: 2.38 inches.
B.	Permeable Pavers: Material shall have the following characteristics:
1.	Material: Solid Composite.
2.	Recycled Content: Up to 95 percent post-consumer.
3.	Infiltration Rate: 480 inches per hour, minimum.
4.	Joints: 0.275 inches space between pavers, filled with small stones.
5.	Subbase: Open-graded.
6.	Color: Redwood.
7.	Color: Boardwalk.
8.	Color: Olive.
9.	Color: Village.
10.	Color: Waterwheel.
11.	Color: To be selected by Architect.
12.	Size: 4 inches x 8 inches.
13.	Paver Grid: 16 inches x 16 inches.
14.	Combined Height of Paver and Grid: 2.38 inches.
C.	Resurfacing Pavers: Material shall have the following characteristics:
1.	Material: Solid Composite.
2.	Recycled Content: Up to 95 percent post-consumer.
3.	Color: Redwood.
4.	Color: Boardwalk.
5.	Color: Olive.
6.	Color: Village.
7.	Color: Waterwheel.
8.	Color: To be selected by Architect.
9.	Size: As indicated on Drawings.
10.	Size: 4 inches x 8 inches.
11.	Size: 4 inches x 4 inches.
12.	Size: 8 inches x 8 inches.
13.	Special Shape: Bullnose Paver.
14.	Special Shape: Transition Paver, Redwood.
15.	Special Shape: Transition Paver, Boardwalk.
16.	Special Shape: Transition Paver, Waterwheel.
17.	Paver Grid: 16 inches x 16 inches Dimpled.
18.	Combined Height of Paver and Grid: 1.75 inches.
2.8	ACCESSORIES
A.	Fasteners: Stainless steel or hot-dip galvanized, with thin shank, blunt point, full round head as recommended by the manufacturer.
B.	Adhesives: AZEK Adhesive, a non-toxic, odorless, UV stable, water-based PVC cement. 
C.	Sealants: Urethane, polyurethane or acrylic based sealants without silicone.
PART 3    EXECUTION
3.1	EXAMINATION
A.	Verification of Conditions: Examine areas and conditions under which Work is to be performed and identify conditions that may be detrimental to proper or timely completion.
B.	For decking and porch flooring installations, ensure surfaces are suitable for installation of decking and that adequate structural support has been provided.
1.	Standard Installation: Confirm that joists are spaced at 16 inches on center maximum, and are sloped at a minimum of 1/4 inch per foot away from the building.
2.	Forty-five Degree Angle Installation: Confirm that joists are spaced at 12 inches on center maximum, and are sloped at a minimum of 1/4 inch per foot away from the building.
C.	Do not proceed until unsatisfactory conditions have been corrected.
3.2	INSTALLATION
A.	General: Install products in accordance with manufacturer's instructions, approved submittals, and in proper relationship with adjacent construction.
1.	Use manufacturer's recommended fasteners, not more than 2 inches from ends.
2.	Glue joints to eliminate joint separation.
3.	Allow for expansion and contraction at ends of the runs.
B.	Decking and Porch Flooring Installation:
1.	Install with grain side up for the walking surface.
2.	Fasten tight to joists. Provide shims if there are variations in framing.
3.	Countersink fasteners slightly to provide necessary clearance when installing the next board.
4.	Cut final boards as required for proper appearance.
3.3	CLEANING AND PROTECTION
A.	Protect from damage during construction operations. Promptly repair any damaged surfaces. Remove and replace work which cannot be satisfactorily repaired.
B.	Clean products, prior to Substantial Completion, using materials recommended by the manufacturer to remove stains, dirt and debris prior to final acceptance.

END OF SECTION