SECTION 07 46 33

ROOFING AND SIDING PANELS

Display hidden notes to specifier. (Don't know how? Click Here) 
 Copyright 2006 -  2026 ARCAT, Inc. - All rights reserved

PART 1    GENERAL
1.1	SECTION INCLUDES
A.	Preformed aluminum siding, trim, and accessories for facing exterior walls.
B.	Preformed aluminum soffit and fascia panels, trim, and accessories for facing exterior roof overhangs, eaves and fascia.
C.	Preformed steel siding, trim, and accessories for facing exterior walls.
D.	Preformed steel fascia panels, trim, and accessories for facing exterior roof overhangs, eaves and fascia.
E.	Preformed vinyl siding, trim, and accessories for facing exterior walls.
F.	Preformed vinyl soffit panels, trim, and accessories for facing exterior roof overhangs, eaves and fascia.
G.	Preformed polypropylene siding, trim, and accessories for facing exterior walls.
1.2	RELATED SECTIONS
A.	Section 05 44 00 - Cold-Formed Metal Trusses.
B.	Section 06 10 00 - Rough Carpentry.
C.	Section 07 21 16 - Blanket Insulation.
D.	Section 07 60 00 - Flashing and Sheet Metal.
E.	Section 07 90 00 - Joint Protection.
1.3	REFERENCES
A.	American Architectural Manufacturer's Association (AAMA) 1402-86 - Aluminum Siding, Soffit, and Fascia.
B.	American Architectural Manufacturer's Association (AAMA) 1406-86 - Steel Siding, Soffit, and Fascia.
C.	American Society for Testing and Materials (ASTM) A653 - Steel Sheet, Zinc Coated (Galvanized) or Zinc-Iron Alloy (Galvannealed by the Hot Dip Process).
D.	American Society for Testing and Materials (ASTM) B209 - Aluminum and Aluminum-Alloy Sheet and Plate.
E.	American Society for Testing and Materials (ASTM) D226 - Asphalt-Saturated Organic Felt Used in Roofing and Waterproofing.
F.	American Society for Testing and Materials (ASTM) D256 - Determining the Izod Pendulum Impact Resistance of Plastics.
G.	American Society for Testing and Materials (ASTM) D635 - Rate of Burning and/or Extent and Time of Burning of Self-Supported Plastics in a Horizontal Position.
H.	American Society for Testing and Materials (ASTM) D638 - Tensile Properties of Plastics.
I.	American Society for Testing and Materials (ASTM) D648 - Deflection Temperature of Plastics Under Flexural Load in the Edgewise Position.
J.	American Society for Testing and Materials (ASTM) D696 - Coefficient of Linear Thermal Expansion of Plastics.
K.	American Society for Testing and Materials (ASTM) D790 - Flexural Properties of Unreinforced and Reinforced Plastics and Electrical Insulating Materials.
L.	American Society for Testing and Materials (ASTM) D1929 - Determining Ignition Temperature of Plastics.
M.	American Society for Testing and Materials (ASTM) D3679 - Rigid Polyvinyl Chloride (PVC) Siding.
N.	American Society for Testing and Materials (ASTM) D4216 - Rigid Poly (Vinyl Chloride) (PVC) and Related PVC and Chlorinated Poly (Vinyl Chloride) (CPVC) Building Products Compounds.
O.	American Society for Testing and Materials (ASTM) E84 - Surface Burning Characteristics of Building Materials.
P.	Underwriters Laboratories (UL) 94 - Test for Flammability of Plastic Materials.
Q.	Vinyl Siding Institute (VSI):  Vinyl Siding Installation, a How-To Guide.
1.4	SUBMITTALS
A.	Submit under provisions of Section 01 30 00.
B.	[ Product Data ]:  Manufacturer's data sheets on each product to be used, including:
1.	Material descriptions, dimensions, and profiles.
2.	Preparation instructions and recommendations.
3.	Storage and handling requirements and recommendations.
4.	Installation methods.
C.	Shop Drawings: Layout, dimensions, weatherproofing, penetrations, terminations, trim, and installation methods.
D.	Selection Samples:  For each finish product specified, two complete sets of color chips representing manufacturer's full range of available colors and patterns.
E.	Verification Samples:  For each finish product specified, two samples, 4 inches (102 mm) long minimum samples of siding and trim in selected finish and color.
1.5	QUALITY ASSURANCE
A.	Manufacturer Qualifications: Company with a minimum of 10 years' successful experience manufacturing aluminum, steel and vinyl siding.
B.	Design:  Panel system shall be fabricated and installed to comply with:
1.	Aluminum Panels:
a.	AAMA 1402.
b.	International Code Council-ES Legacy - Report No. 97-64.
c.	International Conference of Building Officials (ICBO):  Report No. 2027.
2.	Steel Panels:
a.	AAMA 1406.
b.	International Code Council-ES Legacy - Report No. 97-64.
c.	International Conference of Building Officials (ICBO):  Report No. 2027.
3.	Vinyl Panels:
a.	International Code Council-ESR - 1133.
b.	Canadian Construction Materials center (CCMC):  Report No. 06541-L.
c.	New York City Department of Building Material Equipment and Acceptance:  MEA 132-94-M.
d.	Federal Housing Administration (FHA), Department of Housing and Urban Development (HUD):  Minimum Property Standards.
1.6	DELIVERY, STORAGE, AND HANDLING
A.	Deliver siding in manufacturer's protective cartons and clearly labeled as to specific products contained.
B.	During delivery and storage keep siding cartons flat and supported along entire length.
C.	Store materials off ground, out of weather, in dry place. Provide ventilation.  Protect from falling objects and construction activities.
1.7	WARRANTY
A.	Upon Completion, provide a Lifetime limited, transferable warranty.  In the case of siding purchased by, or installed upon property owned by or in part by corporations, government entities or agencies, religious organizations, trusts, condominium or corporate housing arrangements, intangible legal entities or any other entity or organization capable of an infinite life, the warranty period will be fifty (50) years following the installation of the siding (prorated as indicated in the Warranty Transfer Schedule).
B.	Contact with Dissimilar Materials:  Direct contact of aluminum products with certain dissimilar materials, or contact with water runoff from dissimilar materials, is likely to result in corrosion.  Accordingly, care should be taken during installation to avoid such contact of aluminum with dissimilar materials, including: dissimilar metals (copper, zinc, steel, etc.), concrete, stucco, asbestos siding, pressure treated/pretreated lumber, masonry, corrosive non-metallic materials, and roofing materials or roofing systems containing metallic granules or strips.
PART 2    PRODUCTS
2.1	MANUFACTURERS
A.	Acceptable Manufacturer:  Gentek Building Products, Inc., which is located at: P. O.Box 110  ; Akron, OH 44309; Toll Free Tel: 800-548-4542; Fax: 330-922-2354; Email: Dhouston@alside.com; Web: www.gentekinc.com
B.	Substitutions:  Not permitted.
C.	Requests for substitutions will be considered in accordance with provisions of Section 01 60 00 - Product Requirements.
2.2	MATERIALS
A.	Aluminum:  Fabricate siding and trim from sheet aluminum complying ASTM B209, AA3000 Alloy with the following properties:
1.	Ultimate strength:	25 KSI (172MPa).
2.	Yield strength:  22 KSI (152 MPa).
3.	Modulus of elasticity:  10,000 KSI (68948 MPa).
4.	Coefficient of linear thermal expansion:  1.31 x 10 to the minus 5 inch/inch/degree F (2.39 x 10 to the minus 5 mm/mm/degree C).
5.	Melting range:  1175 to 1210 degrees F.  (635 to 654 degrees C).
B.	Steel:  Fabricate siding, fascia and trim from galvanized steel sheet with G90 galvanized coating complying ASTM A653 with the following properties:
1.	Ultimate strength:  45 - 55 KSI (310 -  379 MPa).
2.	Yield strength:	40 - 50 KSI (276 -  345 MPa).
3.	Modulus of elasticity:  29,500 KSI (203395 MPa).
4.	Coefficient of linear thermal expansion:  0.6 x 10 to the minus 5 inch/inch/degree F (1.09 x 10 to the minus 5 mm/mm/degree C.)
5.	Melting temperature:  2,700 degrees F.  (1,481 degrees C).
6.	Elongation:  25 percent.
C.	PVC:  Fabricate siding and trim from polyvinyl chloride (PVC) meeting ASTM D3679 requirements for compound class number 2 with the following properties:
1.	Tensile strength tested in accordance with ASTM D638:  6,700 PSI (46 MPa).
2.	Flexural strength tested in accordance with ASTM D790:  14,000 PSI (96 MPa).
3.	Modulus of elasticity tested in accordance with ASTM D638:  410,000 PSI (2827 MPa).
4.	Impact resistance tested in accordance with ASTM D256:
a.	At 32 degrees F (0 degrees C):  2.0 foot pounds per inch of notch.
b.	At 70 degrees F (21 degrees C):  3.6 foot pounds per inch of notch.
5.	Coefficient of linear thermal expansion tested in accordance with ASTM D696:  (2.9 x 10 to the minus 5 inch/inch/degree F.  (5.3 x 10 to the minus 5 mm/mm/degree C.)
6.	Deflection temperature when tested in accordance with ASTM D648 with 264 PSI (1820 kPa) load:  163 degrees F.  (73 degrees C.)
7.	Average maximum burn distance tested in accordance with ASTM D635:  0.8 inch.  (20 mm.)
8.	Average maximum burn time tested in accordance with ASTM D635:  5 seconds.
9.	Maximum ignition temperature tested in accordance with ASTM D1929:
a.	Flash ignition:  752 degrees F. (400 degrees C.).
b.	Self ignition:  860 degrees F. (460 degrees C).
10.	Flame spread tested in accordance with ASTM E84:  15 maximum.
11.	Smoke development tested in accordance with ASTM E84:  500 maximum.
D.	Polypropylene:  Fabricate siding and trim from polypropylene with the following properties:
1.	Tensile Strength:  2900 psi @ yield, per ASTM D 638.
2.	Windload:  160 mph, per ASTM 5206.
3.	Flexural Modulus:  190,000 psi, per ASTM D 790.
4.	Flexural Strength:  4,800 psi, per ASTM D 790.
5.	Notched Izod Impact:  2.0 ft-lbs/in @23 degrees C, per ASTM D256.
6.	Gardner Impact:  180 in-lbs @ 23 degrees C, per ASTM D 5420.
7.	Burn Rate:  Horizontal Burn Classified 11.66 MM/Minute, per ASTM D 635.
8.	Optical Density of Smoke:  240.4, per ASTM E 662.
2.3	VINYL SIDING PANELS
A.	Sequoia Select: Double 4 inch clapboard
1.	Dimensions:  8 inches (203 mm) exposed width by 150 inches (3810 mm) long with 3/4 inch (19mm) butt.
2.	Thickness:  0.046 inch.  (1.17 mm).
3.	Type:  Advantage lock system with double thick rolled over nail hem.
4.	Surface Finish:  Embossed cedar-grain texture.
5.	Color:  As selected from manufacturer's standard colors.
6.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Arcadian with BASF additives and modifiers for fade protection.
d.	Brownstone with BASF additives and modifiers for fade protection.
e.	Canyon Clay.
f.	Classic Brown with BASF additives and modifiers for fade protection.
g.	Colonial with BASF additives and modifiers for fade protection.
h.	Dover Gray.
i.	Flannel with BASF additives and modifiers for fade protection.
j.	Linen.
k.	Maize.
l.	Mist Blue.
m.	Pearl.
n.	Pebble.
o.	Sage.
p.	Sandalwood.
q.	Sandstone.
r.	Snow White.
s.	Venetian Red with BASF additives and modifiers for fade protection.
t.	Wicker.
B.	Sequoia Select:	Double 4-1/2 inch Dutch Lap.
1.	Dimensions:  9 inches (229 mm) exposed width by 145 inches (3683 mm) long with 3/4 inch (19 mm) butt.
2.	Thickness:  0.046 inch.  (1.17 mm).
3.	Type: Advantage lock system with double thick rolled over nail hem.
4.	Surface Finish:  Embossed cedar-grain texture.
5.	Color:  As selected from manufacturer's standard colors.
6.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Arcadian with BASF additives and modifiers for fade protection.
d.	Brownstone with BASF additives and modifiers for fade protection.
e.	Canyon Clay.
f.	Classic Brown with BASF additives and modifiers for fade protection.
g.	Colonial with BASF additives and modifiers for fade protection.
h.	Dover Gray.
i.	Flannel with BASF additives and modifiers for fade protection.
j.	Linen.
k.	Maize.
l.	Mist Blue.
m.	Pearl.
n.	Pebble.
o.	Sage.
p.	Sandalwood.
q.	Sandstone.
r.	Snow White.
s.	Venetian Red with BASF additives and modifiers for fade protection.
t.	Wicker.
C.	Sequoia Select:	Double 5 inch Clapboard.
1.	Dimensions:  10 inches (254 mm) exposed width by 144 inches (3658 mm) long with 3/4 inch (19 mm) butt.
2.	Thickness:  0.046 inch  (1.17 mm).
3.	Type: Advantage lock system with double thick rolled over nail hem.
4.	Surface Finish:  Embossed cedar-grain texture.
5.	Color:  As selected from manufacturer's standard colors.
6.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Arcadian with BASF additives and modifiers for fade protection.
d.	Brownstone with BASF additives and modifiers for fade protection.
e.	Canyon Clay.
f.	Classic Brown with BASF additives and modifiers for fade protection.
g.	Colonial with BASF additives and modifiers for fade protection.
h.	Dover Gray.
i.	Flannel with BASF additives and modifiers for fade protection.
j.	Linen.
k.	Maize.
l.	Mist Blue.
m.	Pearl.
n.	Pebble.
o.	Sage.
p.	Sandalwood.
q.	Sandstone.
r.	Snow White.
s.	Venetian Red with BASF additives and modifiers for fade protection.
t.	Wicker.
D.	Sequoia Select:  Double 5 inch Dutch Lap.
1.	Dimensions:  10 inches (254 mm) exposed width by 144 inches (3658 mm) long with 3/4 inch (19 mm) butt.
2.	Thickness:  0.046 inch (1.17 mm).
3.	Type:  Advantage lock system with double thick rolled over nail hem.
4.	Surface Finish:  Embossed cedar-grain texture.
5.	Color: As selected from manufacturer's standard colors.
6.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Arcadian with BASF additives and modifiers for fade protection.
d.	Brownstone with BASF additives and modifiers for fade protection.
e.	Canyon Clay.
f.	Classic Brown with BASF additives and modifiers for fade protection.
g.	Colonial with BASF additives and modifiers for fade protection.
h.	Dover Gray.
i.	Flannel with BASF additives and modifiers for fade protection.
j.	Linen.
k.	Maize.
l.	Mist Blue.
m.	Pearl.
n.	Pebble.
o.	Sage.
p.	Sandalwood.
q.	Sandstone.
r.	Snow White.
s.	Venetian Red with BASF additives and modifiers for fade protection.
t.	Wicker.
E.	Sequoia 16:  Double 4 inch Clapboard.
1.	Dimensions: 8 inches (203 mm) exposed width by 193 inches (4903 mm) long with 3/4 inch (19 mm) butt.
2.	Thickness:  0.046 inch (1.17 mm).
3.	Type:  Advantage lock system with double thick rolled over nail hem.
4.	Surface Finish:  Embossed cedar-grain texture.
5.	Color:  As selected from manufacturer's standard colors.
6.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Linen.
f.	Maize.
g.	Mist Blue.
h.	Pearl.
i.	Pebble.
j.	Sage.
k.	Sandalwood.
l.	Sandstone.
m.	Snow White.
n.	Wicker.
F.	Sequoia 16:  Double 5 inch Dutch Lap.
1.	Dimensions:  10 inches (254 mm) exposed width by 196 inches (4979 mm) long with 3/4 inch (19 mm) butt.
2.	Thickness:  0.046 inch  (1.17 mm).
3.	Type:	Advantage lock system with double thick rolled over nail hem.
4.	Surface Finish:  Embossed cedar-grain texture.
5.	Color:  As selected from manufacturer's standard colors.
6.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Linen.
f.	Maize.
g.	Mist Blue.
h.	Pearl.
i.	Pebble.
j.	Sage.
k.	Sandalwood.
l.	Sandstone.
m.	Snow White.
n.	Wicker.
G.	Sequoia Board & Batten:  7 inch Vertical.
1.	Dimensions:  7 inches (178 mm) exposed width by 120 inches (3048 mm) long with 2 inches (51 mm) wide batten.
2.	Thickness:  0.050 inch (1.27 mm).
3.	Surface Finish:  Embossed light roughsawn texture.
4.	Color:  As selected from manufacturer's standard colors.
5.	Color:
a.	Almond.
b.	Canyon Clay.
c.	Dover Gray.
d.	Pearl.
e.	Pebble.
f.	Sage.
g.	Sandalwood.
h.	Sandstone.
i.	Snow White.
j.	Wicker.
H.	Northern Forest:  Double 4 inch Clapboard.
1.	Dimensions:  8 inches (203 mm) exposed width by 150 inches (3810 mm) long with 5/8 inch (16 mm) butt.
2.	Thickness:  0.044 inch (1.12 mm).
3.	Surface finish:  Embossed light roughsawn texture.
4.	Color Appearance:  Variegated.
5.	Color:  As selected from manufacturer's standard colors.
6.	Color:
a.	Aspen.
b.	Birch.
c.	Cedar.
d.	Chestnut.
e.	Maple.
f.	Willow.
I.	Northern Forest:  Double 5 inch Clapboard.
1.	Dimensions:  10 inches (254 mm) exposed width by 144 inches (3658 mm) long with 5/8 inch (16 mm) butt.
2.	Thickness:  0.044 inch (1.12 mm).
3.	Surface finish:  Embossed light roughsawn texture.
4.	Color Appearance:  Variegated.
5.	Color:	As selected from manufacturer's standard colors.
6.	Color:
a.	Aspen.
b.	Birch.
c.	Cedar.
d.	Chestnut.
e.	Maple.
f.	Willow.
J.	Northern Forest:  Double 5 inch Dutch Lap.
1.	Dimensions:  10 inches (254 mm) exposed width by 144 inches (3658 mm) long with 1/2 inch (13 mm) butt
2.	Thickness:  0.044 inch (1.12 mm).
3.	Surface finish:  Embossed light roughsawn texture.
4.	Color Appearance:  Variegated.
5.	Color:  As selected from manufacturer's standard colors.
6.	Color:
a.	Aspen.
b.	Birch.
c.	Cedar.
d.	Chestnut.
e.	Maple.
f.	Willow.
K.	Northern Forest:  12 inch Vertical.
1.	Dimensions:  12 inches (305 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:  0.044 inch  (1.12 mm)
3.	Profile:  Grooves forming three 4 inches (102 mm) wide panels.
4.	Surface finish:  Embossed light roughsawn texture.
5.	Color Appearance:  Variegated.
6.	Color:  As selected from manufacturer's standard colors.
7.	Color:
a.	Aspen.
b.	Birch.
c.	Cedar.
d.	Chestnut.
e.	Maple.
f.	Willow.
L.	Signature Supreme:  Double 4 inch Clapboard.
1.	Dimensions:  8 inches (203 mm) exposed width by 150 inches (3810 mm) long with 1/2 inch (13 mm) butt and rolled edge nail hem.
2.	Thickness:  0.044 inch  (1.12 mm).
3.	Surface finish:  Embossed hardwood texture.
4.	Color:  As selected from manufacturer's standard colors.
5.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Linen.
f.	Maize.
g.	Mist Blue.
h.	Pearl.
i.	Pebble.
j.	Sage.
k.	Sandalwood.
l.	Sandstone.
m.	Snow White.
n.	Wicker.
M.	Signature Supreme:  Double 4 inch Dutch Lap.
1.	Dimensions:  8 inches (203 mm) exposed width by 150 inches (3810 mm) long with 1/2 inch (13 mm) butt and rolled edge nail hem.
2.	Thickness:  0.044 inch (1.12 mm).
3.	Surface finish:  Embossed hardwood texture.
4.	Color:  As selected from manufacturer's standard colors.
5.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Linen.
f.	Maize.
g.	Mist Blue.
h.	Pearl.
i.	Pebble.
j.	Sage.
k.	Sandalwood.
l.	Sandstone.
m.	Snow White.
n.	Wicker.
N.	Signature Supreme:  Double 5 inch Clapboard.
1.	Dimensions:  10 inches (254 mm) exposed width by 144 inches (3658 mm) long with 5/8 inch (16 mm) butt and rolled edge nail hem.
2.	Thickness:  0.044 inch (1.12 mm).
3.	Surface finish:  Embossed hardwood texture.
4.	Color:  As selected from manufacturer's standard colors.
5.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Linen.
f.	Maize.
g.	Mist Blue.
h.	Pearl.
i.	Pebble.
j.	Sage.
k.	Sandalwood.
l.	Sandstone.
m.	Snow White.
n.	Wicker.
O.	Signature Supreme:  Double 5 inch Dutch Lap.
1.	Dimensions:  10 inches (254 mm) exposed width by 144 inches (3658 mm) long with 1/2 inch (13 mm) butt and rolled edge nail hem.
2.	Thickness:  0.044 inch (1.12 mm).
3.	Surface finish:  Embossed hardwood texture.
4.	Color:  As selected from manufacturer's standard colors.
5.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Linen.
f.	Maize.
g.	Mist Blue.
h.	Pearl.
i.	Pebble.
j.	Sage.
k.	Sandalwood.
l.	Sandstone.
m.	Snow White.
n.	Wicker.
P.	Signature Supreme:  Single 8 inch Clapboard.
1.	Dimensions:	8 inches (203 mm) exposed width by 150 inches (3810 mm) long with 5/8 inch (16 mm) butt and rolled edge nail hem.
2.	Thickness:	0.044 inch (1.12 mm).
3.	Surface finish:  Embossed hardwood texture.
4.	Color:  As selected from manufacturer's standard colors.
5.	Color:  Snow white
Q.	Concord:  Double 4 inch Clapboard.
1.	Dimensions:  8 inches (203 mm) exposed width by 150 inches (3810 mm) long with 1/2 inch (13 mm) butt and rolled edge nail hem.
2.	Thickness:  0.042 inch  (1.07 mm)
3.	Surface finish:  Embossed light roughsawn texture.
4.	Color:  As selected from manufacturer's standard colors.
5.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Everglade.
f.	Linen.
g.	Maize.
h.	Mist Blue.
i.	Pearl.
j.	Pebble.
k.	Sage.
l.	Sandalwood.
m.	Sandstone.
n.	Snow white.
o.	Wicker.
R.	Concord:  Double 4 inch Dutch Lap.
1.	Dimensions:  8 inches (203 mm) exposed width by 150 inches (3810 mm) long with 1/2 inch (13 mm) butt and rolled edge nail hem.
2.	Thickness:  0.042 inch (1.07 mm).
3.	Surface finish: Embossed light roughsawn texture.
4.	Color:  As selected from manufacturer's standard colors.
5.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Everglade.
f.	Linen.
g.	Maize.
h.	Mist Blue.
i.	Pearl.
j.	Pebble.
k.	Sage.
l.	Sandalwood.
m.	Sandstone.
n.	Snow white.
o.	Wicker.
S.	Concord:  Double 5 inch Clapboard.
1.	Dimensions:  10 inches (254 mm) exposed width by 144 inches (3658 mm) long with 5/8 inch (16 mm) butt and rolled edge nail hem.
2.	Thickness:  0.042 inch (1.07 mm).
3.	Surface finish:  Embossed light roughsawn texture.
4.	Color:  As selected from manufacturer's standard colors.
5.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Everglade.
f.	Linen.
g.	Maize.
h.	Mist Blue.
i.	Pearl.
j.	Pebble.
k.	Sage.
l.	Sandalwood.
m.	Sandstone.
n.	Snow white.
o.	Wicker.
T.	Concord:  Double 5 inch Dutch Lap.
1.	Dimensions:  10 inches (254 mm) exposed width by 144 inches (3658 mm) long with 1/2 inch (13 mm) butt and rolled edge nail hem.
2.	Thickness:  0.042 inch (1.07 mm).
3.	Surface finish:  Embossed light roughsawn texture.
4.	Color:  As selected from manufacturer's standard colors.
5.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Everglade.
f.	Linen.
g.	Maize.
h.	Mist Blue.
i.	Pearl.
j.	Pebble.
k.	Sage.
l.	Sandalwood.
m.	Sandstone.
n.	Snow white.
o.	Wicker.
U.	Aurora:  Double 4 inch Clapboard.
1.	Dimensions:  8 inches (203 mm) exposed width by 150 inches (3810 mm) long with 1/2 inch (13 mm) butt and rolled edge nail hem.
2.	Thickness:  0.040 inch  (1.02 mm)
3.	Surface finish:  Embossed brushed texture.
4.	Color:  As selected from manufacturer's standard colors.
5.	Color:
a.	Almond.
b.	Canyon Clay.
c.	Linen.
d.	Maize.
e.	Pearl.
f.	Pebble.
g.	Sandalwood.
h.	Sandstone.
i.	Snow white.
V.	Aurora:	Double 4-1/2 inch Dutch Lap.
1.	Dimensions:  9 inches (229 mm) exposed width by 145 inches (3683 mm) long with 7/16 inch (11 mm) butt and rolled edge nail hem.
2.	Thickness:  0.040 inch  (1.02 mm)
3.	Surface finish:  Embossed brushed texture.
4.	Color:	As selected from manufacturer's standard colors.
5.	Color:
a.	Almond.
b.	Canyon Clay.
c.	Linen.
d.	Maize.
e.	Pearl.
f.	Pebble.
g.	Sandalwood.
h.	Sandstone.
i.	Snow white.
W.	Driftwood:  Double 4 inch Clapboard.
1.	Dimensions:  8 inches (203 mm) exposed width by 150 inches (3810 mm) long with 7/16 inch (11 mm) butt and rolled edge nail hem.
2.	Thickness:  0.040 inch (1.02 mm).
3.	Surface finish:	Embossed driftwood texture.
4.	Color:  As selected from manufacturer's standard colors.
5.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Linen.
f.	Maize.
g.	Pearl.
h.	Pebble.
i.	Sage.
j.	Sandalwood.
k.	Sandstone.
l.	Snow White.
m.	Wicker.
X.	Driftwood:  Double 4-1/2 inch Dutch Lap.
1.	Dimensions:  9 inches (229 mm) exposed width by 145 inches (3683 mm) long with 7/16 inch (11 mm) butt and rolled edge nail hem.
2.	Thickness: 0.040 inch  (1.02 mm)
3.	Surface finish:  Embossed driftwood texture.
4.	Color:  As selected from manufacturer's standard colors.
5.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Linen.
f.	Maize.
g.	Pearl.
h.	Pebble.
i.	Sage.
j.	Sandalwood.
k.	Sandstone.
l.	Snow White.
m.	Wicker.
Y.	Type:	Horizontal, triple panel siding with slotted attachment holes along top edge; Gentek Advantage III:  Triple 3 inch Clapboard.
1.	Dimensions:  9 inches (229 mm) exposed width by 145 inches (3683 mm) long with 1/2 inch (13 mm) butt.
2.	Thickness:  0.042 inch  (1.07 mm)
3.	Surface finish:  Embossed brushed texture.
4.	Color: As selected from manufacturer's standard colors.
5.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Linen.
f.	Maize.
g.	Mist Blue.
h.	Pearl.
i.	Pebble.
j.	Sage.
k.	Sandalwood.
l.	Sandstone.
m.	Snow White.
n.	Wicker.
Z.	Type: Berkshire Beaded:  Single 6-1/2 inch Beaded.
1.	Dimensions:  6.5 inches (165 mm) exposed width by 147-3/4 inches (3753 mm) long with 9/16 inch (14 mm) butt.
2.	Thickness:  0.046 inch (1.17 mm).
3.	Profile:  Horizontal siding panel with half-round decorative bead at the bottom edge.
4.	Surface finish:  Embossed brushed texture.
5.	Color:  As selected from manufacturer's standard colors.
6.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Linen.
f.	Maize.
g.	Mist Blue.
h.	Pearl.
i.	Pebble.
j.	Sage.
k.	Sandalwood.
l.	Sandstone.
m.	Snow White.
n.	Wicker.
2.4	POLYPROPYLENE SIDING PANELS
A.	Fairhaven Sound Double 7 inch Shake.
1.	Dimensions:  14 inches exposed width by 48 inches long with 1/2 inch (12.7 mm) butt height.
2.	Thickness:  .100 inch (2.5 mm).
3.	Surface finish:  Natural cedar texture
4.	Color:  As selected from manufacturer's standard colors.
5.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Linen.
f.	Maize.
g.	Pearl.
h.	Pebble.
i.	Sage.
j.	Sandstone.
k.	Snow White.
l.	Wicker.
m.	Classic Brown.
n.	Venetian Red.
B.	Fairhaven Sound double 6 3/8 inch Scallop.
1.	Dimensions:  12 3/4 inches (324 mm) exposed width by 35 inches (889 mm) long with 3/8 inch (9.5 mm) butt height.
2.	Thickness:  .100 inch (2.5 mm).
3.	Surface finish:  Natural cedar texture
4.	Color:  As selected from manufacturer's standard colors.
5.	Color:
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Linen.
f.	Maize.
g.	Pearl.
h.	Pebble.
i.	Sage.
j.	Sandstone.
k.	Snow White.
l.	Wicker.
m.	Classic Brown.
n.	Venetian Red.
2.5	VINYL  SOFFIT PANELS
A.	Advantage Plus Premium:  Triple 4 Inch.
1.	Dimensions:	12 inches (305 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:  0.042 inch.  (1.07 mm.)
3.	Profile:  V-grooves forming three panels.
4.	Surface finish:  Embossed brushed texture.
a.	Color:  Snow White.
B.	Advantage Plus Premium:  Triple 4 Inch.
1.	Dimensions:  12 inches (305 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:  0.042 inch (1.07 mm).
3.	Profile:  V-grooves forming three panels and center panel provided with vent perforations.
4.	Net free open area:  1.9 square inches per linear foot (40 square cm per meter).
5.	Surface finish:  Embossed brushed texture.
a.	Color:  Snow White.
C.	Advantage Plus Premium:  Triple 4 Inch.
1.	Dimensions:  12 inches (305 mm) exposed width by 144 inches (3858 mm) long.
2.	Thickness:  0.042 inch (1.07 mm).
3.	Profile:  V-grooves forming three panels and all panels provided with vent perforations.
4.	Net free open area:	5.8 square inches per linear foot (123 square cm per meter).
5.	Surface finish:  Embossed brushed texture.
a.	Color:  Snow White.
D.	Oxford Premium:  Double 5 inch.
1.	Dimensions:  10 inches (254 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:  0.042 inch (1.07 mm).
3.	Profile:  V-groove forming two panels.
4.	Surface finish:  Embossed light roughsawn texture.
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Linen.
f.	Maize.
g.	Mist Blue.
h.	Pearl.
i.	Pebble.
j.	Sage.
k.	Sandalwood.
l.	Sandstone.
m.	Snow White.
n.	Wicker.
E.	Oxford Premium:  Double 5 inch.
1.	Dimensions:  10 inches (254 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness: 0.042 inch (1.07 mm).
3.	Profile:  V-groove forming two panels and all panels provided with vent perforations.
4.	Net free open area:  5.3 square inches per linear foot (112 square cm per meter).
5.	Surface finish:  Embossed light roughsawn texture.
a.	Almond.
b.	Antique Ivory.
c.	Canyon Clay.
d.	Dover Gray.
e.	Linen.
f.	Maize.
g.	Mist Blue.
h.	Pearl.
i.	Pebble.
j.	Sage.
k.	Sandalwood.
l.	Sandstone.
m.	Snow White.
n.	Wicker.
F.	Beaded Premium:
1.	Dimensions:  8 inches (203 mm) exposed width by 150 inches (3810 mm) long.
2.	Thickness:  0.042 inch (1.07 mm).
3.	Profile:  Two beaded corrugations forming three equal panels.
4.	Surface finish:  Matte texture.
a.	Color:  Canyon Clay.
b.	Color:	Linen.
c.	Color:  Pebble.
d.	Color:  Sandalwood.
e.	Color:  Snow White.
f.	Color:  Wicker.
G.	Beaded Premium:
1.	Dimensions:  8 inches (203 mm) exposed width by 150 inches) (3810 mm) long.
2.	Thickness:  0.042 inch (1.07 mm.).
3.	Profile:  Two beaded corrugations with vent perforations and forming three equal panels.
4.	Net free open area:  2.4 square inches per linear foot) (51 square cm per meter).
5.	Surface finish:  Matte texture.
a.	Color:  Canyon Clay.
b.	Color:  Linen.
c.	Color:  Pebble.
d.	Color:  Sandalwood.
e.	Color:  Snow White.
f.	Color:  Wicker.
H.	Fairweather Soffit: Triple 4 Inch.
1.	Dimensions: 12 inches (305 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:  0.040 inch (1.02 mm).
3.	Profile:  V-grooves forming three panels.
4.	Surface finish:  Embossed brushed texture.
a.	Almond.
b.	Antique Ivory.
c.	Brownstone.
d.	Canyon Clay.
e.	Dover Gray.
f.	Everglade.
g.	Linen.
h.	Maize.
i.	Mist Blue.
j.	Pearl.
k.	Pebble.
l.	Sage.
m.	Sandalwood.
n.	Sandstone.
o.	Snow White.
p.	Wicker.
I.	Fairweather Soffit: Triple 4 Inch.
1.	Dimensions:  12 inches (305 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:	0.040 inch (1.02 mm).
3.	Profile:  V-grooves forming three panels and center panel provided with vent perforations.
4.	Net free open area:  1.9 square inches per linear foot (40 square cm per meter).
5.	Surface finish:  Embossed brushed texture.
a.	Almond.
b.	Antique Ivory.
c.	Brownstone.
d.	Canyon Clay.
e.	Dover Gray.
f.	Everglade.
g.	Linen.
h.	Maize.
i.	Mist Blue.
j.	Pearl.
k.	Pebble.
l.	Sage.
m.	Sandalwood.
n.	Sandstone.
o.	Snow White.
p.	Wicker.
J.	Fairweather Soffit:  Triple 4 Inch.
1.	Dimensions:  12 inches (305 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:  0.040 inch (1.02 mm).
3.	Profile:	V-grooves forming three panels and all panels provided with vent perforations.
4.	Net free open area:  5.8 square inches per linear foot (123 square cm per meter).
5.	Surface finish:  Embossed brushed texture.
a.	Almond.
b.	Antique Ivory.
c.	Brownstone.
d.	Canyon Clay.
e.	Dover Gray.
f.	Everglade.
g.	Linen.
h.	Maize.
i.	Mist Blue.
j.	Pearl.
k.	Pebble.
l.	Sage.
m.	Sandalwood.
n.	Sandstone.
o.	Snow White.
p.	Wicker.
2.6	TRIM
A.	Standard Accessories:
1.	Consistent with shape, size, and properties shown on the drawings and as required for complete installation.
2.	Produced from the same compound materials and with comparable properties as the siding.
3.	Color:  Matching or color coordinated with siding.
B.	Trim Essentials Decorative Vinyl Accessories:
1.	Outside corner post:
a.	6 inches (152 mm) designer.
b.	6-5/8 inches (168 mm) beaded with foam insert.
c.	5-3/4 (146 mm) inch fluted.
2.	2 inches (51 mm) quarter round beaded corner starter.
3.	2-1/2 inches (64 mm) wide face J-channel.
4.	Window and Door Surround:
a.	3-1/2 (89 mm) inch.
b.	5 inch (127 mm).
c.	5 inch (127 mm) fluted.
d.	Surround starter.
5.	Soffit crown molding.
6.	45 degree bay/bow corner.
7.	3-1/2 inches (89 mm) H-trim.
8.	Color:  Matching or color coordinated with siding.
2.7	ALUMINUM SIDING PROFILE
A.	Cedarwood:  Double 5 inch Clapboard.
1.	Dimensions:  10 inches (254 mm) exposed width by 144 inches (3658 mm) long with 1/2 inch (13 mm) butt.
2.	Thickness:  0.024 inch (0.61 mm).
3.	Surface:  Wood-grain texture.
4.	Finish:	Fluoropolymer thermoplastic polymer coating with 70 percent PVDF2, cured at 475 degrees F (246 degrees C), and meeting Kynar 500/Hylar 5000 specifications.
a.	Pattern:  Variegated paint pattern with intertwining natural hues in random patterns.
b.	Color:   Aspen Gray.
c.	Color:   Chestnut Brown.
d.	Color:   Maple Tan.
e.	Color:   Tawny Oak.
B.	Woodgrain Series 2000:  Double 4 inch Clapboard.
1.	Dimensions:  8 inches (203 mm) exposed width by 150 inches (3810 mm) long with 1/2 inch (13 mm) butt.
2.	Thickness:  0.019 inch (0.48 mm).
3.	Surface:  Wood-grain texture.
4.	Finish:  Polyester thermoset coating cured at 450 degrees F (232 degrees C).
a.	Color:   Bright White.
b.	Color:   Almond.
c.	Color:   Antique Ivory.
d.	Color:  Canyon Clay.
e.	Color:  Dover Gray.
f.	Color:  Sandstone.
g.	Color:  Wicker.
C.	Deluxe:  Double 4 inch Clapboard.
1.	Dimensions:  8 inches (203 mm) exposed width by 150 inches (3810 mm) long with 1/2 inch (13 mm) butt.
2.	Thickness:  0.019 inch (0.48 mm).
3.	Surface:  Smooth.
4.	Finish:  Polyester thermoset coating cured at 450 degrees F (232 degrees C).
a.	Color:	 Bright White.
D.	Deluxe:  Single 8 inch Clapboard.
1.	Dimensions:  8 inches (203 mm) exposed width by 150 inches (3810 mm) long with 1/2 inch (13 mm) butt.
2.	Thickness:  0.024 inch (0.61 mm).
3.	Surface:  Smooth.
4.	Finish:  Polyester thermoset coating cured at 450 degrees F (232 degrees C).
a.	Color:   Bright White.
2.8	ALUMINUM SOFFIT PANELS
A.	Supreme Soffit:  Quad 4 inch
1.	Dimensions:	16 inches (406.4 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:  0.016 inch  (0.41 mm).
3.	Profile:  V-grooves forming four 4 inches (102 mm) panels.
4.	Surface:	Striated texture.
5.	Finish:  PVC thermoplastic polymer coating melted and fused on aluminum at 360 degrees F (182 degrees C).
a.	Color:  Bright White.
b.	Color:  Brownstone.
c.	Color:  Antique Ivory.
d.	Color:  Classic Brown.
e.	Color:  Grecian Green.
f.	Color:  London Brown.
g.	Color:  Sage.
h.	Color:  Venetian Red.
B.	Supreme Soffit:  Quad 4 inch.
1.	Dimensions:  16 inches (406.4 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:  0.016 inch (0.41 mm).
3.	Profile:  V-grooves forming four 4 inches (102 mm) panels with two center panels perforated.
4.	Net free open area:  7.8 square inches per linear foot (165 square cm per meter).
5.	Surface:  Striated texture.
6.	Finish:  PVC thermoplastic polymer coating melted and fused on aluminum at 360 degrees F (182 degrees C).
a.	Color:  Bright White.
b.	Color:  Brownstone.
c.	Color:  Antique Ivory.
d.	Color:  Classic Brown.
e.	Color:  Grecian Green.
f.	Color:  London Brown.
g.	Color:  Sage.
h.	Color:  Venetian Red.
C.	Supreme Soffit:  Quad 4 inch.
1.	Dimensions:  16 inches (406.4 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:	0.016 inch (0.41 mm).
3.	Profile:  V-grooves forming four 4 inches (102 mm) panels, all panels provided with vent perforations.
4.	Net free open area:  15.5 square inches per linear foot (328.1 square cm per meter).
5.	Surface: Striated texture.
6.	Finish:  PVC thermoplastic polymer coating melted and fused on aluminum at 360 degrees F (182 degrees C).
a.	Color:  Bright White.
b.	Color:  Brownstone.
c.	Color:  Antique Ivory.
d.	Color:  Classic Brown.
e.	Color:  Grecian Green.
f.	Color:  London Brown.
g.	Color:  Sage.
h.	Color:  Venetian Red.
D.	Hi-Tensile Soffit:  Triple 4 inch.
1.	Dimensions:  12 inches (304 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:  0.016 inch (0.41 mm).
3.	Profile:  V-grooves forming three 4 inches (102) wide panels.
4.	Surface:  Smooth.
5.	Finish: Polyester thermoset coating cured at 450 degrees F (232 degrees C).
a.	Color:  Bright White.
b.	Color:  Almond.
c.	Color:  Antique Ivory.
d.	Color:  Brown.
e.	Color:  Brownstone.
f.	Color:  Canyon Clay.
g.	Color:  Dover Gray.
h.	Color:  Grecian Green.
i.	Color:  Linen.
j.	Color:  London Brown.
k.	Color:  Norwood.
l.	Color:	Pebble.
m.	Color:  Royal Brown.
n.	Color:  Sage.
o.	Color:  Sandalwood.
p.	Color:  Sandstone.
q.	Color:  Terratone.
r.	Color:  Thistle.
s.	Color:  White.
t.	Color:  Wicker.
E.	Hi-Tensile Soffit:  Triple 4 inch.
1.	Dimensions:  12 inches (305 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:  0.016 inch (0.41 mm).
3.	Profile:  V-grooves forming three 4 inches (102) wide panels with center panel vented.
4.	Net free open area:  3.9 square inches per linear foot (83 square cm per meter).
5.	Surface:	Smooth.
6.	Finish: Polyester thermoset coating cured at 450 degrees F (232 degrees C).
a.	Color:  Bright White.
b.	Color:  Almond.
c.	Color:  Antique Ivory.
d.	Color:  Brown.
e.	Color:  Brownstone.
f.	Color:  Canyon Clay.
g.	Color:  Dover Gray.
h.	Color:  Grecian Green.
i.	Color:  Linen.
j.	Color:	London Brown.
k.	Color:  Norwood.
l.	Color:  Pebble.
m.	Color:  Royal Brown.
n.	Color:  Sage.
o.	Color:  Sandalwood.
p.	Color:  Sandstone.
q.	Color:  Terratone.
r.	Color:  Thistle.
s.	Color:  White.
t.	Color:  Wicker.
F.	Hi-Tensile Soffit:  Triple 4 inch.
1.	Dimensions:  12 inches (305 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:  0.016 inch (0.41 mm).
3.	Profile:  V-grooves forming three 4 inches (102) wide panels with all panels vented.
4.	Net free open area:  11.6 square inches per linear foot (245 square cm per meter).
5.	Surface:  Smooth.
6.	Finish: Polyester thermoset coating cured at 450 degrees F (232 degrees C).
a.	Color:  Bright White.
b.	Color:  Almond.
c.	Color:  Antique Ivory.
d.	Color:  Brown.
e.	Color:  Brownstone.
f.	Color:  Canyon Clay.
g.	Color:  Dover Gray.
h.	Color:  Grecian Green.
i.	Color:  Linen.
j.	Color:  London Brown.
k.	Color:  Norwood.
l.	Color:  Pebble.
m.	Color:  Royal Brown.
n.	Color:  Sage.
o.	Color:  Sandalwood.
p.	Color:  Sandstone.
q.	Color:  Terratone.
r.	Color: Thistle.
s.	Color:  White.
t.	Color:  Wicker.
G.	Hi-Tensile Soffit:  Double 6 inch.
1.	Dimensions:  12 inches (305 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:  0.016 inch (0.41 mm).
3.	Profile:  V-groove forming two 6 inches (152 mm) wide panels.
4.	Surface:  Smooth.
5.	Finish: Polyester thermoset coating cured at 450 degrees F (232 degrees C).
a.	Color:  Bright White.
b.	Color:  Almond.
c.	Color:  Antique Ivory.
d.	Color:  Brown.
e.	Color:  Brownstone.
f.	Color:  Canyon Clay.
g.	Color:  Dover Gray.
h.	Color:	Grecian Green.
i.	Color:  Linen.
j.	Color:	London Brown.
k.	Color:  Norwood.
l.	Color:  Pebble.
m.	Color:  Royal Brown.
n.	Color:  Sage.
o.	Color:	Sandalwood.
p.	Color:  Sandstone.
q.	Color:  Terratone.
r.	Color:  Thistle.
s.	Color:  White.
t.	Color:  Wicker.
H.	Hi-Tensile Soffit:  Double 6 inch.
1.	Dimensions:  12 inches (305 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:  0.016 inch (0.41 mm).
3.	Profile:  Single V-groove forming two 6 inches (152 mm) wide panels with all panels vented.
4.	Net free open area:  7.2 square inches per linear foot (152 square cm per meter).
5.	Surface:  Smooth.
6.	Finish: Polyester thermoset coating cured at 450 degrees F (232 degrees C).
a.	Color:  Bright White.
b.	Color:  Almond.
c.	Color:  Antique Ivory.
d.	Color:  Brown.
e.	Color:  Brownstone.
f.	Color:  Canyon Clay.
g.	Color:  Dover Gray.
h.	Color:  Grecian Green.
i.	Color:  Linen.
j.	Color:  London Brown.
k.	Color:  Norwood.
l.	Color:  Pebble.
m.	Color:  Royal Brown.
n.	Color:  Sage.
o.	Color:  Sandalwood.
p.	Color:  Sandstone.
q.	Color:  Terratone.
r.	Color:  Thistle.
s.	Color:  White.
t.	Color:  Wicker.
I.	Hi-Tensile Soffit:	Quad 4 inch.
1.	Dimensions:  16 inches (406 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:  0.016 inch (0.41 mm).
3.	Profile:  V-grooves forming four equal width panels.
4.	Surface:  Smooth.
5.	Finish: Polyester thermoset coating cured at 450 degrees F (232 degrees C).
a.	Color:  Bright White.
b.	Color:  Almond.
c.	Color:  Antique Ivory.
d.	Color:  Brown.
e.	Color:  Brownstone.
f.	Color:  Canyon Clay.
g.	Color:  Charcoal.
h.	Color:  Dover Gray.
i.	Color:  Grecian Green.
j.	Color:  Linen.
k.	Color:  London Brown.
l.	Color:  Norwood.
m.	Color:  Pebble.
n.	Color:  Royal Brown.
o.	Color:  Sage.
p.	Color:  Sandalwood.
q.	Color:  Sandstone.
r.	Color:  Terratone.
s.	Color:  Thistle.
t.	Color:  White.
u.	Color:  Wicker.
J.	Hi-Tensile Soffit:  Quad 4 inch.
1.	Dimensions:  16 inches (406 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:	0.016 inch (0.41 mm).
3.	Profile:	V-grooves forming four equal width panels with center panel vented.
4.	Net free open area:  7.8 square inches per linear foot (165 square cm per meter).
5.	Surface:  Smooth.
6.	Finish: Polyester thermoset coating cured at 450 degrees F (232 degrees C).
a.	Color:  Bright White.
b.	Color:  Almond.
c.	Color:  Antique Ivory.
d.	Color:  Brown.
e.	Color:  Brownstone.
f.	Color:  Canyon Clay.
g.	Color:  Charcoal.
h.	Color:  Dover Gray.
i.	Color:  Grecian Green.
j.	Color:  Linen.
k.	Color:  London Brown.
l.	Color:	Norwood.
m.	Color:  Pebble.
n.	Color:  Royal Brown.
o.	Color:  Sage.
p.	Color:  Sandalwood.
q.	Color:  Sandstone.
r.	Color:  Terratone.
s.	Color:  Thistle.
t.	Color:  White.
u.	Color:  Wicker.
K.	Hi-Tensile Soffit:  Quad 4 inch.
1.	Dimensions: 16 inches (406 mm) exposed width by 144 inches (3658 mm) long.
2.	Thickness:  0.016 inch (0.41 mm).
3.	Profile: V-grooves forming four equal width panels with all panels vented.
4.	Net free open area:  15.5 square inches per linear foot (328 square cm per meter).
5.	Surface:  Smooth.
6.	Finish: Polyester thermoset coating cured at 450 degrees F (232 degrees C).
a.	Color:  Bright White.
b.	Color:	Almond.
c.	Color:  Antique Ivory.
d.	Color:  Brown.
e.	Color:  Brownstone.
f.	Color:  Canyon Clay.
g.	Color:  Charcoal.
h.	Color:  Dover Gray.
i.	Color:  Grecian Green.
j.	Color:  Linen.
k.	Color:  London Brown.
l.	Color:  Norwood.
m.	Color:  Pebble.
n.	Color:  Royal Brown.
o.	Color:  Sage.
p.	Color:  Sandalwood.
q.	Color:  Sandstone.
r.	Color:  Terratone.
s.	Color:  Thistle.
t.	Color:  White.
u.	Color:  Wicker.
2.9	ALUMINUM FASCIA PANELS
A.	Type:  4 inches (102 mm) wide by 150 inches (3810 mm) long aluminum fascia panel; Gentek Fascia Cover as provided by Gentek Building Products.
1.	Thickness:  0.024 inch.  (0.61 mm).
2.	Profile:  Angle shape with 1 inch (25 mm) attachment flange along bottom and two pairs of horizontal half-round ribs on face.
3.	Surface:  Smooth.
4.	Finish: Polyester thermoset coating cured at 450 degrees F (232 degrees C).
a.	Color:  Bright White.
B.	Type:  6 inches (152 mm) wide by 150 inches (3810 mm) long aluminum fascia panel; Gentek Fascia Cover as provided by Gentek Building Products.
1.	Thickness:  0.024 inch (0.61 mm.)
2.	Profile:  Angle shape with 1 inch (25 mm) attachment flange along bottom and three pairs of horizontal half-round ribs on face.
3.	Surface: Smooth.
4.	Finish: Polyester thermoset coating cured at 450 degrees F (232 degrees C).
a.	Color:  Bright White.
b.	Color:  Almond.
c.	Color:	Antique Ivory.
d.	Color:  Brown.
e.	Color:  Brownstone.
f.	Color:  Canyon Clay.
g.	Color:  Dover Gray.
h.	Color:  Grecian Green.
i.	Color:  Linen.
j.	Color:  London Brown.
k.	Color:	Norwood.
l.	Color:  Pebble.
m.	Color:  Royal Brown.
n.	Color:  Sage.
o.	Color:  Sandalwood.
p.	Color:  Sandstone.
q.	Color:  Terratone.
r.	Color:	Thistle.
s.	Color:  White.
t.	Color:  Wicker.
C.	Type:  8 inches (203 mm) wide by 150 inches (3810 mm) long aluminum fascia panel; Gentek Fascia Cover as provided by Gentek Building Products.
1.	Thickness:  0.024 inch (0.61 mm).
2.	Profile:  Angle shape with 1 inch) (25 mm) attachment flange along bottom and three pairs of horizontal half-round ribs on face.
3.	Surface:  Smooth.
4.	Finish: Polyester thermoset coating cured at 450 degrees F (232 degrees C).
a.	Color:  Bright White.
b.	Color:  Almond.
c.	Color:  Antique Ivory.
d.	Color:	Brown.
e.	Color:  Brownstone.
f.	Color:  Canyon Clay.
g.	Color:  Dover Gray.
h.	Color:  Grecian Green.
i.	Color:  London Brown.
j.	Color:  Norwood.
k.	Color:  Pebble.
l.	Color:  Royal Brown.
m.	Color:  Sage.
n.	Color:  Sandalwood.
o.	Color:  Sandstone.
p.	Color:  Terratone.
q.	Color:  White.
r.	Color:  Wicker.
2.10	TRIM
A.	Standard Accessories:
1.	Consistent with shape, size, and properties shown on the drawings and as required for complete installation.
2.	Produced from the same compound materials and with comparable properties as the siding.
3.	Color:  Matching or color coordinated with siding.
2.11	STEEL SIDING PANELS
A.	Steeltek:  Double 4 inch Clapboard.
1.	Dimensions:  8 inches (203 mm) exposed width by 150 inches (3810 mm) long with 1/2 inch (13 mm) butt.
2.	Thickness:  0.017 inch (0.43 mm) (29 gauge).
3.	Surface:  Wood-grain texture.
4.	Finish:  PVC thermoplastic polymer coating melted and fused on steel at 360 degrees F (182 degrees C).
a.	Color:  Bright White.
b.	Color:  Almond.
c.	Color:  Antique Ivory.
d.	Color:  Brownstone.
e.	Color:  Canyon Clay.
f.	Color:  Dover Gray.
g.	Color:  Norwood.
h.	Color:  Sage.
i.	Color:  Thistle.
j.	Color:  Wicker.
B.	Steeltek:  Single 8 inch Clapboard.
1.	Dimensions: 8 inches (203 mm) exposed width by 150 inches (3810 mm) with 1/2 inch (13 mm) butt.
2.	Thickness:  0.017 inch (0.43 mm) (29 gauge).
3.	Surface:  Wood-grain texture.
4.	Finish:  PVC thermoplastic polymer coating melted and fused on steel at 360 degrees F (182 degrees C).
a.	Color:  Bright White.
b.	Color:	Almond.
c.	Color:  Antique Ivory.
d.	Color:  Brownstone.
e.	Color:  Canyon Clay.
f.	Color:  Dover Gray.
g.	Color:  Norwood.
h.	Color:  Sage.
i.	Color:	Thistle.
j.	Color:  Wicker.
C.	Steelside:  Double 5 inch Clapboard.
1.	Dimensions:  10 inches (254 mm) exposed width by 144 inches (3658 mm) long with 1/2 inch (13 mm) butt.
2.	Thickness:  0.017 inch.  (0.43 mm).
3.	Surface:  Wood-grain texture.
4.	Finish:  PVC thermoplastic polymer coating melted and fused on steel at 360 degrees F (182 degrees C).
a.	Color:  Bright White.
b.	Color:  Almond.
c.	Color:  Antique Ivory.
d.	Color:  Brownstone.
e.	Color:  Canyon Clay.
f.	Color:  Dover Gray.
g.	Color:  Norwood.
h.	Color:  Sage.
i.	Color:  Thistle.
j.	Color:  Wicker.
D.	Steelside:  Single 8 inch Clapboard.
1.	Dimensions:  8 inches (203 mm) exposed width by 150 inches (3810 mm) long with 1/2 inch (13 mm) butt.
2.	Thickness:  0.017 inch.  (0.43 mm).
3.	Surface:  Wood-grain texture.
4.	Finish:  PVC thermoplastic polymer coating melted and fused on steel at 360 degrees F (182 degrees C).
a.	Color:  Bright White.
b.	Color:  Almond.
c.	Color:  Antique Ivory.
d.	Color:	Brownstone.
e.	Color:  Canyon Clay.
f.	Color:  Dover Gray.
g.	Color:  Norwood.
h.	Color:  Sage.
i.	Color:  Thistle.
j.	Color:  Wicker.
E.	Driftwood:  Double 5 inch Clapboard.
1.	Dimensions:  10 inches (254 mm) exposed width by 144 inches (3658 mm) long with 1/2 inch (13 mm) butt.
2.	Thickness:  0.017 inch.  (0.43 mm).
3.	Surface:  Wood-grain texture.
4.	Finish:  PVC thermoplastic polymer coating melted and fused on steel at 360 degrees F (182 degrees C).
a.	Color:  Poplar.
b.	Color:  Southern Pecan.
c.	Color:  Sycamore.
d.	Color:  Winter Oak.
F.	Driftwood:  Single 8 inch Clapboard.
1.	Dimensions:  8 inches (203 mm) exposed width by 150 inches (3810 mm) long with 1/2 inch (13 mm) butt.
2.	Thickness:  0.017 inch.  (0.43 mm).
3.	Surface:  Wood-grain texture.
4.	Finish:	PVC thermoplastic polymer coating melted and fused on steel at 360 degrees F (182 degrees C).
a.	Color:  Poplar.
b.	Color:  Southern Pecan.
c.	Color:  Sycamore.
d.	Color:  Winter Oak.
G.	Universal:  Double 5 inch Dutch Lap.
1.	Dimensions:  10 inches (254 mm) exposed width by 144 inches (3658 mm) long with 1/2 inch (13 mm) butt.
2.	Thickness:  0.017 inch  (0.43 mm).
3.	Surface:  Wood-grain texture.
4.	Finish:  PVC thermoplastic polymer coating melted and fused on steel at 360 degrees F (182 degrees C).
a.	Color:  Bright White.
b.	Color:  Almond.
c.	Color:  Antique Ivory.
d.	Color:  Brownstone.
e.	Color:	Canyon Clay.
f.	Color:  Dover Gray.
g.	Color:  Norwood.
h.	Color:  Sage.
i.	Color:  Thistle.
j.	Color:  Wicker.
H.	Vertical Board and Batten:  12 inch Vertical.
1.	Dimensions:  12 inches (305 mm) exposed width by 120 inches (3048 mm) long with 2 inches (51 mm) wide batten.
2.	Thickness:  0.017 inch.  (0.43 mm).
3.	Surface:  Medium wood-grain texture.
4.	Finish:  PVC thermoplastic polymer coating melted and fused on steel at 360 degrees F (182 degrees C).
a.	Color:  Bright White.
b.	Color:  Almond.
c.	Color:  Antique Ivory.
d.	Color:  Brownstone.
e.	Color:  Canyon Clay.
f.	Color:  Dover Gray.
g.	Color:	Norwood.
h.	Color:  Sage.
i.	Color:  Thistle.
j.	Color:  Wicker.
2.12	STEEL FASCIA PANELS
A.	Type:  4 inches (102 mm) wide by 120 inches (3048 mm) long steel fascia panel; Gentek Fascia Cover as provided by Gentek Building Products.
1.	Thickness:  0.017 inch (0.43 mm).
2.	Profile:  Angle shape with 1 inch (25 mm) attachment flange along bottom and two horizontal half-round ribs on face.
3.	Surface: Wood-grain texture.
4.	Finish:  PVC thermoplastic polymer coating melted and fused on steel at 360 degrees F (182 degrees C).
a.	Color:  Bright White.
b.	Color:  Almond.
c.	Color:  Antique Ivory.
d.	Color:  Brownstone.
e.	Color:  Canyon Clay.
f.	Color:  Dover Gray.
g.	Color:  London Brown.
h.	Color: Norwood.
i.	Color:  Sage.
j.	Color:  Thistle.
k.	Color:  Wicker.
B.	Type: 6 inches (152 mm) wide by 120 inches (3048 mm) long steel fascia panel; Gentek Fascia Cover as provided by Gentek Building Products.
1.	Thickness:  0.017 inch (0.43 mm).
2.	Profile:  Angle shape with 1 inch (25 mm) attachment flange along bottom and three horizontal half-round ribs on face.
3.	Surface:  Wood-grain texture.
4.	Finish:  PVC thermoplastic polymer coating melted and fused on steel at 360 degrees F (182 degrees C).
a.	Color:  Bright White.
b.	Color:  Almond.
c.	Color:  Antique Ivory.
d.	Color:  Brownstone.
e.	Color: Canyon Clay.
f.	Color:  Dover Gray.
g.	Color:	London Brown.
h.	Color:  Norwood.
i.	Color:  Sage.
j.	Color:	Thistle.
k.	Color:  Wicker.
C.	Type: 8 inches (203 mm) wide by 120 inches (3048 mm) long steel fascia panel; Gentek Fascia Cover as provided by Gentek Building Products.
1.	Thickness:  0.017 inch (0.43 mm).
2.	Profile:  Angle shape with 1 inch (25 mm) attachment flange along bottom and four horizontal half-round ribs on face.
3.	Surface:  Wood-grain texture.
4.	Finish:  PVC thermoplastic polymer coating melted and fused on steel at 360 degrees F (182 degrees C).
a.	Color:	Bright White.
b.	Color:  Almond.
c.	Color:  Antique Ivory.
d.	Color:  Brownstone.
e.	Color:  Canyon Clay.
f.	Color:  Dover Gray.
g.	Color:  London Brown.
h.	Color:  Norwood.
i.	Color: Sage.
j.	Color:  Thistle.
k.	Color:  Wicker.
D.	Type:  10 inches (203 mm) wide by 120 inches (3048 mm) long steel fascia panel; Gentek Fascia Cover as provided by Gentek Building Products.
1.	Thickness:  0.017 inch (0.43 mm).
2.	Profile:  Angle shape with 1 inch (25 mm) attachment flange along bottom and five horizontal half-round ribs on face.
3.	Surface:  Wood-grain texture.
4.	Finish:  PVC thermoplastic polymer coating melted and fused on steel at 360 degrees F (182 degrees C).
a.	Color:  Bright White.
b.	Color:  Antique Ivory.
c.	Color: London Brown.
2.13	TRIM
A.	Standard Accessories:
1.	Consistent with shape, size, and properties shown on the drawings and as required for complete installation.
2.	Produced from the same compound materials and with comparable properties as the siding.
3.	Color:  Matching or color coordinated with siding.
PART 3    EXECUTION
3.1	EXAMINATION
A.	Confirm that all critical dimensions are as specified on the drawings
B.	Beginning installation indicates Installer's acceptance of substrate as suitable to accept siding and soffits.
3.2	PREPARATION
A.	Repair substrate flaws or defects before applying siding or soffits.
B.	Where necessary, fur surfaces to an even plane and free from obstructions before application.
3.3	INSTALLATION
A.	Install vinyl siding and vinyl soffits in accordance with the latest edition of "Vinyl Siding Installation Manual," published by  the Vinyl Siding Institute (VSI) and special details from the drawings.
B.	Install aluminum and steel siding products in accordance with manufacturers printed installation manual.
C.	Install siding, soffits, and accessories in accordance with best practice, with all joint members plumb and true.
3.4	FIELD QUALITY CONTROL
A.	After installation of siding and soffits, check entire surface for obvious flaws or defects.
B.	Replace and repair any problem areas, paying close attention to the substrate for causes of the problem.
3.5	CLEANING AND PROTECTION
A.	After application of siding and soffits, clean as necessary to remove all fingerprints and soiled areas.
B.	Upon completion of siding application, clean entire area, removing all scrap, packaging, and unused materials related to this work.

END OF SECTION