SECTION 03 05 00

COMMON WORK RESULTS FOR CONCRETE - TEMPORARY SURFACE (FLOOR) PROTECTION

Display hidden notes to specifier. (Don't know how? Click Here)

Copyright 2025 - 2025 ARCAT, Inc. - All rights reserved

** NOTE TO SPECIFIER ** GoldiLox: Concrete Surfaces Protective Covering.
This section is based on the products of GoldiLox, which is located at:
13 Pfeiffer Rd.
Boerne, TX 78006
Phone: 830-981-2210
Email: info@goldiloxusa.com
Web: www.godiloxusa.com 
[Click Here] for additional information.
A Protective Cover for Your Concrete Surfaces During Construction
Protecting Polished Concrete Surfaces During All Stages of Construction
What is Goldilox?
GoldiLox is a breathable, industrial composite that is temporarily adhered to polished or smooth concrete surfaces. Our adhesive permeates and encapsulates a proprietary industrial textile, creating a composite floor covering that protects from weather, abrasion, spills, and markings during all stages of construction. GoldiLox is antimicrobial and antifungal, allowing you to frame directly on top of the protective surface. At the end of construction, simply peel off the composite material to reveal the clean surface underneath.
GoldiLox was designed specifically for polished concrete floors by polished concrete contractors. After years of experience, it became obvious that the industry needed real-world concrete surface protection with construction budgets in mind. We designed GoldiLox to protect polished concrete floors from the vast majority of construction damage typically incurred during the life of the project. Easy to apply and cost-effective, GoldiLox offers the just-right protection.

- GENERAL

  - SECTION INCLUDES

** NOTE TO SPECIFIER ** Delete items below not required for project.

    - Protective cover fabric.

    - Related adhesive.

    - Oil and grease stain remover.

    - Liquid and oil sorbent and traction agent.

  - RELATED SECTIONS

** NOTE TO SPECIFIER ** Delete any sections below not relevant to this project; add others as required.

    - Section 03 30 00 - Cast in Place Concrete.

    - Section 03 35 00 - Polished Concrete Finishing.

    - Section 03 53 00 - Concrete Topping.

    - Section 03 39 35 - Concrete Densifier, Sealer, Hardener.

    - Section 07 19 00 - Water Repellants.

    - Section 09 97 23 - Concrete and Masonry Coatings.

  - REFERENCES

** NOTE TO SPECIFIER ** Delete references from the list below that are not actually required by the text of the edited section.

    - ASTM International (ASTM):

      - ASTM E648 - Standard Test Method for Critical Radiant Flux of Floor-Covering Systems Using a Radiant Heat Source.

      - ASTM G21 - Standard Practice for Determining Resistance of Synthetic Polymeric Materials to Fungi.

    - National Fire Protection Association (NFPA):

      - NFPA 253 - Standard Method of Test for Critical Radiant Flux of Floor Covering Systems Using a Radiant Heat Energy Source.

    - International Organization for Standardization (ISO):

      - ISO 20743 - Textiles - Determination of Antibacterial Activity of Textile Products.

    - Occupational Safety and Health Administration (OSHA).

    - American National Standards Institute (ANSI).

    - National Floor Safety Institute (NFSI).

      - Rated for High Traction.

  - SUBMITTALS

    - Submit under provisions of Section 01 30 00.

    - Product Data:

      - Manufacturer's data sheets on each product to be used.

      - Preparation instructions and recommendations.

      - Storage and handling requirements and recommendations.

      - Typical installation methods.

** NOTE TO SPECIFIER ** Delete if not applicable to product type.

    - Verification Samples: Manufacturer will supply one 70 sq ft sample upon request only.

      - Installer should sample GL prior to installation and use to ensure performance and compatibility.

    - Two representative units of each type, size, pattern, and color.

    - Shop Drawings: Include details of materials and application Include relationship with adjacent construction and termination points, control and decorative joints, and lines of intentional color differences in finish surfaces.

  - QUALITY ASSURANCE

    - Manufacturer Qualifications: Company specializing in manufacturing products specified in this section with a minimum of five years documented experience.

    - Installer Qualifications: Company specializing in performing Work of this section with minimum two years documented experience with projects of similar scope and complexity.

    - Source Limitations: Provide each type of product from a single manufacturing source to ensure uniformity.

** NOTE TO SPECIFIER ** Include mock-up if the project size or quality warrant the expense. The following is one example of how a mock-up might be specified. When deciding on the extent of the mock-up, consider all the major different types of work on the project.

    - Mock-Up: Construct a mock-up with actual materials in sufficient time for Architect's review and to not delay construction progress. Locate mock-up as acceptable to Architect and provide temporary foundations and support.

      - The intent of a mock-up is to demonstrate quality of workmanship and visual appearance.

      - If the mock-up is not acceptable, rebuild the mock-up until satisfactory results are achieved.

      - Retain mock-up during construction as a standard for comparison with completed work.

      - Do not alter or remove mock-up until work is completed or removal is authorized.

  - PRE-INSTALLATION CONFERENCE

    - Convene a conference approximately two weeks before scheduled commencement of the Work. Attendees shall include Architect, Contractor and trades involved. Agenda shall include schedule, responsibilities, critical path items and approvals.

  - DELIVERY, STORAGE, AND HANDLING

    - Store and handle in strict compliance with manufacturer's written instructions and recommendations.

    - Protect from damage due to weather, excessive temperature, and construction operations.

  - PROJECT CONDITIONS

    - Maintain environmental temperature, humidity and ventilation conditions within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's recommended limits.

  - WARRANTY

    - Manufacturer's standard limited warranty unless indicated otherwise.

- PRODUCTS

  - MANUFACTURERS

    - Acceptable Manufacturer: Goldilox USA, which is located at:
13 Pfeiffer Rd.
 Boerne, TX 78006
Tel: 830-981-2210
Email: request info (info@goldiloxusa.com);Web: https://www.goldiloxusa.com

** NOTE TO SPECIFIER ** Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

    - Substitutions: Not permitted.

    - Requests for substitutions will be considered in accordance with the provisions of Section 01 60 00.

** NOTE TO SPECIFIER ** Delete paragraphs not required. The GoldiLox Glue Down Protective System is developed specifically for polished and smooth concrete floors. GoldiLox adhesive has also been proven suitable for non-acrylic, non-porous surfaces such as stone, marble, terrazzo, sealed concrete, epoxy, metal, glass, tile, PVC, sanitary ware tube and stainless steel. Must be tested on inconspicuous area prior to application on non-polished or smooth concrete floors.

  - CONCRETE PROTECTION - POLISHED AND SMOOTH

    - Basis of Design: Goldilox Protective Cover Fabric; as manufactured and supplied by Goldilox.

      - Standards Compliance:

        - ASTM G21: Standards for Antifungal Properties.

        - ASTM E648, NFPA 253: Class 1 Flame and Fire Retardant.

        - ISO 20743: Standards for Antimicrobial Properties.

        - NFSI, ANSI: High Traction Standards for Friction.

      - Description: Breathable, seamless, antimicrobial, antifungal., UV, weather, scratch and abrasion, traffic, welding, debris, construction vehicle, spill and slip resistant glue down composite floor protection for temporary adhesion to polished or smooth concrete surfaces.

        - Fabric Roll Dimensions: 65 inch x 375 ft (1.65 x 114.3 m).

        - Fabric Coverage Area: 2.000 sq.ft. (185.81 m2) per roll.

        - UV and Weather Protection Duration: 24 months.

    - Basis of Design: GoldiLox Adhesive; as manufactured and supplied by Goldilox.

      - Adhesive Description: Permeating, encapsulating, non-staining, and low VOC formula.

      - Adhesive Coverage Area: 70 sq.ft. (7.43 sq m) per gallon.

      - Adhesive Volume: 5 gallons (18.93 L) per bucket.

        - Coverage: 350 sq.ft. (32.52 sq m).

    - Basis of Design: GoldiLox Oil and Grease Stain Remover; as manufactured an supplied by GoldiLox.

      - Oil, Grease and Stain Remover Description: Poultice for use in removing oil and grease stains from concrete, stone, and other porous surfaces.

    - Basis of Design: GoldiLox Liquid and Oil Sorbent and Traction Agent; as manufactured an supplied by GoldiLox.

      - Liquid and Oil Sorbent and Traction Agent Description: Super sorbent, leaves surface completely dry.

- EXECUTION

  - EXAMINATION

    - Do not begin installation until the substrates have been properly constructed, troweled, cured and prepared. Do not install over "green", porous, or topically coated surfaces. concrete.

    - If substrate preparation is the responsibility of another installer, notify Architect in writing of unsatisfactory preparation before proceeding.

  - PREPARATION

    - Clean surfaces thoroughly prior to installation according to manufacturer's recommendations.

    - Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

  - INSTALLATION

    - Install in accordance with manufacturer's instructions, approved submittals, and in proper relationship with adjacent construction and substrate installation or preparation.

      - Install glue down protective system using manufacturer's recommended supplies.

      - Do not apply to porous surfaces, rubber, carpet, linoleum, vinyl, latex-based grout, painted, coated, or sealed surfaces. See Manufacturer's installation instructions for more details.

      - Align fabric with termination points and defining breaks as recommended by the manufacturer.

      - Allow installed system to dry for 24 hours, or tack free before allowing heavy traffic.

      - Spot treat, patch, and repair rips, tears, and cuts as required.

  - FIELD QUALITY CONTROL

    - Field Inspection: Coordinate field inspection in accordance with appropriate sections in Division 01.

** NOTE TO SPECIFIER ** Include if manufacturer provides field quality control with onsite personnel for instruction or supervision of product installation, application, erection, or construction. Delete if not required.

    - Manufacturer's Services: Coordinate manufacturer's services in accordance with appropriate sections in Division 01.

  - CLEANING AND PROTECTION

    - Clean glue down protection system in accordance with the manufacturers recommendations.

    - Apply oil and grease stain remover poultice, and clean affected surfaces in accordance with manufacturer's instructions.

    - Apply liquid and oil sorbent and traction agent, and clean affected surfaces in accordance with manufacturer's instructions.

    - Remove glue down protective system in accordance with manufacturer's instructions upon Substantial Completion.

END OF SECTION