SECTION 10 73 13.23

FABRIC AWNINGS

Display hidden notes to specifier. (Don't know how? Click Here) 
 Copyright 2024 -  2026 ARCAT, Inc. - All rights reserved

PART 1    GENERAL
1.1	SECTION INCLUDES
A.	Weathertyte Awning Fabrics:
1.	Weathertyte +.
2.	Weathertyte Proof.
3.	Weathertyte Canopy Fabric.
B.	Cooley-Brite Awning Fabrics:
1.	Cooley-Brite Lite.
2.	Cooley-Brite II.
C.	Haven Awning Fabric.
D.	Tempotest Awning Fabrics:
1.	Tempotest Solids / Textures and Tweeds / Stripes Awning Fabric.
2.	Tempotest Starlight FR Fire Retardant Awning Fabric.
3.	Tempotest Starscreen PET Solar Mesh.
1.2	RELATED SECTIONS
A.	Section 10 71 13 - Exterior Sun Control Devices.
B.	Section 10 71 13.43 - Fixed Sun Screens.
C.	Section 10 73 13 - Awnings.
D.	Section 10 73 13.23 - Fabric Awnings.
E.	Section 10 73 16 - Canopies.
F.	Section 10 73 16.23 - Fabric Canopies.
G.	Section 10 73 26 - Walkway Coverings.
H.	Section 10 73 26.23 - Fabric Walkway Coverings.
I.	Section 13 31 00 - Fabric Structures.
J.	Section 13 31 23 - Tensioned Fabric Structures.
K.	Section 13 31 33 - Framed Fabric Structures.
1.3	REFERENCES
A.	American Association of Textile Chemists and Colorists (AATCC): 
1.	AATCC 22: Test Method for Water Repellency: Spray Test. 
2.	AATCC 118: Test Method for Oil Repellency: Hydrocarbon Resistance.
3.	AATCC 127: Test Method for Water Resistance: Hydrostatic Pressure. 
4.	AATCC 135: Test Method for Dimensional Changes of Fabrics after Home Laundering.
5.	AATCC 169: Test Method for Weather Resistance of Textiles: Xenon Lamp Exposure.
6.	AATCC 183: Test Method for Transmittance or Blocking of Erthemally Weighted Ultraviolet Radiation through Fabrics.
7.	AATCC 193: Test Method for Aqueous Liquid Repellency: Water/Alcohol Solution Resistance Test.
B.	American Society for Testing and Materials (ASTM): 
1.	ASTM D737: Standard Test Method for Air Permeability of Textile Fabrics. 
2.	ASTM D751: Standard Test Methods for Coated Fabrics. 
3.	ASTM D1004: Standard Test Method for Tear Resistance (Graves Tear) of Plastic Film and Sheeting. 
4.	ASTM D1204: Standard Test Method for Linear Dimensional Changes of Nonrigid Thermoplastic Sheeting or Film at Elevated Temperature.
5.	ASTM D1777: Standard Test Method for Thickness of Textile Materials.
6.	ASTM D1894: Standard Test Method for Static and Kinetic Coefficients of Friction of Plastic Film and Sheeting.
7.	ASTM D1912: Standard Test Method for Cold-Crack Resistance of Upholstery Leather.
8.	ASTM D2136: Standard Test Method for Coated Fabrics - Low-Temperature Bend Test. 
9.	ASTM D2261: Standard Test Method for Tearing Strength of Fabrics by the Tongue Procedure. 
10.	ASTM D3774: Standard Test Method for Width of Textile Fabric.
11.	ASTM D3776: Standard Test Methods for Mass Per Unit Area (Weight) of Fabric.
12.	ASTM D3786: Standard Test Method for Bursting Strength of Textile Fabrics - Diaphragm Bursting Strength Tester Method.
13.	ASTM D4157: Standard Test Method for Abrasion Resistance of Textile Fabrics.
14.	ASTM D5034: Standard Test Method for Breaking Strength and Elongation of Textile Fabrics.
15.	ASTM D6796: Standard Test Method for Bursting Strength of Fabrics Constant-Rate-of-Extension Ball Burst Test.
16.	ASTM E84: Standard Test Method for Surface Burning Characteristics of Building Materials.
17.	ASTM E96: Standard Test Method for Gravimetric Determination of Water Vapor Transmission Rate of Materials.
18.	ASTM G21: Standard Practice for Determining Resistance of Synthetic Polymeric Materials to Fungi. 
19.	ASTM G155: Standard Practice for Operating Xenon Arc Lamp Apparatus for Exposure of Materials.
C.	California State Fire Marshall: 
1.	Flame Retardant Fabric Registration.
2.	California State Fire Marshall Title 19.
D.	Deutsches Institut fUr Normung (DIN): 
1.	DIN 4102-1: Fire Behavior of Building Materials and Components Part 1: Classification of Building Materials and Requirements.
E.	European Standards (EN Standards): 
1.	EN 13561: External Blinds and Awnings. Performance Requirements Including Safety. 
2.	EN 13934-1: Textiles - Tensile Properties of Fabrics - Part 1: Determination of Maximum Force and Elongation at Maximum Force Using the Strip Method.
3.	EN 24920: Textiles - Determination of Resistance to Surface Wetting (Spray Test) of Fabrics.
F.	Industrial Fabrics Association International (IFAI): 
1.	CPAI-84: A Specification for Flame-Resistant Materials Used in Camping Tentage.
G.	International Organization for Standardization (ISO): 
1.	ISO 105-B02: Textiles - Tests for Colour Fastness - Part B02: Colour Fastness to Artificial Light: Xenon Arc Fading Lamp Test.
2.	ISO 105-B04: Textiles - Tests for Colour Fastness - Part B04: Colour Fastness to Artificial Weathering: Xenon Arc Fading Lamp Test.
H.	Italian Standardization Body (UNI): 
1.	UNI 9177: Reaction to Fire - Flammable Product Classification.
I.	National Fire Protection Association (NFPA): 
1.	NFPA 701-10: Standard Methods of Fire Tests for Flame Propagation of Textiles and Films.
J.	Oeko-Tex Association: 
1.	Oeko-Tex Standard 100 Certificate.
K.	Underwriters' Laboratories (UL): 
1.	UL Certified.
1.4	DEFINITIONS
A.	DWR: Durable Water Repellent.
1.5	SUBMITTALS
A.	Submit under provisions of Section 01 30 00.
B.	Product Data:
1.	Manufacturer's data sheets on each product to be used.
2.	Preparation instructions and recommendations.
3.	Storage and handling requirements and recommendations.
4.	Typical installation methods.
C.	Verification Samples: Two representative units of each type, size, pattern, and color.
D.	Shop Drawings: Include details of materials, construction, and finish. Include relationship with adjacent construction. 
1.6	QUALITY ASSURANCE
A.	Manufacturer Qualifications: Company specializing in manufacturing products specified in this section with a minimum of 90 years documented experience in the manufacturing of awning fabrics.
B.	Installer Qualifications: Company specializing in performing Work of this section with minimum two years documented experience with projects of similar scope and complexity.
C.	Source Limitations: Provide each type of product from a single manufacturing source to ensure uniformity.
1.7	DELIVERY, STORAGE, AND HANDLING
A.	Store and handle in strict compliance with manufacturer's written instructions and recommendations.
1.	Store fabrics in the manufacturer's unopened packaging until ready for use.
2.	Do not store rolls flat. Store rolls standing on end.
B.	Protect from damage due to weather, excessive temperature, and construction operations.
1.8	PROJECT CONDITIONS
A.	Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's recommended limits.
1.9	WARRANTY
A.	The manufacturer's standard limited warranty is in effect at the date of purchase unless indicated otherwise.
PART 2    PRODUCTS
2.1	MANUFACTURERS
A.	Acceptable Manufacturer: Miami Corporation, which is located at:<BR />720 Anderson Ferry Rd.<BR />Cincinnati, OH 45238<BR />Email: request info (csmith@miamicorp.com);Web: https://www.miamicorp.com 
B.	Substitutions: Not permitted.
C.	Requests for substitutions will be considered in accordance with the provisions of Section 01 60 00.
2.2	AWNING FABRICS - WEATHERTYTE
A.	Fabric: Weathertyte + as manufactured by the Cooley Group and distributed by Miami Corporation.
1.	Composition: 
a.	Base Fabric: 
1)	Fiber: Polyester low-wick scrim. 
2)	Weight: 2.7 ounces per square yard (91 grams per square meter). 
b.	Coated Fabric:
1)	Coating Type: PVC.
2)	Total Weight: 16 ounces per square yard (542 grams per square meter). 
2.	Performance Requirements: Meets the following.
a.	Tensile Strength, Grab (Warp) ASTM D751-A: 230 pounds force (1023 Newtons). 
b.	Tensile Strength, Grab (Fill) ASTM D751-A: 150 pounds force (667 Newtons). 
c.	Tensile Strength, Tongue (Warp) ASTM D751-B: 50 pounds force (222 Newtons). 
d.	Tensile Strength, Tongue (Fill) ASTM D751-B: 30 pounds force (133 Newtons). 
e.	Puncture, Screwdriver ASTM D751: 50 pounds force (222 Newtons). 
f.	Puncture, Ball ASTM D751: 250 pounds force (1,112 Newtons). 
g.	Hydrostatic Resistance ASTM D751: 300 pounds per square inch (2.1 Megapascals). 
h.	Abrasion Resistance (H18/1 kg) ASTM D3389: 900 cycles.
i.	Low-Temperature Bend ASTM D2136: 0 degrees Fahrenheit (-18 degrees Celsius). 
j.	High Temperature, Continuous / Intermittent ASTM D1204: 180 / 200 degrees Fahrenheit (82 / 93 degrees Celsius). 
k.	Fungus Resistant ASTM G21: Yes. 
l.	Weldable: Dielectric radio frequency or thermal.
m.	Flame Certifications: 
1)	UL. 
2)	NFPA 701. 
3)	CSFM: California State Fire Marshall Approved. 
4)	ASTM E84 (Class A).
3.	Width: Up to 74 inches (1.88 meters).
4.	Watertight. 
5.	Embossed. 
6.	Resists sagging.
7.	Ink Compatibility: 
a.	Solvent. 
b.	Eco-solvent. 
c.	Solvent. 
d.	UV. 
e.	Screen Printing. 
f.	Latex.
8.	Color: As determined by the Architect from Manufacturer's options.
9.	Color: WTY24PLS Black 74.
10.	Color: WTY97PLS Charcoal 74.
11.	Color: WTY11PLS Dark Red 74.
12.	Color: WTY5PLS Forest Green 74.
13.	Color: WTY15PLS White 74].
14.	Color: WTY75PLS Navy 74.
15.	Color: WTY81PLS Chocolate Brown 74.
16.	Color: WTY151PLS Linen 74.
17.	Color: WTY416PLS Pacific Blue 74.
18.	Color: WTY426PLS Terracotta Brick 74.
19.	Color: WETY6PLS Pool Green 74.
20.	Color: WTY56PLS Paris Red 74.
21.	Color: WTY12PLS Sunflower 74.
22.	Color: WTY79PLS Silver 74.
23.	Color: WTY73PLS Burgundy 74.
B.	Fabric: Weathertyte Proof Awning Fabric as manufactured by the Cooley Group and distributed by Miami Corporation.
1.	Composition:
a.	Coated Fabric:
1)	Coating Type: PVC.
2)	Total Weight: 11 ounces per square yard (373 grams per square meter).
2.	Performance Requirements: Meets the following.
a.	Tensile Strength, Grab (Warp) ASTM D751-A: 220 pounds force (979 Newtons). 
b.	Tensile Strength, Grab (Fill) ASTM D751-A: 150 pounds force (667 Newtons). 
c.	Tensile Strength, Tongue (Warp) ASTM D751-B: 50 pounds force (222 Newtons). 
d.	Tensile Strength, Tongue (Fill) ASTM D751-B: 30 pounds force (133 Newtons). 
e.	Puncture, Screwdriver ASTM D751: 40 pounds force (178 Newtons). 
f.	Puncture, Ball ASTM D751: 200 pounds force (890 Newtons). 
g.	Hydrostatic Resistance ASTM D751: 250 pounds per square inch (1.7 Megapascals). 
h.	Abrasion Resistance (H18/1 kg) ASTM D3389: 200 cycles.
i.	Low-Temperature Bend ASTM D2136: 0 degrees Fahrenheit (-18 degrees Celsius). 
j.	High Temperature, Continuous / Intermittent ASTM D1204: 180 / 200 degrees Fahrenheit (82 / 93 degrees Celsius). 
k.	Fungus Resistant ASTM G21: Yes. 
l.	Weldable: Dielectric radio frequency or thermal.
m.	Flame Certifications: 
1)	UL. 
2)	NFPA 701. 
3)	CSFM: California State Fire Marshall Approved. 
4)	ASTM E84 (Class A).
3.	Width: Up to 61 inches (1.88 meters).
4.	Watertight. 
5.	Resists sagging.
6.	Ink Compatibility: 
a.	Solvent. 
b.	Eco-solvent. 
c.	Solvent. 
d.	UV. 
e.	Pressure Sensitive Vinyl.
f.	Screen Printing. 
g.	Latex.
7.	Color: As determined by the Architect from Manufacturer's options.
8.	Color: WTY24PLS Black 74.
9.	Color: WTY5PLS Forest Green 74.
10.	Color: WTY15PLS White 74.
11.	Color: WTY416PLS Pacific Blue 74.
12.	Color: WTY56PLS Paris Red 74.
13.	Color: WTY12PLS Sunflower 74.
14.	Color: WTY79PLS Silver 74.
15.	Color: WTY73PLS Burgundy 74.
C.	Fabric: Weathertyte Canopy Fabric as manufactured by the Cooley Group and distributed by Miami Corporation.
1.	Composition: 
a.	Coated Fabric:
1)	Coating Type: PVC with polycarbonate topcoat.
2)	Total Weight: 16 ounces per square yard (542 grams per square meter). 
2.	Performance Requirements: Meets the following.
a.	Tensile Strength, Grab ASTM D751: 
1)	Minimum: 325 x 250 pounds force (1446 x 1112 Newtons). 
2)	Typical: 395 x 340 pounds force (1757 x 1512 Newtons).
b.	Tensile Elongation, Grab ASTM D751: 
1)	Minimum: 15 x 15 percent. 
2)	Typical 25 x 28 percent.
c.	Tear Strength, Tongue ASTM D751: 
1)	Minimum: 30 x 25 pound force (133 x 111 Newtons). 
2)	Typical: 65 x 45 pounds force (289 x 200 Newtons).
d.	Tear Strength, Trapezoid ASTM D751:
1)	Minimum: 25 x 25 pound force (111 x 111 Newtons). 
2)	Typical: 40 x 40 pounds force (178 x 178 Newtons).
e.	Ply Adhesion ASTM D751: 
1)	Minimum: 15 pounds per inch (2627 Newtons per meter). 
2)	Typical: 20 pounds per inch (3503 Newtons per meter). 
f.	Shrinkage ASTM D1204: 
1)	Minimum: Less than 1 percent. 
2)	Typical: 0.3 percent.
g.	Low-Temperature Cracking ASTM D2136: -30 degrees Fahrenheit (-34 degrees Celsius).
h.	Weathering ASTM G155: 10,000 hours, equivalent to 10 years of natural outdoor weathering.
i.	Weldable: Thermal.
j.	Flame Certifications: 
1)	UL. 
2)	NFPA 701. 
3)	CSFM: California State Fire Marshall Approved. 
4)	ASTM E84 (Class A).
3.	Width: Up to 78 inches (1.98 meters).
4.	Mildew and mold resistant.
5.	Waterproof. 
6.	Ink Compatibility: 
a.	Paint. 
b.	Pressure Sensitive Vinyl.
c.	Screen Printing. 
7.	Color: As determined by the Architect from Manufacturer's options.
8.	Color: WTY24CAN Black 78.
9.	Color: WTY15CAN White 78.
10.	Color: WTY416CAN Pacific Blue 78.
11.	Color: WTY11CAN Red 78, WTY75CAN Navy 78.
12.	Color: WTY73CAN Burgundy 78.
13.	Color: WTY5CAN Forest Green 78.
14.	Color: WTY79CAN Canopy Silver 78.
15.	Color: WTY57CAN Coffee 78.
16.	Color: WTY1593CAN Snow 78.
17.	Color: WTY6CAN Pool Green 78.
18.	Color: WTY12CAN Yellow 78.
2.3	AWNING FABRICS - COOLEY-BRITE
A.	Fabric: Cooley-Brite Lite as manufactured by the Cooley Group and Distributed by the Miami Corporation.
1.	Composition: 
a.	Coating Type: PVC. 
b.	Scrim Type: 500 x 500 Polyester denier.
2.	Meets Requirements: 
a.	Tensile Strength, Grab ASTM D751-A: 225 x 150 pounds force (1000 x 667 Newtons). 
b.	Tear Strength, Butterfly ASTM D1004: 50 x 30 pounds force (222 x 133 Newtons). 
c.	Puncture, Screwdriver ASTM D751: 35 pounds force (156 Newtons). 
d.	Shrinkage at 200 degrees Fahrenheit (93 degrees Celsius) ASTM D1204: Less than 1.5 percent. 
e.	Low-Temperature Bend ASTM D2136: -20 degrees Fahrenheit (-29 degrees Celsius). 
f.	High Temperature, Continuous / Intermittent ASTM D1204: 180 / 200 degrees Fahrenheit (82 / 93 degrees Celsius). 
g.	Fungus Resistant ASTM G21: Yes. 
h.	Weldable: Dielectric radio frequency or thermal.
i.	Flame Certifications: 
1)	UL. 
2)	NFPA 701. 
3)	CSFM: California State Fire Marshall Approved. 
4)	ASTM E84 (Class A).
3.	Standard Widths: 78 inches (1.98 meters).
4.	Roll Size: 10 yards (9.1 meters).
5.	Roll Size: 25 yards (22.9 meters).
6.	Roll Size: 50 yards (45.7).
7.	Weight: 16 ounces per square yard (542 grams per square meter).
8.	Water repellant. 
9.	Heat sealable.
10.	Ink Compatibility: 
a.	Solvent. 
b.	Eco-solvent.
c.	UV. 
d.	Screen printing. 
e.	Eradicable. 
f.	Inkjet printable. 
g.	Print translucent, pressure-sensitive graphics.
11.	Color: As determined by the Architect from Manufacturer's options.
12.	Color: CBL0606 White.
13.	Color: CBL4 Lemon Yellow.
14.	Color: CBL20 Sunflower Yellow.
15.	Color: CBL17-Tangerine.
16.	Color: CBL2 Bright Red.
17.	Color: CBL18 Ruby Red.
18.	Color: CBL186 Cherry Red.
19.	Color: CBL22 Burgundy.
20.	Color: CBL19 Raspberry.
21.	Color: CBL6 Royal Blue.
22.	Color: CBL16 Intense Blue.
23.	Color: CBL5 Navy Blue.
24.	Color: CBL11 Plum Purple.
25.	Color: CBL13 Teal.
26.	Color: CBL15 Petro Green.
27.	Color: CBL21 Holly Green.
28.	Color: CBL7 Emerald Green.
29.	Color: CBL10 Black.
B.	Cooley-Brite II as manufactured by the Cooley Group and Distributed by the Miami Corporation.
1.	Composition: 
a.	Coating Type: PVC. 
b.	Scrim Type: 500 x 500 Polyester denier.
2.	Meets Requirements: 
a.	Tensile Strength, Grab ASTM D751-A: 225 x 150 pounds force (1000 x 667 Newtons). 
b.	Tear Strength, Butterfly ASTM D1004: 50 x 30 pounds force (222 x 133 Newtons). 
c.	Puncture, Screwdriver ASTM D751: 35 pounds force (156 Newtons). 
d.	Shrinkage at 200 degrees Fahrenheit (93 degrees Celsius) ASTM D1204: Less than 1.5 percent. 
e.	Low-Temperature Bend ASTM D2136: -20 degrees Fahrenheit (-29 degrees Celsius). 
f.	High Temperature, Continuous / Intermittent ASTM D1204: 180 / 200 degrees Fahrenheit (82 / 93 degrees Celsius). 
g.	Fungus Resistant ASTM G21: Yes. 
h.	Weldable: Dielectric radio frequency or thermal.
i.	Flame Certifications: 
1)	UL. 
2)	NFPA 701. 
3)	CSFM: California State Fire Marshall Approved. 
4)	ASTM E84 (Class A).
3.	Standard Widths: 78 inches (1.98 meters).
4.	Roll Size: 10 yards (9.1 meters).
5.	Roll Size: 25 yards (22.9 meters).
6.	Roll Size: 50 yards (45.7).
7.	Weight: 20 ounces per square yard (680 grams per square meter).
8.	Water repellant. 
9.	Heat sealable.
10.	Ink Compatibility: 
a.	Solvent. 
b.	Eco-solvent.
c.	UV. 
d.	Screen printing. 
e.	Eradicable. 
f.	Inkjet printable. 
g.	Print translucent, pressure-sensitive graphics.
11.	Color: As determined by the Architect from Manufacturer's options.
12.	Color: 0606 White.
13.	Color: 2146 Ivory.
14.	Color: 2037 Yellow.
15.	Color: 0123 Sunflower Yellow.
16.	Color: 2119 Orange.
17.	Color: 2662 Light Red.
18.	Color: 0132 Bright Red.
19.	Color: 2283 Dark Red.
20.	Color: 2020 Burgundy.
21.	Color: 0219 Pink.
22.	Color: 0248 Plum.
23.	Color: 2025M Black.
24.	Color: 2648 Light Blue.
25.	Color: 0310 Mid Blue.
26.	Color: 5025 Reflex Blue.
27.	Color: 2114 Dark Blue.
28.	Color: 5019 Teal.
29.	Color: 0355 Light Green.
30.	Color: 2108 Green.
31.	Color: 4048 Forest Green.
2.4	AWNING FABRIC - HAVEN
A.	Fabric: Haven Awning Fabric as manufactured by Snyder Manufacturing Inc. and Distributed by Miami Corporation.
1.	Composition: 
a.	Construction: Vinyl laminated.
b.	Yarn: Polyester. 
2.	Performance Requirements: Meets the following.
a.	California State Fire Marshall Title 19 for Decorative Materials.
b.	Flammability: NFPA-701 2015
c.	Flame Spread Rating Class A: ASTM E-84-81A.
3.	Width: 61 inches (1.54 meters).
4.	Roll Size: 50 yards (45.7 meters).
5.	Mold and mildew resistant.
6.	Dull Embossed. 
7.	Cold Crack: -40 degrees Fahrenheit (-40 degrees Celsius). 
8.	Abrasion Resistance: High.
9.	Tensile Strength: High.
10.	Tear Strength: High.
11.	UV Resistance: Extreme.
12.	Dimensional Stability: Excellent.
13.	Ink Compatibility: 
a.	Eco-solvent. 
b.	Solvent. 
c.	Digital Printing.
d.	Screen Printing. 
14.	Color: As determined by the Architect from Manufacturer's options.
15.	Color: HAV24 Black
16.	Color: HAV11 Red
17.	Color: HAV415 Maroon.
18.	Color: HAV73 Burgundy.
19.	Color: HAV426 Brick.
20.	Color: HAV102 Cappuccino.
21.	Color: HAV1552 Latte.
22.	Color: HAV414 Intense Blue.
23.	Color: HAV Prussian Blue.
24.	Color: HAV978 Jungle.
25.	Color: HAV8 Pine.
26.	Color: HAV92 Indigo.
27.	Color: HAV94 Grey.
28.	Color: HAV79 Silver.
29.	Color: HAV930 Hazelnut.
30.	Color: HAV15 White.
31.	Color: HAV206 Royal Purple.
32.	Color: HAV72 Orange.
33.	Color: HAV12 Sunflower.
2.5	FABRIC AWNINGS - TEMPOTEST
A.	Tempotest Fabric: As manufactured by PARA and distributed by Miami Corporation.
1.	Type: Tempotest Solids.
2.	Type: Tempotest Textures and Tweeds.
3.	Type: Tempotest Stripes.
4.	Composition: 100 percent solution-dyed acrylic fiber.
5.	Performance Requirements: Meets the following.
a.	Paragraph 15.2 of UNI EN 13561:2009. 
b.	Oeko-Tex Association's Oeko-TexStandard 100 certificate of approval designation signifying the products have been tested for harmful substances and found to pose no risk to health.
c.	Water repellant.
d.	Water Column: Greater than or equal to 15 inches (38 centimeters).
6.	Available Widths: 47 inches (119 centimeters).
7.	Available Widths: 60 inches (152 centimeters).
8.	Available Widths: 80 inches (203 centimeters).
9.	Weight (+/- 5 percent): 8.8 ounces per square yard (298 grams per square meter).
10.	Fabric Protection:
a.	EchoShield: Tempotest fabrics finished with EcoShield are oil cleanable, water repellent, and UV resistant. The surface treatment forms a molecular barrier around each fiber to repel water.
b.	Hi-Clean Finishing: Hi-Clean creates an impenetrable barrier without compromising the fabric's breathability. This finish repels water, grease, and oil and protects against rotting and the formation of mold and fungus. Hi-Clean makes the fabric self-cleaning, allowing dirt, fine dust, and pollution to wash away with water and rain.
11.	Solids Color: ________.
12.	Textures and Tweeds Color: ________.
13.	Stripes Colors: ________.
B.	Fabric: Tempotest Starlight FR Fire Retardant Awning Fabric as manufactured and supplied by Miami Corporation.
1.	Composition: 100 percent solution-dyed PET fiber with inherent flame retardant properties.
2.	Performance Requirements: Meets the following.
a.	Fire Resistance: Class 1 UN EN9177, BI (DIN 4102), NFPA 701-10, NVSS 302 Title 19 Section 1237, CPAI 84.
b.	Oeko-Tex Association' Oeko-TexStandard 100 certificate of approval designation signifying the products have been tested for harmful substances and found to post no risk to health. 
c.	Flame Retardant Fabric Registration License Number F-025801 signifying this product meets the minimum requirement of flame resistance established by the California State Fire Marshall for products identified in Section NOREPL13115 of the California Health and Safety Code. 
d.	Spray Test: Grade 4 (UNI EN 24920). 
e.	Lightfastness: 4/5 - 5 degree grey scale (UNI EN ISO 105-B04, 1000 hours). 
f.	Breaking Load (UNI EN 13934-1): 
1)	Warp: 517 pound-force (2300 Newtons) - elongation 40 percent.
2)	Weft: 247 pound-force (1100 Newtons) - elongation 40 percent.
g.	Meets or exceeds the maximum UV protection value for fabrics: Ultraviolet Protection Factor of 50+.
h.	Resistant to UV degradation.
i.	Water Column: Greater than or equal to 14 inches (35 centimeters).
j.	High-tenacity fabric. 
k.	Excellent color fastness. 
3.	Width: 60 inches (152 centimeters). 
4.	Weight (+/- 5 percent): 8.8 ounces per square yard (298 grams per square meter).
5.	Fabric Protection: EchoShield: Tempotest fabrics finished with EcoShield are oil cleanable, water repellent, and UV resistant. The surface treatment forms a molecular barrier around each fiber to repel water.
6.	Color: ________.
C.	Fabric: Tempotest Starscreen PET Solar Mesh:
1.	Composition: 100 percent solution-dyed PET fiber with inherent flame retardant properties.
2.	Performance Requirements: Meets the following.
a.	Fire Resistance: Class 1 UN EN9177, BI (DIN 4102), NFPA 701-10, NVSS 302 Title 19 Section 1237, CPAI 84.
b.	Oeko-Tex Association' Oeko-TexStandard 100 certificate of approval designation signifying the products have been tested for harmful substances and found to pose no risk to health. 
c.	Flame Retardant Fabric Registration License Number F-025801 signifying this product meets the minimum requirement of flame resistance established by the California State Fire Marshall for products identified in Section NOREPL13115 of the California Health and Safety Code. 
d.	Spray Test: Grade 4 (UNI EN 24920). 
e.	Lightfastness: 7/8 - 8 degree blue scale (EN ISO BO2), greater than 4 degree grey scale (UNI EN ISO 105-B04, 1000 hours). 
f.	Breaking Load (UNI EN 13934-1): 
1)	Warp: 270 pound-force (1200 Newtons) - elongation 32.5 percent.
2)	Weft: 207 pound-force (920 Newtons) - elongation 37.5 percent. 
g.	Tear Strength: 
1)	Warp: 82.
2)	Weft: 54. 
h.	Openness Factor: 3.5 percent.
3.	Width: 128 inches (325 centimeters). 
4.	Thickness: 0.02 inches (0.5 millimeters).
5.	Weight (+/- 5 percent): 6.49 ounces per square yard (220 grams per square meter).
6.	Fabric Protection:
a.	EchoShield: Tempotest fabrics finished with EcoShield are oil cleanable, water repellent, and UV resistant. The surface treatment forms a molecular barrier around each fiber to repel water.
7.	Color: _________.
D.	Accessories:
1.	Tempotest Awning Binding Tape:
a.	Color coordinated with the Tempotest line of the awning and marine fabric. 
b.	Suitable for use with any awning and marine fabric.
c.	Has the same solution-dyed construction as the Tempotest fabric.
d.	Excellent exposure resistance to sun and atmospheric contents and the actions of mold, micro-organisms, and salt.
2.6	FABRICATION
A.	Fabricate tension structures and awnings using methods recommended by the manufacturer and Miami Corporation.
B.	Test all inks for compatibility.
PART 3    EXECUTION
3.1	EXAMINATION
A.	Do not begin installation until the substrates have been properly constructed and prepared.
B.	If substrate preparation is the responsibility of another installer, notify Architect in writing of unsatisfactory preparation before proceeding.
3.2	PREPARATION
A.	Clean surfaces thoroughly prior to installation.
B.	Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.
3.3	INSTALLATION
A.	Install in accordance with manufacturer's instructions, approved submittals, and in proper relationship with adjacent construction.
3.4	FIELD QUALITY CONTROL
A.	Field Inspection: Coordinate field inspection in accordance with appropriate sections in Division 01.
B.	Manufacturer's Services: Coordinate manufacturer's services in accordance with appropriate sections in Division 01.
3.5	CLEANING AND PROTECTION
A.	Clean products in accordance with the manufacturers recommendations. 
B.	Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION