SECTION 09 90 00

PAINTS AND COATINGS

Display hidden notes to specifier. (Don't know how? Click Here) 
 Copyright 2004 -  2025 ARCAT, Inc. - All rights reserved

PART 1    GENERAL
1.1	SECTION INCLUDES
A.	Exterior Paint Systems: Surface preparation and field painting of exposed exterior items and surfaces.
B.	Exterior stain and natural finish woodwork systems.
C.	Interior Paint Systems: Surface preparation and field painting of exposed interior items and surfaces.
D.	Interior stain and natural finish woodwork systems.
E.	Exterior High Performance Coating Systems: Surface preparation and field application of exterior high-performance coating systems to items and surfaces scheduled.
F.	Interior High Performance Coating Systems: Surface preparation and field application of interior high-performance coating systems to items and surfaces scheduled.
1.2	RELATED SECTIONS
A.	Section 03 30 00 - Cast-in-Place Concrete.
B.	Section 05 12 13 - Architecturally-Exposed Structural Steel Framing.
C.	Section 05 50 00 - Metal Fabrications.
D.	Section 06 20 00 - Finish Carpentry.
E.	Section 08 11 13.13 - Standard Hollow Metal Doors and Frames.
F.	Section 09 21 16.33 - Gypsum Board Area Separation Wall Assemblies.
G.	Section 22 05 00 - Common Work Results for Plumbing.
H.	Section 26 05 00 - Common Work Results for Electrical.
1.3	REFERENCES
A.	American Society for Testing and Materials (ASTM) D16 - Standard Terminology for Paint, Related Coatings, Materials, and Applications.
B.	Steel Structures Painting Council (SSPC) SP6 - Commercial Blast Cleaning Procedures.
C.	Steel Structures Painting Council (SSPC) SP10 - Near White Blast Cleaning Procedure.
1.4	DEFINITIONS
A.	General: Standard coating terms in accordance with ASTM D523.
1.	Gloss Level 1 (Flat): Not more than 5 units at 60 degrees and 10 units at 85 degrees, in accordance with ASTM D523.
2.	Gloss Level 2 (Low Sheen): Not more than 10 units at 60 degrees and 10 to 35 units at 85 degrees, in accordance with ASTM D523.
3.	Gloss Level 3 (Eggshell): 10 to 25 units at 60 degrees and 10 to 35 units at 85 degrees, in accordance with ASTM D523.
4.	Gloss Level 4 (Satin): 20 to 35 units at 60 degrees and not less than 35 units at 85 degrees, in accordance with ASTM D523.
5.	Gloss Level 5 (Semi-Gloss): 35 to 70 units at 60 degrees, in accordance with ASTM D523.
6.	Gloss Level 6 (Gloss): 70 to 85 units at 60 degrees, in accordance with ASTM D523.
7.	Gloss Level 7 (High-Gloss): More than 85 units at 60 degrees, in accordance with ASTM D523.
B.	Environments: The following terms distinguish between different corrosive exposures:
1.	Severe Environments: Highly corrosive industrial atmospheres. Sustained exposure to high humidity and condensation and with frequent cleaning using strong chemicals. Environments with heavy concentrations of strong chemical fumes and frequent splashing and spilling of harsh chemical products are severe environments.
2.	Moderate Environments: Corrosive industrial atmospheres with intermittent exposure to high humidity and condensation, occasional mold and mildew development, and regular cleaning with strong chemicals. Environments with exposure to heavy concentrations of chemical fumes and occasional splashing and spilling of chemical products are moderate environments.
3.	Mild Environment: Industrial atmospheres with normal exposure to moderate humidity and condensation, occasional mold and mildew development, and infrequent cleaning with strong chemicals. Environments with low levels of mild chemical fumes and occasional splashing and spilling of chemical products are mild environments. Normal outdoor weathering is also considered a mild environment.
1.5	SUBMITTALS
A.	Submit under provisions of Section 01 30 00 - Administrative Requirements.
B.	Product Data: For each paint system indicated, including:
1.	Material List: An inclusive list of required coating materials. Indicate each material and cross reference specific coating, finish system, and application. Identify each material by manufacturer's catalog number and general classification.
2.	Preparation instructions and recommendations.
3.	Manufacturer's Information: Manufacturer's technical information, including label analysis and instructions for handling, storing, and applying each coating material.
C.	Selection Samples: For each finish product specified, two complete sets of color chips representing manufacturer's full range of available colors and patterns.
D.	Verification Samples: For each finish product specified, two samples, minimum size 6 inches (150 mm) square, representing actual product, color, and patterns.
1.6	QUALITY ASSURANCE
A.	Installer Qualifications: A firm or individual experienced in applying paints and coatings similar in material, design, and extent to those indicated for this Project, whose work has resulted in applications with a record of successful in-service performance.
B.	Obtain block fillers and primers for each coating system from the same manufacturer as the finish coats.
C.	Paint exposed surfaces. If an item or a surface is not specifically mentioned, paint the item, or surface the same as similar adjacent materials or surfaces. If a color of finish is not indicated, Architect will select from standard colors and finishes available.
D.	Do not paint prefinished items, concealed surfaces, finished metal surfaces, operating parts, and labels.
E.	Mock-Up: Provide a mock-up for evaluation of surface preparation techniques and application workmanship.
1.	Finish areas designated by Architect.
2.	Do not proceed with remaining work until workmanship, color, and sheen are approved by Architect.
3.	Refinish mock-up area as required to produce acceptable work.
1.7	DELIVERY, STORAGE, AND HANDLING
A.	Deliver materials to Project site in manufacturer's original, unopened packages and containers bearing manufacturer's name and label:
B.	Store materials not in use in tightly covered containers in a well-ventilated area at a minimum ambient temperature of 45 degrees F (7 degrees C). Maintain storage containers in a clean condition, free of foreign materials and residue.
1.8	PROJECT CONDITIONS
A.	Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's absolute limits.
B.	Apply waterborne paints only when temperatures of surfaces to be painted and surrounding air are between 50 and 90 degrees F (10 and 32 degrees C).
C.	Apply solvent-thinned paints only when temperatures of surfaces to be painted and surrounding air are between 45 and 95 degrees F (7 and 35 degrees C).
D.	Do not apply paint in snow, rain, fog, or mist, when relative humidity exceeds 85 percent, at temperatures less than 5 degrees F (3 degrees C) above the dew point, or to damp or wet surfaces.
1.	Painting may continue during inclement weather if surfaces and areas to be painted are enclosed and heated within temperature limits specified by manufacturer during application and drying periods.
1.9	EXTRA MATERIALS
A.	Furnish extra paint materials from the same production run as the materials applied in the quantities described below. Package with protective covering for storage and identify with labels describing contents. Deliver extra materials to Owner.
B.	Quantity: Furnish Owner with an additional three percent, but not less than 1 gal (3.8 liters) or 1 case, as appropriate, of each material and color applied.
PART 2    PRODUCTS
2.1	MANUFACTURERS
A.	Acceptable Manufacturer: Pittsburgh Paints (formerly PPG Paints), which is located at:<BR />400 Bertha Lamme Drive<BR />Cranberry Township, PA 16066<BR />Toll Free Tel: 1-888-PPG-IDEA<BR />Fax: 888-434-3127<BR />Email: request info (brian.joyce@ppg.com);Web: https://pittsburghpaints.com 
1.	Basis of Design: Pittsburgh Paints as manufactured and supplied by Pittsburgh Paints.
B.	Substitutions: Not permitted.
C.	Requests for substitutions will be considered in accordance with provisions of Section 01 60 00 - Product Requirements.
2.2	PAINT MATERIALS GENERAL
A.	Material Compatibility: Provide block fillers, primers, and finish-coat materials that are compatible with one another and with the substrates indicated under conditions of service and application, as demonstrated by manufacturer based on testing and field experience.
B.	VOC Classification: Provide high-performance coating materials, including primers, undercoats, and finish-coat materials, that meet the applicable local, state, or federal VOC requirements.
C.	Color: Refer to Finish Schedule and Paint Legend for paint colors.
2.3	EXTERIOR PAINT FINISH SYSTEMS
A.	Acrylic Finish: Two finish coats over a primer.
1.	Substrate:
a.	Concrete, stucco, and brick masonry; other than concrete masonry units.
b.	Mineral-fiber-reinforced cement panels.
c.	Exterior gypsum soffit board.
2.	Primer:
a.	Pittsburgh Paints: Seal Grip Gripper Interior/Exterior Universal Acrylic Primer, 17-921XI Series. Applied Dry Film Thickness: 1.6 mils min.
b.	Pittsburgh Paints: Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI. Applied Dry Film Thickness: 1.4 mils min.
3.	Exterior Gloss Level 1 Acrylic Finish:
a.	Pittsburgh Paints: Speedhide Exterior House Latex Flat, 6-610XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: Sun Proof Exterior Acrylic Latex Flat, 72-110XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Flat, 519-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	Pittsburgh Paints: Permanizer Exterior Acrylic Latex Flat, 759-10 Series. Applied Dry Film Thickness: 2.3 mils min.
4.	Exterior Gloss Level 1 High Build Acrylic Finish:
a.	Pittsburgh Paints: Perma-Crete High Build 100 Percent Acrylic Topcoat Flat, 4-22XI Series. Applied Dry Film Thickness: 3.2 mils min.
5.	Exterior Gloss Level 2 Acrylic Finish:
a.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Eggshell, 589-10 Series. Applied Dry Film Thickness: 1.6 mils min.
6.	Exterior Gloss Level 3 and 4 Acrylic Finish:
a.	Pittsburgh Paints: Speedhide Exterior House and Trim Acrylic Latex Satin, 6-2045XI Series. Applied Dry Film Thickness: 1.0 mil min.
b.	Pittsburgh Paints: Sun Proof Exterior Acrylic Latex Satin, 76-110XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Satin, 739-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	Pittsburgh Paints: Permanizer Exterior Acrylic Latex Satin, 769-10 Series. Applied Dry Film Thickness: 2.2 mils min.
7.	Exterior Gloss Level 3 and 4 High Build Acrylic Finish:
a.	Pittsburgh Paints: Perma-Crete High Build 100 Percent Acrylic Topcoat Satin, 4-422 Series. Applied Dry Film Thickness: 3.0 mils min.
8.	Exterior Gloss Level 5 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Exterior House and Trim Acrylic Latex Semi-Gloss, 6-900XI Series. Applied Dry Film Thickness: 1.5 mils min.
b.	Pittsburgh Paints: Sun Proof Exterior Acrylic Latex Semi-Gloss, 78-811XI Series. Applied Dry Film Thickness: 1.5 mils min.
c.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Semi-Gloss, 649-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	Pittsburgh Paints: Permanizer Exterior Acrylic Latex Semi-Gloss, 749-10 Series. Applied Dry Film Thickness: 2.1 mils min.
e.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Semi-Gloss, 919-10 Series. Applied Dry Film Thickness: 1.5 mils min.
9.	Exterior Gloss Level 6 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior/Exterior High Gloss Acrylic, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
b.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series. Applied Dry Film Thickness: 1.5 mils min.
10.	Exterior Acrylic Texture Finish:
a.	Pittsburgh Paints: Perma-Crete 100 Percent Acrylic Texture Coating, 4-50 Series. Applied Dry Film Thickness: 6.8 mils min.
11.	Exterior Elastomeric Coating:
a.	Pittsburgh Paints: Perma-Crete Pitt-Flex Elastomeric Coating, 4-110XI Series. Applied Dry Film Thickness: 5.4 mils min.
B.	Acrylic Finish: Two finish coats over a block filler.
1.	Substrate:
a.	Exterior Concrete Masonry Units: 
2.	Block Filler: Acrylic.
a.	Pittsburgh Paints: Perma-Crete Concrete Block and Masonry Surfacer/Filler, 4-100XI. Applied Dry Film Thickness: 8.0 mils min.
b.	Pittsburgh Paints: Speedhide Interior/Exterior Masonry Latex Block Filler, 6-7. Applied Dry Film Thickness: 7.1 mils min.
c.	Pittsburgh Paints: Speedhide Interior/Exterior Masonry Hi-Fill Latex Block Filler, 6-15XI. Applied Dry Film Thickness: 8.0 mils min.
3.	Exterior Gloss Level 1 Acrylic Finish:
a.	Pittsburgh Paints: Speedhide Exterior House Flat Latex, 6-610XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: Sun Proof Exterior Acrylic Latex Flat, 72-110XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Flat, 519-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	Pittsburgh Paints: Permanizer Exterior Acrylic Latex Flat, 759-10 Series. Applied Dry Film Thickness: 2.3 mils min.
4.	Exterior Gloss Level 1 High Build Acrylic Finish:
a.	Pittsburgh Paints: Perma-Crete High Build 100 Percent Acrylic Topcoat Flat, 4-22XI Series. Applied Dry Film Thickness: 3.2 mils min.
5.	Exterior Gloss Level 2 Acrylic Finish:
a.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Eggshell, 589-10 Series. Applied Dry Film Thickness: 1.6 mils min.
6.	Exterior Gloss Level 3 and 4 Acrylic Finish:
a.	Pittsburgh Paints: Speedhide Exterior House and Trim Satin-Acrylic Latex, 6-2045XI Series. Applied Dry Film Thickness: 1.0 mil min.
b.	Pittsburgh Paints: Sun Proof Exterior Acrylic Latex Satin, 76-110XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Satin, 739-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	Pittsburgh Paints: Permanizer Exterior Acrylic Latex Satin, 769-10 Series. Applied Dry Film Thickness: 2.2 mils min.
7.	Exterior Gloss Level 3 and 4 High Build Acrylic Finish:
a.	Pittsburgh Paints: Perma-Crete High Build 100 Percent Acrylic Topcoat Satin, 4-422 Series. Applied Dry Film Thickness: 3.0 mils min.
8.	Exterior Gloss Level 5 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Exterior House and Trim Semi-Gloss Acrylic Latex Paint, 6-900XI Series. Applied Dry Film Thickness: 1.5 mils min.
b.	Pittsburgh Paints: Sun Proof Exterior Acrylic Latex Semi-Gloss, 78-811XI Series. Applied Dry Film Thickness: 1.5 mils min.
c.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Semi-Gloss, 649-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	Pittsburgh Paints: Permanizer Exterior Acrylic Latex Semi-Gloss, 749-10 Series. Applied Dry Film Thickness: 2.1 mils min.
e.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Semi-Gloss, 919-10 Series. Applied Dry Film Thickness: 1.5 mils min.
9.	Exterior Gloss Level 6 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior/Exterior High Gloss Acrylic, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
b.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series. Applied Dry Film Thickness: 1.5 mils min.
10.	Exterior Acrylic Texture Finish:
a.	Pittsburgh Paints: Perma-Crete 100 Percent Acrylic Texture Coating, 4-50 Series. Applied Dry Film Thickness: 6.8 mils min.
11.	Exterior Elastomeric Coating:
a.	Pittsburgh Paints: Perma-Crete Pitt-Flex Elastomeric Coating, 4-110XI Series. Applied Dry Film Thickness: 5.4 mils min.
C.	Acrylic or Alkyd Finish: Two finish coats over a primer.
1.	Substrates:
a.	Smooth wood siding.
b.	Wood trim.
c.	Plywood.
d.	Smooth exterior wood surfaces.
2.	Primer:
a.	Pittsburgh Paints: Seal Grip Gripper Interior/Exterior Universal Acrylic Primer, 17-921XI Series. Applied Dry Film Thickness: 1.6 mils min.
b.	Pittsburgh Paints: Seal Grip Interior/Exterior Alkyd Primer, 17-941NF. Applied Dry Film Thickness: 2.2 mils min.
3.	Exterior Gloss Level 1 Acrylic Finish:
a.	Pittsburgh Paints: Speedhide Exterior House Flat Latex, 6-610XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: Sun Proof Exterior Acrylic Latex Flat, 72-110XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Flat, 519-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	Pittsburgh Paints: Permanizer Exterior Acrylic Latex Flat, 759-10 Series. Applied Dry Film Thickness: 2.3 mils min.
4.	Exterior Gloss Level 2 Acrylic Finish:
a.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Eggshell, 589-10 Series. Applied Dry Film Thickness: 1.6 mils min.
5.	Exterior Gloss Level 3 and 4 Acrylic Finish:
a.	Pittsburgh Paints: Speedhide Exterior House and Trim Satin-Acrylic Latex, 6-2045XI Series. Applied Dry Film Thickness: 1.0 mils min.
b.	Pittsburgh Paints: Sun Proof Exterior Acrylic Latex Satin, 76-110XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Satin, 739-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	Pittsburgh Paints: Permanizer Exterior Acrylic Latex Satin, 769-10 Series. Applied Dry Film Thickness: 2.2 mils min.
6.	Exterior Gloss Level 5 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Exterior House and Trim Semi-Gloss Acrylic Latex, 6-900XI Series. Applied Dry Film Thickness: 1.5 mils min.
b.	Pittsburgh Paints: Sun Proof Exterior Acrylic Latex Semi-Gloss, 78-811XI Series. Applied Dry Film Thickness: 1.5 mils min.
c.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Semi-Gloss, 649-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	Pittsburgh Paints: Permanizer Exterior Acrylic Latex Semi-Gloss, 749-10 Series. Applied Dry Film Thickness: 2.1 mils min.
e.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Semi-Gloss, 919-10 Series. Applied Dry Film Thickness: 1.5 mils min.
7.	Exterior Gloss Level 6 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior/Exterior High Gloss Acrylic, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
b.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series. Applied Dry Film Thickness: 1.5 mils min.
8.	Exterior Gloss Level 6 Alkyd Enamel Low Odor Finish:
a.	Pittsburgh Paints: Glyptex Interior/Exterior Alkyd Gloss Enamel, 4139-10 Series. Applied Dry Film Thickness: 1.8 mils min.
D.	Acrylic or Alkyd Finish: Two finish coats over a rust-inhibitive primer.
1.	Substrates:
a.	Ferrous metal.
b.	Aluminum.
2.	Primer:
a.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Primer, 90-1912 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	Pittsburgh Paints: Multiprime 4160 Rust-Inhibitive Interior/Exterior Alkyd Primer, 4160-1000. Applied Dry Film Thickness: 2.0 mils min.
c.	Pittsburgh Paints: Speedhide Alkyd Metal Primer, 6-208N Series. Applied Dry Film Thickness: 2.3 mils min.
3.	Exterior Gloss Level 1 Acrylic Paint Finish:
a.	Pittsburgh Paints: Speedhide Exterior House Flat Latex, 6-610XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: Sun Proof Exterior Acrylic Latex Flat, 72-110XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Flat, 519-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	Pittsburgh Paints: Permanizer Exterior Acrylic Latex Flat, 759-10 Series. Applied Dry Film Thickness: 2.3 mils min.
4.	Exterior Gloss Level 2 Acrylic Finish:
a.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Eggshell, 589-10 Series. Applied Dry Film Thickness: 1.6 mils min.
5.	Exterior Gloss Level 3 and 4 Acrylic Finish:
a.	Pittsburgh Paints: Speedhide Exterior House and Trim Satin-Acrylic Latex, 6-2045XI Series. Applied Dry Film Thickness: 1.0 mils min.
b.	Pittsburgh Paints: Sun Proof Exterior Acrylic Latex Satin, 76-110XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Satin, 739-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	Pittsburgh Paints: Permanizer Exterior Acrylic Latex Satin, 769-10 Series. Applied Dry Film Thickness: 2.2 mils min.
e.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic Satin DTM Industrial Enamel, 90-1710 Series. Applied Dry Film Thickness: 2.0 mils min.
6.	Exterior Gloss Level 5 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Exterior House and Trim Semi-Gloss Acrylic Latex, 6-900XI Series. Applied Dry Film Thickness: 1.5 mils min.
b.	Pittsburgh Paints: Sun Proof Exterior Acrylic Latex Semi-Gloss, 78-811XI Series. Applied Dry Film Thickness: 1.5 mils min.
c.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Semi-Gloss, 649-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	Pittsburgh Paints: Permanizer Exterior Acrylic Latex Semi-Gloss, 749-10 Series. Applied Dry Film Thickness: 2.1 mils min.
e.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Semi-Gloss, 919-10 Series. Applied Dry Film Thickness: 1.5 mils min.
f.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Semi-Gloss, 90-1610 Series. Applied Dry Film Thickness: 2.0 mils min.
7.	Exterior Gloss Level 5 Alkyd Enamel Finish:
a.	Pittsburgh Paints: HPC Urethane Alkyd Semi-Gloss Enamel, 4336H Series. Applied Dry Film Thickness: 2.0 mils min.
8.	Exterior Gloss Level 6 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior/Exterior High Gloss Acrylic, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
b.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series. Applied Dry Film Thickness: 1.5 mils min.
c.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic Gloss DTM Industrial Enamel, 90-1510 Series. Applied Dry Film Thickness: 2.0 mils min.
9.	Exterior Gloss Level 6 Alkyd Enamel Finish:
a.	Pittsburgh Paints: HPC Industrial Alkyd 4308H Interior/Exterior Low VOC, Gloss, 4308H-1000. Applied Dry Film Thickness: 2.0 mils min.
b.	Pittsburgh Paints: 7-Line Interior/Exterior Alkyd Enamel Gloss, 7-282N Series. Applied Dry Film Thickness: 2.0 mils min.
E.	Acrylic or Alkyd Finish: Two finish coats over a rust-inhibitive primer.
1.	Substrates:
a.	Zinc-coated metal.
2.	Primer:
a.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Primer, 90-1912 Series. Applied Dry Film Thickness: 2.0 mils min.
3.	Exterior Gloss Level 1 Acrylic Paint Finish:
a.	Pittsburgh Paints: Speedhide Exterior House Flat Latex, 6-610XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: Sun Proof Exterior Acrylic Latex Flat, 72-110XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Flat, 519-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	Pittsburgh Paints: Permanizer Exterior Acrylic Latex Flat, 759-10 Series. Applied Dry Film Thickness: 2.3 mils min.
4.	Exterior Gloss Level 2 Acrylic Finish:
a.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Eggshell, 589-10 Series. Applied Dry Film Thickness: 1.6 mils min.
5.	Exterior Gloss Level 3 and 4 Acrylic Finish:
a.	Pittsburgh Paints: Speedhide Exterior House and Trim Satin-Acrylic Latex, 6-2045XI Series. Applied Dry Film Thickness: 1.0 mils min.
b.	Pittsburgh Paints: Sun Proof Exterior Acrylic Latex Satin, 76-110XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Satin, 739-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	Pittsburgh Paints: Permanizer Exterior Acrylic Latex Satin, 769-10 Series. Applied Dry Film Thickness: 2.2 mils min.
e.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Satin, 90-1710 Series. Applied Dry Film Thickness: 2.0 mils min.
6.	Exterior Gloss Level 5 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Exterior House and Trim Semi-Gloss Acrylic Latex, 6-900XI Series. Applied Dry Film Thickness: 1.5 mils min.
b.	Pittsburgh Paints: Sun Proof Exterior Acrylic Latex Semi-Gloss, 78-811XI Series. Applied Dry Film Thickness: 1.5 mils min.
c.	Pittsburgh Paints: Acri-Shield Max Exterior Acrylic Latex Semi-Gloss, 649-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	Pittsburgh Paints: Permanizer Exterior Acrylic Latex Semi-Gloss, 749-10 Series. Applied Dry Film Thickness: 2.1 mils min.
e.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Semi-Gloss, 919-10 Series. Applied Dry Film Thickness: 1.5 mils min.
f.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Semi-Gloss, 90-1610 Series. Applied Dry Film Thickness: 2.0 mils min.
7.	Exterior Gloss Level 6 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior/Exterior High Gloss Acrylic, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
b.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series. Applied Dry Film Thickness: 1.5 mils min.
c.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic Gloss DTM Industrial Enamel, 90-1510 Series. Applied Dry Film Thickness: 2.0 mils min.
2.4	EXTERIOR STAIN SYSTEMS
A.	Alkyd-Based Toner Wood Finish: Penetrating sealer/finish system applied on properly cleaned and prepared wood surface.
1.	Substrate:
a.	Stained Woodwork: Provide the following stain finishes over new exterior woodwork, for use with both vertical siding/trim and horizontal deck applications unless otherwise stated.
2.	Sealer/Finish Coat:
a.	Pittsburgh Paints: Flood CWF-OIL Penetrating Oil Wood Finish, FLD447. Apply two coats using a wet-on-wet application.
b.	Pittsburgh Paints: ProLuxe SRD Wood Finish (Transparent Matte). Apply 1 coat, SIK240 Series.
c.	Pittsburgh Paints: ProLuxe SRD RE Wood Finish (Transparent Matte), SIK250 Series. Apply 1 coat.
d.	Pittsburgh Paints:  ProLuxe Premium Deck RE Wood Finish (Transparent Satin), SIK440xxLV Series. Apply two coats.
e.	Pittsburgh Paints: ProLuxe Premium Deck Wood Finish (Transparent Satin), SIK440 Series. Apply two coats.
B.	Alkyd-Based Toner Wood Finish Penetrating sealer/finish system applied on properly cleaned and prepared vertical wood surface. Not for deck applications.
1.	Substrate:
a.	Vertical Siding/Trim Applications:
2.	Sealer Coat:
a.	Pittsburgh Paints: ProLuxe 1 Primary RE Wood Finish (Transparent Matte), SIK410 Series. Use with SIK300 Series 23 Top Coat RE Wood Finish.
3.	Finish Coat:
a.	Pittsburgh Paints: ProLuxe 23 Top Coat RE Wood Finish (Transparent Satin), SIK300 Series. Apply 2 coats over SIK410 Series 1 Primary RE Wood Finish.
4.	Sealer/Finish Coat:
a.	Pittsburgh Paints:  ProLuxe Door and Window RE Wood Finish (Transparent Satin), SIK480xxLV Series. Apply 3 coats.
b.	Pittsburgh Paints:  ProLuxe Door and Window Wood Finish (Transparent Satin), SIK480 Series. Apply 3 coats.
c.	Pittsburgh Paints:  ProLuxe Log and Siding RE Wood Finish (Transparent Satin), SIK420xxLV Series. Apply 2 coats. 
d.	ProLuxe:  Log and Siding Wood Finish (Transparent Satin), SIK420 Series. Apply 2 coats.
5.	Clear Coat:
a.	Pittsburgh Paints: ProLuxe Door and Window Wood Finish (Transparent Satin), SIK48003. Apply over SIK480 Series as needed to maintain sheen.
6.	Clear Maintenance Coat:
a.	Pittsburgh Paints: ProLuxe Maintenance RE Wood Finish (Clear Satin), SIK61003LV. Apply over SIK420xxLV, SIK420 or SIK 300 Series as needed to maintain sheen. Vertical applications only.
b.	Pittsburgh Paints: ProLuxe Maintenance RE Wood Finish (Clear Satin), SIK61003. Apply over SIK420 or SIK 300 Series as needed to maintain sheen. Vertical applications only.
C.	Acrylic-Oil Toner Wood Finish: Penetrating sealer/finish system.
1.	Substrate:
a.	Properly cleaned and prepared wood surface:
2.	Sealer/Finish Coat:
a.	Pittsburgh Paints: Flood CWF-UV Penetrating Wood Finish, FLD520 Series. Apply 1 coat.
b.	Pittsburgh Paints: Flood CWF-UV5 Penetrating Wood Finish, FLD565 Series. Apply 1 coat.
D.	Alkyd-Based Semi-Transparent Wood Finish: Penetrating sealer/finish system.
1.	Substrate:
a.	Properly cleaned and prepared wood surface.
2.	Sealer/Finish Coat:
a.	Pittsburgh Paints: Flood Semi-Transparent Alkyd-Oil Wood Finish, FLD802 Series. Apply 1 coat.
E.	Acrylic-Oil Semi-Transparent Wood Finish: Penetrating sealer/finish systems.
1.	Substrate: Properly cleaned and prepared wood surface.
2.	Sealer/Finish Coat:
a.	Pittsburgh Paints: Flood Semi-Transparent Acrylic-Oil Wood Finish, FLD812 Series. Apply 1 coat.
F.	Acrylic Based Semi-Transparent Wood Finish: Penetrating sealer/finish system.
1.	Substrate:
a.	Properly cleaned and prepared wood surface.
2.	Sealer/Finish Coat:
a.	Pittsburgh Paints: ProLuxe SRD Semi-Transparent Wood Finish (Matte), SIK500 Series. Apply 1 coat.
G.	Alkyd-Oil Semi-Opaque Wood Finish: Penetrating sealer/finish system.
1.	Substrate:
a.	Properly cleaned and prepared wood surface.
2.	Sealer/Finish Coat:
a.	Pittsburgh Paints: Flood Semi-Opaque Alkyd-Oil Wood Finish, FLD842 Series. Apply 2 coats using a wet-on-wet application.
H.	Acrylic Solid Color Wood Finish: Acrylic topcoat system.
1.	Substrate:
a.	Properly cleaned and prepared wood surface.
2.	Sealer/Finish Coat:
a.	Pittsburgh Paints: Flood Acrylic Solid Color Matte Wood Finish, FLD820 Series. Apply 2 coats.
b.	Pittsburgh Paints: ProLuxe Premium Solid Stain Wood Finish (Matte), SIK710 Series. Apply 2 coats.
2.5	EXTERIOR NATURAL FINISH WOODWORK SYSTEMS - STAINED FINISHES OVER NEW WOODWORK.
A.	Clear Penetrating Wood Finish: Penetrating sealer/finish system.
1.	Substrate:
a.	Properly cleaned and prepared wood surface.
2.	Sealer/Finish Coat:
a.	Pittsburgh Paints: Flood CWF Multi-Surface Waterproofing Clear Sealant, FLD540XI. Apply 2 coats using a wet-on-wet application.
b.	Pittsburgh Paints: Flood CWF-UV Clear/Natural Penetrating Wood Finish, FLD542 Series. Apply 1 coat.
c.	Pittsburgh Paints: Flood CWF-UV5 Clear/Natural Penetrating Wood Finish, FLD565 Series. Apply 1 coat.
2.6	INTERIOR PAINT SYSTEMS
A.	Acrylic or Alkyd Finish: Two finish coats over a primer.
1.	Substrates:
a.	Concrete and masonry other than concrete unit masonry.
b.	Gypsum board.
c.	Plaster.
d.	Acoustical plaster.
e.	Wood and hardboard.
2.	Level-Five Primer: To achieve level-five finish on drywall/gypsum board only.
a.	Pittsburgh Paints: Speedhide Maxbuild Interior High Build Drywall Surfacer, 6-1. Applied Dry Film Thickness: 6.9 mils min.
3.	Primer:
a.	Pittsburgh Paints: Seal Grip Gripper Interior/Exterior Universal Acrylic Primer, 17-921XI Series. Applied Dry Film Thickness: 1.6 mils min.
b.	Pittsburgh Paints: Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI. Applied Dry Film Thickness: 1.4 mils min.
c.	Pittsburgh Paints: Speedhide Interior Quick-Drying Latex Sealer, 6-2. Applied Dry Film Thickness: 1.0 mils min.
d.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Primer, 6-4900XI. Applied Dry Film Thickness: 1.2 mils min.
e.	Pittsburgh Paints: Seal Grip Interior/Exterior Alkyd Universal Primer/Sealer, 17-941NF. Applied Dry Film Thickness: 2.3 mils min.
4.	Interior Gloss Level 1 Acrylic Finish Low VOC:
a.	Pittsburgh Paints: Speedhide Interior Latex Ultra-Flat, 6-0011 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: Hi-Hide Interior Latex Ultra-Flat, 679-10 Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh Paints: Speedhide Interior Wall Flat-Latex Paint, 6-70 Series. Applied Dry Film Thickness: 1.3 mils min.
d.	Pittsburgh Paints: Hi-Hide Interior Latex Flat, 689-10 Series. Applied Dry Film Thickness: 1.1 mils min.
e.	Pittsburgh Paints: Hi-Hide Interior Latex Ceramic Matte, 369-10 Series. Applied Dry Film Thickness: 1.1 mils min.
5.	Interior Gloss Level 1 Acrylic Finish - Zero VOC:
a.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series. Applied Dry Film Thickness: 1.3 mils min. 
b.	Pittsburgh Paints: Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series. Applied Dry Film Thickness: 1.3 mils min.
c.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series. Applied Dry Film Thickness:   1.2 mils min.
d.	Pittsburgh Paints: Pure Performance Interior Acrylic Latex Flat, 9-110XI Series. Applied Dry Film Thickness: 1.4 mils min.
e.	Pittsburgh Paints: Prominence Interior Acrylic Latex Flat, 84-3110 Series. Applied Dry Film Thickness: 1.8 mils min.
6.	Interior Gloss Level 1 High Build Acrylic Finish:
a.	Pittsburgh Paints: Perma-Crete High Build 100 Percent Acrylic Topcoat Flat, 4-22XI Series. Applied Dry Film Thickness:   3.2 mils min.
7.	Interior Gloss Level 2 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior Latex Low-Sheen Eggshell, 6-4101 Series. Applied Dry Film Thickness:   1.5 mils min.
b.	Pittsburgh Paints: Speedhide Interior Latex Eggshell, 6-411 Series. Applied Dry Film Thickness:   1.5 mils min.
c.	Pittsburgh Paints: Hi-Hide Interior Latex Eggshell, 389-10 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	Pittsburgh Paints: UltraLast Interior Latex Paint and Primer in One Matte, 13-210 Series. Applied Dry Film Thickness: 1.7 mils min.
8.	Interior Gloss Level 2 Acrylic Enamel Finish-Zero VOC:
a.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Low-Sheen Eggshell, 6-4101ZV Series. Applied Dry Film Thickness: 1.5 mils min. 
b.	Pittsburgh Paints: Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series. Applied Dry Film Thickness: 1.3 mils min.
c.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series. Applied Dry Film Thickness:   1.5 mils min.
d.	Pittsburgh Paints:  Speedhide Max Interior Latex Eggshell, 6-9310 Series. Applied Dry Film Thickness:  1.3 mils min. 
e.	Pittsburgh Paints: Pure Performance Interior Acrylic Latex Eggshell, 9-310XI Series. Applied Dry Film Thickness: 1.4 mils min.
f.	Pittsburgh Paints: Prominence Interior Acrylic Latex Eggshell, 84-3310 Series. Applied Dry Film Thickness: 1.6 mils min.
9.	Interior Gloss Level 3 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior Latex Satin, 6-3511 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: UltraLast Interior Latex Paint and Primer Eggshell, 13-310 Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Satin, 90-1710 Series. Applied Dry Film Thickness: 2.0 mils min.
10.	Interior Gloss Level 3 Acrylic Enamel Finish Zero VOC:
a.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series. Applied Dry Film Thickness:   1.4 mils min.
b.	Pittsburgh Paints:   Speedhide Max Interior Latex Satin, 6-9410 Series. Applied Dry Film Thickness:  1.4 mils min. 
c.	Pittsburgh Paints: Prominence Interior Acrylic Latex Satin, 84-3410 Series. Applied Dry Film Thickness: 1.6 mils min.
11.	Interior Gloss Level 3 High Build Acrylic Finish:
a.	Pittsburgh Paints: Perma-Crete High Build 100 Percent Acrylic Topcoat Satin, 4-422 Series. Applied Dry Film Thickness: 3.0 mils min.
12.	Interior Gloss Level 3 Alkyd Enamel Finish:
a.	Pittsburgh Paints: Glyptex Interior Alkyd Enamel Satin, 39-10 Series. Applied Dry Film Thickness: 2.0 mils min.
13.	Interior Gloss Level 3 Water-Based Epoxy Finish:
a.	Pittsburgh Paints: Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series. Applied Dry Film Thickness: 1.5 mils min.
14.	Interior Gloss Level 4 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior Lo Lustre Latex, 6-3011 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: Hi-Hide Interior Latex Satin, 379-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	Pittsburgh Paints: Breakthrough Interior/Exterior Waterborne Acrylic Satin, V52-410 Series. Applied Dry Film Thickness: 1.4 mils min.
15.	Interior Gloss Level 4 Acrylic Enamel Finish Zero VOC:
a.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series. Applied Dry Film Thickness: 1.1 mils min.
b.	Pittsburgh Paints:  Speedhide Max Interior Latex Lo Lustre, 6-9610 Series. Applied Dry Film Thickness:  1.4 mils min.
16.	Interior Gloss Level 5 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior Semi-Gloss Latex, 6-500 Series. Applied Dry Film Thickness: 1.4 mils min.
b.	Pittsburgh Paints: Hi-Hide Interior Latex Semi-Gloss, 109-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Semi-Gloss, 919-10 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	Pittsburgh Paints: UltraLast Interior Latex Paint and Primer in One Semi-Gloss, 13-510 Series. Applied Dry Film Thickness: 1.5 mils min.
e.	Pittsburgh Paints: Breakthrough Interior/Exterior Waterborne Acrylic Semi-Gloss, V62-510 Series. Applied Dry Film Thickness: 1.5 mils min.
f.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic Semi-Gloss DTM Industrial Enamel, 90-1610 Series. Applied Dry Film Thickness: 2.0 mils min.
17.	Interior Gloss Level 5 Acrylic Enamel Finish-Zero VOC:
a.	Pittsburgh Paints: Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh  Paints: Speedhide zero Interior Latex Semi-Gloss, 6-500ZV Series. Applied Dry Film Thickness:   1.5 mils min.
c.	Pittsburgh Paints: Pure Performance Interior Acrylic Latex Semi-Gloss, 9-510XI Series. Applied Dry Film Thickness: 1.4 mils min.
d.	Pittsburgh Paints: Prominence Interior Acrylic Latex Semi-Gloss, 84-3510 Series. Applied Dry Film Thickness: 1.6 mils min.
18.	Interior Gloss Level 5 Alkyd Enamel Finish:
a.	Pittsburgh Paints: Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	Pittsburgh Paints: HPC Urethane Alkyd Semi-Gloss Enamel, 4336H Series. Applied Dry Film Thickness: 2.0 mils min.
19.	Interior Gloss Level 5 Water-Based Epoxy Finish:
a.	Pittsburgh Paints: Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series. Applied Dry Film Thickness: 1.6 mils min.
20.	Interior Gloss Level 6 and 7 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior/Exterior High Gloss Acrylic, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
b.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	Pittsburgh Paints: Breakthrough Interior/Exterior Waterborne Acrylic Gloss, V72-610 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic Gloss DTM Industrial Enamel, 90-1510 Series. Applied Dry Film Thickness: 1.5 mils min.
21.	Interior Gloss Level 6 and 7 Alkyd Enamel Low Odor Finish:
a.	Pittsburgh Paints: Glyptex Interior/Exterior Alkyd Gloss Enamel, 4139-10 Series. Applied Dry Film Thickness: 1.8 mils min.
b.	Pittsburgh Paints: HPC Industrial Alkyd 4308H Interior/Exterior Low VOC, Gloss, 4308H-1000. Applied Dry Film Thickness: 2.0 mils min.
c.	Pittsburgh Paints: 7-Line Interior/Exterior Alkyd Enamel Gloss, 7-282N Series. Applied Dry Film Thickness:   2.0 mils min.
22.	Interior Acrylic Texture Finish:
a.	Pittsburgh Paints: Perma-Crete 100 Percent Acrylic Texture Coating, 4-50 Series. Applied Dry Film Thickness: 6.8 mils min.
23.	Interior Elastomeric Coating:
a.	Pittsburgh Paints: Perma-Crete Pitt-Flex Elastomeric Coating, 4-110XI Series. Applied Dry Film Thickness: 5.4 mils min.
B.	Acrylic or Alkyd Finish: Two finish coats over a block filler.
1.	Substrate:
a.	Concrete Unit Masonry. 
2.	Block Filler:
a.	Pittsburgh Paints: Perma-Crete Concrete Block and Masonry Surfacer/Filler, 4-100XI. Applied Dry Film Thickness: 8.0 mils min.
b.	Pittsburgh Paints: Speedhide Interior/Exterior Masonry Latex Block Filler, 6-7. Applied Dry Film Thickness: 6.0 to 14.0 mils min.
c.	Pittsburgh Paints: Speedhide Interior/Exterior Acrylic Masonry Block Filler, 6-15XI. Applied Dry Film Thickness: 8.0 mils min.
3.	Interior Gloss Level 1 Acrylic Finish:
a.	Pittsburgh Paints:   Speedhide Interior Latex Ultra-Flat, 6-0011 Series. Applied Dry Film Thickness:  1.3 mils min. 
b.	Pittsburgh Paints: Hi-Hide Interior Latex Ultra-Flat, 679-10 Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh Paints: Speedhide Interior Flat-Latex, 6-70 Series. Applied Dry Film Thickness: 1.3 mils min.
d.	Pittsburgh Paints: Hi-Hide Interior Latex Flat, 689-10 Series. Applied Dry Film Thickness: 1.1 mils min.
e.	Pittsburgh Paints: Hi-Hide Interior Latex Ceramic Matte, 369-10 Series. Applied Dry Film Thickness: 1.1 mils min.
4.	Interior Gloss Level 1 Acrylic Finish-Zero VOC:
a.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series. Applied Dry Film Thickness:  1.3 mils min. 
b.	Pittsburgh Paints: Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series. Applied Dry Film Thickness: 1.3 mils min.
c.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series. Applied Dry Film Thickness:   1.2 mils min.
d.	Pittsburgh Paints: Pure Performance Interior Acrylic Latex Flat, 9-110XI Series. Applied Dry Film Thickness: 1.4 mils min.
e.	Pittsburgh Paints: Prominence Interior Acrylic Latex Flat, 84-3110 Series. Applied Dry Film Thickness: 1.8 mils min.
5.	Interior Gloss Level 1 High Build Acrylic Finish:
a.	Pittsburgh Paints: Perma-Crete High Build 100 Percent Acrylic Topcoat Flat, 4-22XI Series. Applied Dry Film Thickness: 3.2 mils min.
6.	Interior Gloss Level 2 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior Latex Low-Sheen Eggshell 6-4101 Series. Applied Dry Film Thickness: 1.5 mils min.
b.	Pittsburgh Paints: Speedhide Eggshell Acrylic Latex Enamel, 6-411 Series. Applied Dry Film Thickness: 1.5 mils min.
c.	Pittsburgh Paints: Hi-Hide Interior Latex Eggshell, 389-10 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	Pittsburgh Paints: UltraLast Interior Latex Paint and Primer Matte, 13-210 Series. Applied Dry Film Thickness: 1.7 mils min.
7.	Interior Gloss Level 2 Acrylic Enamel Finish-Zero VOC:
a.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Low-Sheen Eggshell, 6-4101ZV Series. Applied Dry Film Thickness:  1.5 mils min. 
b.	Pittsburgh Paints: Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series. Applied Dry Film Thickness: 1.3 mils min.
c.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series. Applied Dry Film Thickness:   1.5 mils min.
d.	Pittsburgh Paints: Speedhide Max Interior Latex Eggshell, 6-9310 Series. Applied Dry Film Thickness:  1.3 mils min.
e.	Pittsburgh Paints: Pure Performance Interior Acrylic Latex Eggshell, 9-310XI Series. Applied Dry Film Thickness: 1.4 mils min.
f.	Pittsburgh Paints: Prominence Interior Acrylic Latex Eggshell, 84-3310 Series. Applied Dry Film Thickness: 1.6 mils min.
8.	Interior Gloss Level 3 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior Satin Latex, 6-3511 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: UltraLast Interior Latex Paint and Primer Eggshell, 13-310 Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic Satin DTM Industrial Enamel, 90-1710 Series. Applied Dry Film Thickness: 2.0 mils min.
9.	Interior Gloss Level 3 Acrylic Enamel Finish Zero VOC:
a.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series. Applied Dry Film Thickness:   1.4 mils min.
b.	Pittsburgh Paints: Speedhide Max Interior Latex Satin, 6-9410 Series. Applied Dry Film Thickness:  1.4 mils min. 
c.	Pittsburgh Paints: Prominence Interior Acrylic Latex Satin, 84-3410 Series. Applied Dry Film Thickness: 1.6 mils min.
10.	Interior Gloss Level 3 High Build Acrylic Finish:
a.	Pittsburgh Paints: Perma-Crete High Build 100 Percent Acrylic Topcoat Satin, 4-422 Series. Applied Dry Film Thickness: 3.0 mils min.
11.	Interior Gloss Level 3 Alkyd Enamel Finish:
a.	Pittsburgh Paints: Glyptex Interior Alkyd Enamel Satin, 39-10 Series. Applied Dry Film Thickness: 2.0 mils min.
12.	Interior Gloss Level 3 Water-Based Epoxy Finish:
a.	Pittsburgh Paints: Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series. Applied Dry Film Thickness: 1.5 mils min.
13.	Interior Gloss Level 4 Acrylic Enamel Finish:
a.	Pittsburgh  Paints: Speedhide Interior Latex Lo-Lustre, 6-3011 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: Hi-Hide Interior Latex Satin, 379-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	Pittsburgh Paints: Breakthrough Interior/Exterior Waterborne Acrylic Satin, V52-410 Series. Applied Dry Film Thickness:   1.4 mils min.
14.	Interior Gloss Level 4 Acrylic Enamel Finish Zero VOC:
a.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series. Applied Dry Film Thickness: 1.1 mils min.
b.	Pittsburgh Paints:  Speedhide Max Interior Latex Lo Lustre, 6-9610 Series. Applied Dry Film Thickness:  1.4 mils min. 
15.	Interior Gloss Level 5 Acrylic Enamel:
a.	Pittsburgh Paints: Speedhide Interior Latex Semi-Gloss, 6-500 Series. Applied Dry Film Thickness:   1.4 mils min.
b.	Pittsburgh Paints: Hi-Hide Interior Latex Semi-Gloss, 109-10 Series. Applied Dry Film Thickness:   1.4 mils min.
c.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Semi-Gloss, 919-10 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	Pittsburgh Paints: UltraLast Interior Latex Paint and Primer Semi-Gloss, 13-510 Series. Applied Dry Film Thickness: 1.5 mils min.
e.	Pittsburgh Paints: Breakthrough Interior/Exterior Waterborne Acrylic Semi-Gloss, V62-510 Series. Applied Dry Film Thickness: 1.5 mils min.
f.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Semi-Gloss, 90-1610 Series. Applied Dry Film Thickness: 2.0 mils min.
16.	Interior Gloss Level 5 Acrylic Enamel-Zero VOC:
a.	Pittsburgh Paints: Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series. Applied Dry Film Thickness:   1.5 mils min.
c.	Pittsburgh Paints: Pure Performance Interior Acrylic Latex Semi-Gloss, 9-510XI Series. Applied Dry Film Thickness: 1.4 mils min.
d.	Pittsburgh Paints: Prominence Interior Acrylic Latex Semi-Gloss, 84-3510 Series. Applied Dry Film Thickness: 1.6 mils min.
17.	Interior Gloss Level 5 Alkyd Enamel Finish:
a.	Pittsburgh Paints: Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	Pittsburgh Paints: HPC Urethane Alkyd Enamel Semi-Gloss, 4336H Series. Applied Dry Film Thickness:   2.0 mils min.
18.	Interior Gloss Level 5 Water-Based Epoxy Finish:
a.	Pittsburgh Paints: Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series. Applied Dry Film Thickness: 1.6 mils min.
19.	Interior Gloss Level 6 and 7 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior/Exterior Acrylic High Gloss, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
b.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	Pittsburgh Paints: Breakthrough Interior/Exterior Waterborne Acrylic Gloss, V72-610 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Gloss, 90-1510 Series. Applied Dry Film Thickness: 1.5 mils min.
20.	Interior Gloss Level 6 and 7 Alkyd Enamel Low Odor Finish:
a.	Pittsburgh Paints: Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series. Applied Dry Film Thickness:   1.8 mils min.
b.	Pittsburgh Paints: HPC Industrial Alkyd 4308H Interior/Exterior Low VOC Gloss, 4308H-1000 Series. Applied Dry Film Thickness:   2.0 mils min.
c.	Pittsburgh Paints: 7-Line Interior/Exterior Alkyd Enamel Gloss, 7-282N Series. Applied Dry Film Thickness:   2.0 mils min.
21.	Interior Acrylic Texture Finish:
a.	Pittsburgh Paints: Perma-Crete 100 Percent Acrylic Texture Coating, 4-50 Series. Applied Dry Film Thickness: 6.8 mils min.
22.	Interior Elastomeric Coating:
a.	Pittsburgh Paints: Perma-Crete Pitt-Flex Elastomeric Coating, 4-110XI Series. Applied Dry Film Thickness: 5.4 mils min.
C.	Acrylic or Alkyd Finish: Two finish coats over a primer.
1.	Substrate:
a.	Ferrous Metal.
2.	Primer:
a.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Primer, 90-1912 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	Pittsburgh Paints: Multiprime 4160 Rust-Inhibitive Interior/Exterior Alkyd Primer, 4160-1000 Series. Applied Dry Film Thickness: 2.0 mils min.
c.	Pittsburgh Paints: Speedhide Alkyd Metal Primer, 6-208N Series. Applied Dry Film Thickness: 2.3 mils min.
3.	Interior Gloss Level 1 Acrylic Finish:
a.	Pittsburgh Paints: Speedhide Interior Latex Ultra-Flat, 6-0011 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: Hi-Hide Interior Latex Ultra-Flat, 679-10 Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh Paints: Speedhide Interior Latex Flat, 6-70 Series. Applied Dry Film Thickness: 1.3 mils min.
d.	Pittsburgh Paints: Hi-Hide Interior Latex Flat, 689-10 Series. Applied Dry Film Thickness: 1.1 mils min.
e.	Pittsburgh Paints: Hi-Hide Interior Latex Ceramic Matte, 369-10 Series. Applied Dry Film Thickness: 1.1 mils min.
4.	Interior Gloss Level 1 Acrylic Finish-Zero VOC:
a.	Pittsburgh  Paints:   Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series. Applied Dry Film Thickness:  1.3 mils min. 
b.	Pittsburgh Paints: Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series. Applied Dry Film Thickness: 1.3 mils min.
c.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series. Applied Dry Film Thickness:   1.2 mils min.
d.	Pittsburgh Paints: Pure Performance Interior Acrylic Latex Flat, 9-110XI Series. Applied Dry Film Thickness: 1.4 mils min.
e.	Pittsburgh Paints: Prominence Interior Acrylic Latex Flat, 84-3110 Series. Applied Dry Film Thickness: 1.8 mils min.
5.	Interior Gloss Level 2 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior Latex Low-Sheen Eggshell, 6-4101 Series. Applied Dry Film Thickness:   1.5 mils min.
b.	Pittsburgh Paints: Speedhide Interior Latex Eggshell, 6-411 Series. Applied Dry Film Thickness: 1.5 mils min.
c.	Pittsburgh Paints: Hi-Hide Interior Latex Eggshell, 389-10 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	Pittsburgh Paints: UltraLast Interior Latex Paint and Primer Matte, 13-210 Series. Applied Dry Film Thickness: 1.7 mils min.
6.	Interior Gloss Level 2 Acrylic Enamel Finish-Zero VOC:
a.	Pittsburgh Paints:   Speedhide Interior Zero VOC Latex Low-Sheen Eggshell, 6-4101ZV Series. Applied Dry Film Thickness:  1.5 mils min. 
b.	Pittsburgh Paints: Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series. Applied Dry Film Thickness: 1.3 mils min.
c.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series. Applied Dry Film Thickness:   1.5 mils min.
d.	Pittsburgh Paints:  Speedhide Max Interior Latex Eggshell, 6-9310 Series. Applied Dry Film Thickness:  1.3 mils min. 
e.	Pittsburgh Paints: Pure Performance Interior Acrylic Latex Eggshell, 9-310XI Series. Applied Dry Film Thickness: 1.4 mils min.
f.	Pittsburgh Paints: Prominence Interior Acrylic Latex Eggshell, 84-3310 Series. Applied Dry Film Thickness: 1.6 mils min.
7.	Interior Gloss Level 3 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior Latex Satin, 6-3511 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: UltraLast Interior Latex Paint and Primer Eggshell, 13-310 Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh  Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Satin, 90-1710 Series. Applied Dry Film Thickness: 2.0 mils min.
8.	Interior Gloss Level 3 Acrylic Enamel Finish Zero VOC:
a.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Satin, 6-3511ZV Series. Applied Dry Film Thickness:   1.4 mils min.
b.	Pittsburgh Paints:   Speedhide Max Interior Latex Satin, 6-9410 Series. Applied Dry Film Thickness:  1.4 mils min.
c.	Pittsburgh Paints: Prominence Interior Acrylic Latex Satin, 84-3410 Series. Applied Dry Film Thickness: 1.6 mils min.
9.	Interior Gloss Level 3 Alkyd Enamel Finish:
a.	Pittsburgh Paints: Glyptex Interior Alkyd Enamel Satin, 39-10 Series. Applied Dry Film Thickness: 2.0 mils min.
10.	Interior Gloss Level 3 Water-Based Epoxy Finish:
a.	Pittsburgh Paints: Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series. Applied Dry Film Thickness: 1.5 mils min.
11.	Interior Gloss Level 4 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior Latex Lo-Lustre, 6-3011 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: Hi-Hide Interior Latex Satin, 379-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	Pittsburgh  Paints: Breakthrough Interior/Exterior Waterborne Acrylic Satin, V52-410 Series. Applied Dry Film Thickness:   1.4 mils min.
12.	Interior Gloss Level 4 Acrylic Enamel Finish Zero VOC:
a.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Lo Lustre, 6-3011ZV Series. Applied Dry Film Thickness: 1.1 mils min.
b.	Pittsburgh Paints: Speedhide Max Interior Latex Lo Lustre, 6-9610 Series. Applied Dry Film Thickness:  1.4 mils min.
13.	Interior Gloss Level 5 Acrylic Enamel:
a.	Pittsburgh Paints: Speedhide Interior Latex Semi-Gloss, 6-500 Series. Applied Dry Film Thickness:   1.4 mils min.
b.	Pittsburgh Paints: Hi-Hide Interior Latex Semi-Gloss, 109-10 Series. Applied Dry Film Thickness:   1.4 mils min.
c.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Semi-Gloss, 919-10 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	Pittsburgh Paints: UltraLast Interior Latex Paint and Primer Semi-Gloss, 13-510 Series. Applied Dry Film Thickness: 1.5 mils min.
e.	Pittsburgh Paints: Breakthrough Interior/Exterior Waterborne Acrylic Semi-Gloss, V62-510 Series. Applied Dry Film Thickness: 1.5 mils min.
f.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Semi-Gloss, 90-1610 Series. Applied Dry Film Thickness: 2.0 mils min.
14.	Interior Gloss Level 5 Acrylic Enamel-Zero VOC:
a.	Pittsburgh Paints: Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Semi-Gloss, 6-500ZV Series. Applied Dry Film Thickness:   1.5 mils min.
c.	Pittsburgh Paints: Pure Performance Interior Acrylic Latex Semi-Gloss, 9-510XI Series. Applied Dry Film Thickness: 1.4 mils min.
d.	Pittsburgh Paints: Prominence Interior Acrylic Latex Semi-Gloss, 84-3510 Series. Applied Dry Film Thickness: 1.6 mils min.
15.	Interior Gloss Level 5 Alkyd Enamel Finish:
a.	Pittsburgh Paints: Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	Pittsburgh Paints: HPC Urethane Alkyd Enamel Semi-Gloss, 4336H Series. Applied Dry Film Thickness:   2.0 mils min.
16.	Interior Gloss Level 5 Water-Based Epoxy Finish:
a.	Pittsburgh Paints: Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series. Applied Dry Film Thickness:   1.6 mils min.
17.	Interior Gloss Level 6 and 7 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior/Exterior Acrylic High Gloss, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
b.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	Pittsburgh Paints: Breakthrough Interior/Exterior Waterborne Acrylic Gloss, V72-610 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Gloss, 90-1510 Series. Applied Dry Film Thickness: 2.0 mils min.
18.	Interior Gloss Level 6 and 7 Alkyd Enamel Finish:
a.	Pittsburgh Paints: Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series. Applied Dry Film Thickness:   1.8 mils min.
b.	Pittsburgh Paints: HPC Industrial Alkyd 4308H Interior/Exterior Low VOC Gloss, 4308H-1000 Series. Applied Dry Film Thickness:   2.0 mils min.
c.	Pittsburgh Paints: 7-Line Interior/Exterior Alkyd Enamel Gloss, 7-282N Series. Applied Dry Film Thickness:   2.0 mils min.
D.	Acrylic or Alkyd Finish: Two finish coats over a primer.
1.	Substrates:
a.	Zinc-Coated Metal.
2.	Primer:
a.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Primer, 90-1912 Series. Applied Dry Film Thickness: 2.0 mils min.
3.	Interior Gloss Level 1 Acrylic Finish:
a.	Pittsburgh Paints: Speedhide Interior Latex Ultra-Flat, 6-0011 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: Hi-Hide Interior Latex Ultra-Flat, 679-10 Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh Paints: Speedhide Interior Latex Flat, 6-70 Series. Applied Dry Film Thickness: 1.3 mils min.
d.	Pittsburgh Paints: Hi-Hide Interior Latex Flat, 689-10 Series. Applied Dry Film Thickness: 1.1 mils min.
e.	Pittsburgh Paints: Hi-Hide Interior Latex Ceramic Matte, 369-10 Series. Applied Dry Film Thickness: 1.1 mils min.
4.	Interior Gloss Level 1 Acrylic Finish-Zero VOC:
a.	Pittsburgh Paints:   Speedhide Interior Zero VOC Latex Ultra-Flat, 6-0011ZV Series. Applied Dry Film Thickness:  1.3 mils min. 
b.	Pittsburgh Paints: Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series. Applied Dry Film Thickness: 1.3 mils min.
c.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Flat, 6-70ZV Series. Applied Dry Film Thickness:   1.2 mils min.
d.	Pittsburgh Paints: Pure Performance Interior Acrylic Latex Flat, 9-110XI Series. Applied Dry Film Thickness: 1.4 mils min.
e.	Pittsburgh Paints: Prominence Interior Acrylic Latex Flat, 84-3110 Series. Applied Dry Film Thickness: 1.8 mils min.
5.	Interior Gloss Level 2 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior Latex Low-Sheen Eggshell, 6-4101 Series. Applied Dry Film Thickness:   1.5 mils min.
b.	Pittsburgh Paints: Speedhide Interior Latex Eggshell, 6-411 Series. Applied Dry Film Thickness:   1.5 mils min.
c.	Pittsburgh Paints: Hi-Hide Interior Latex Eggshell, 389-10 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	Pittsburgh Paints: UltraLast Interior Latex Paint and Primer Matte, 13-210 Series. Applied Dry Film Thickness: 1.7 mils min.
6.	Interior Gloss Level 2 Acrylic Enamel Finish-Zero VOC:
a.	Pittsburgh Paints:   Speedhide Interior Zero VOC Latex Low-Sheen Eggshell, 6-4101ZV Series. Applied Dry Film Thickness:  1.5 mils min. 
b.	Pittsburgh Paints: Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series. Applied Dry Film Thickness: 1.3 mils min.
c.	Pittsburgh Paints: Speedhide Interior Zero VOC Latex Eggshell, 6-411ZV Series. Applied Dry Film Thickness:   1.5 mils min.
d.	Pittsburgh Paints:  Speedhide Max Interior Latex Eggshell, 6-9310 Series. Applied Dry Film Thickness:  1.3 mils min. 
e.	Pittsburgh Paints: Pure Performance Interior Acrylic Latex Eggshell, 9-310XI Series. Applied Dry Film Thickness: 1.4 mils min.
f.	Pittsburgh Paints: Prominence Interior Acrylic Latex Eggshell, 84-3310 Series. Applied Dry Film Thickness: 1.6 mils min.
7.	Interior Gloss Level 3 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior Satin Latex, 6-3511 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: UltraLast Interior Latex Paint and Primer Eggshell, 13-310 Series. Applied Dry Film Thickness: 1.6 mils min.
c.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic Satin DTM Industrial Enamel, 90-1710 Series. Applied Dry Film Thickness: 2.0 mils min.
8.	Interior Gloss Level 3 Acrylic Enamel Finish Zero VOC:
a.	Pittsburgh Paints: Speedhide zero Interior Latex Satin, 6-3511ZV Series. Applied Dry Film Thickness:   1.4 mils min.
b.	Pittsburgh Paints:  Speedhide Max Interior Latex Satin, 6-9410 Series. Applied Dry Film Thickness:  1.4 mils min. 
c.	Pittsburgh Paints: Prominence Interior Acrylic Latex Satin, 84-3410 Series. Applied Dry Film Thickness: 1.6 mils min.
9.	Interior Gloss Level 3 Water-Based Epoxy Finish:
a.	Pittsburgh Paints: Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series. Applied Dry Film Thickness: 1.5 mils min.
10.	Interior Gloss Level 4 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior Latex Lo-Lustre, 6-3011 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: Hi-Hide Interior Latex Satin, 379-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	Pittsburgh Paints: Breakthrough Interior/Exterior Waterborne Acrylic Satin, V52-410 Series. Applied Dry Film Thickness: 1.4 mils min.
11.	Interior Gloss Level 4 Acrylic Enamel Finish Zero VOC:
a.	Pittsburgh Paints: Speedhide zero Interior Latex Lo Lustre, 6-3011ZV Series. Applied Dry Film Thickness: 1.1 mils min.
b.	Pittsburgh Paints:  Speedhide Max Interior Latex Lo Lustre, 6-9610 Series. Applied Dry Film Thickness:  1.4 mils min.
12.	Interior Gloss Level 5 Acrylic Enamel:
a.	Pittsburgh Paints: Speedhide Interior Latex Semi-Gloss, 6-500 Series. Applied Dry Film Thickness:   1.4 mils min.
b.	Pittsburgh Paints: Hi-Hide Interior Latex Semi-Gloss, 109-10 Series. Applied Dry Film Thickness:   1.4 mils min.
c.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Semi-Gloss, 919-10 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	Pittsburgh Paints: UltraLast Interior Latex Paint and Primer Semi-Gloss, 13-510 Series. Applied Dry Film Thickness: 1.5 mils min.
e.	Pittsburgh Paints: Breakthrough Interior/Exterior Waterborne Acrylic Semi-Gloss, V62-510 Series. Applied Dry Film Thickness: 1.5 mils min.
f.	Pittsburgh  Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Semi-Gloss, 90-1610 Series. Applied Dry Film Thickness:   2.0 mils min.
13.	Interior Gloss Level 5 Acrylic Enamel-Zero VOC:
a.	Pittsburgh Paints: Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	Pittsburgh Paints: Speedhide Interior Zero VOC Semi-Gloss Latex, 6-500ZV Series. Applied Dry Film Thickness: 1.5 mils min.
c.	Pittsburgh Paints: Pure Performance Acrylic Latex Semi-Gloss, 9-510XI Series. Applied Dry Film Thickness: 1.4 mils min.
d.	Pittsburgh Paints: Prominence Interior Acrylic Latex Semi-Gloss, 84-3510 Series. Applied Dry Film Thickness: 1.6 mils min.
14.	Interior Gloss Level 5 Water-Based Epoxy Finish:
a.	Pittsburgh Paints: Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy, 16-1510 Series. Applied Dry Film Thickness: 1.6 mils min.
15.	Interior Gloss Level 6 and 7 Acrylic Enamel Finish:
a.	Pittsburgh Paints: Speedhide Interior/Exterior Acrylic High Gloss, 6-8534 Series. Applied Dry Film Thickness:   1.2 mils min.
b.	Pittsburgh Paints: Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	Pittsburgh Paints: Breakthrough Interior/Exterior Waterborne Acrylic Gloss, V72-610 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Gloss, 90-1510 Series. Applied Dry Film Thickness: 2.0 mils min.
E.	Dry-Fall Finish: Two Finish Coats, Self-Priming or over Primer:
1.	Substrate:
a.	Ferrous Metal Ceiling Deck.
2.	Primer: Spot prime only, as needed.
a.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Primer, 90-1912 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	Pittsburgh Paints: Multiprime 4160 Rust-Inhibitive Interior/Exterior Alkyd Primer, 4160-1000 Series. Applied Dry Film Thickness:   2.0 mils min.
c.	Pittsburgh Paints: Speedhide Alkyd Metal Primer, 6-208N Series. Applied Dry Film Thickness: 2.3 mils min.
3.	Interior Gloss Level 1 Water-Based Finish:
a.	Pittsburgh Paints: Speedhide Super Tech WB Interior Dry-Fog Flat, 6-725XI. Applied Dry Film Thickness: 2.2 mils min.
4.	Interior Gloss Level 3 Water-Based Finish:
a.	Pittsburgh Paints: Speedhide Super Tech WB Interior Dry-Fog Eggshell, 6-724XI. Applied Dry Film Thickness: 2.0 mils min.
5.	Interior Gloss Level 5 Water-Based Finish:
a.	Pittsburgh Paints: Speedhide Super Tech WB Interior Dry-Fog Semi-Gloss, 6-727XI. Applied Dry Film Thickness: 2.2 mils min.
F.	Dry-Fall Finish - Two Finish Coats, Self-Priming or over Primer:
1.	Substrate:
a.	Zinc-Coated Metal Ceiling Deck.
2.	Primer: Spot prime only, as needed.
a.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Primer, 90-1912 Series. Applied Dry Film Thickness: 2.0 mils min.
3.	Interior Gloss Level 1 Water-Based Finish:
a.	Pittsburgh Paints: Speedhide Super Tech WB Interior Dry-Fog Flat, 6-725XI. Applied Dry Film Thickness: 2.2 mils min.
4.	Interior Gloss Level 3 Water-Based Finish:
a.	Pittsburgh Paints: Speedhide Super Tech WB Interior Dry-Fog Eggshell, 6-724XI. Applied Dry Film Thickness: 2.0 mils min.
5.	Interior Gloss Level 5 Water-Based Finish:
a.	Pittsburgh Paints: Speedhide Super Tech WB Interior Dry-Fog Semi-Gloss, 6-727XI. Applied Dry Film Thickness: 2.2 mils min.
2.7	EXTERIOR HIGH PERFORMANCE COATING SYSTEMS
A.	Urethane or Siloxane Finish over Epoxy Primer:
1.	Substrates:
a.	Concrete and Masonry, other than concrete masonry units.
b.	Ferrous Metal.
c.	Nonferrous Metal.
2.	Primer:
a.	PPG Paints: Amerlock Sealer Penetrating Epoxy Primer/Sealer, AK-0A Series. Applied Dry Film Thickness: 1.0 mils min.
b.	PPG Paints: Amerlock 2 VOC Fast Dry, High Solids Epoxy Coating, Semi-Gloss, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
c.	PPG Paints: Amerlock 600 High Build Epoxy Coating, Semi-Gloss, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
d.	PPG Paints: Amerlock 2/400 High Solids Epoxy Coating, Semi-Gloss, AK2-T3 Series. Applied Dry Film Thickness: 4.0 mils min.
3.	Intermediate Coat:
a.	PPG Paints: Amerlock 2 VOC Fast Dry, High Solids Epoxy Semi-Gloss, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints: Amerlock 600 High Build Epoxy Semi-Gloss, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
c.	PPG Paints: Amerlock 2/400 High Solids Epoxy Semi-Gloss, AK2-T3 Series. Applied Dry Film Thickness: 4.0 mils min.
4.	Topcoat: Gloss Level 3 and 4:
a.	Pittsburgh Paints: Pitthane Ultra LS Urethane Enamel Low Sheen, 95-8901/95-899 Series. Applied Dry Film Thickness:   2.0 mils min.
b.	PPG Paints: PSX 805 Polysiloxane Satin, PX8053 Series. Applied Dry Film Thickness:   3.0 mils min.
5.	Topcoat: Gloss Level 6 and 7:
a.	Pittsburgh Paints: Durethane DTM Urethane Mastic Gloss, 95-3300/95-339 Series. Applied Dry Film Thickness:   3.0 mils min.
b.	Pittsburgh Paints: Pitthane Ultra Urethane Enamel Gloss, 95-812/95-819 Series. Applied Dry Film Thickness:  2.0 mils min. 
c.	PPG Paints:  Amershield VOC Low VOC Polyester Acrylic Polyurethane Gloss, AMV-3 Series. Applied Dry Film Thickness:  3.0 mils min. 
d.	PPG Paints:  PSX 700 Polysiloxane Gloss, PX7003 Series. Applied Dry Film Thickness:  3.0 mils min. 
B.	Urethane or Siloxane Finish over Zinc-Rich Epoxy Primer: 
1.	Substrate: 
a.	Ferrous Metal. 
2.	Primer: 
a.	PPG Paints: Amercoat 68HS Zinc Rich Epoxy Primer, Flat, AT68HS Series. Applied Dry Film Thickness: 2.0 mils min. 
3.	Intermediate Coat: 
a.	PPG Paints: Amerlock 2 VOC Fast Dry, High Solids Epoxy Coating, Semi-Gloss, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min. 
b.	PPG Paints: Amerlock 600 High Build Semi-Gloss Epoxy Coating, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min. 
c.	PPG Paints: Amerlock 2/400 High Solids Epoxy Coating, Semi-Gloss, AK2-T3 Series. Applied Dry Film Thickness: 4.0 mils min. 
4.	Topcoat: Gloss Level 3 and 4: 
a.	Pittsburgh Paints: Pitthane Ultra LS Low Sheen Urethane Enamel, 95-8901/95-899 Series. Applied Dry Film Thickness: 2.0 mils min. 
b.	PPG Paints: PSX 805 Polysiloxane, Satin, PX8053 Series. Applied Dry Film Thickness: 3.0 mils min. 
5.	Topcoat: Gloss Level 6 and 7: 
a.	Pittsburgh Paints: Durethane DTM Urethane Mastic, 95-3300/95-339 Series. Applied Dry Film Thickness: 3.0 mils min. 
b.	Pittsburgh Paints: Pitthane Ultra Gloss Urethane Enamel, 95-812/95-819 Series. Applied Dry Film Thickness: 2.0 mils min.
c.	PPG Paints: Amershield VOC Low VOC Gloss Polyester Acrylic Polyurethane, AMV-3 Series. Applied Dry Film Thickness: 3.0 mils min.
d.	PPG Paints: PSX 700 Polysiloxane, Gloss, PX7003 Series. Applied Dry Film Thickness: 3.0 mils min.
C.	Urethane or Siloxane Finish over Epoxy Block Filler:
1.	Substrate:
a.	Concrete masonry units:
2.	Block Filler:
a.	PPG Paints: Amerlock 400BF Epoxy Block Filler, AK400B-30/AK400B-B. Applied Dry Film Thickness: 4.0 mils min.
3.	Intermediate Coat:
a.	PPG Paints: Amerlock 2 VOC Fast Dry, High Solids Epoxy Coating, Semi-Gloss, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints: Amerlock 600 High Build Semi-Gloss Epoxy Coating, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
c.	PPG Paints: Amerlock 2/400 High Solids Epoxy Coating, Semi-Gloss, AK2-T3 Series. Applied Dry Film Thickness: 4.0 mils min.
d.	Pittsburgh Paints: Pitthane Ultra LS Urethane Enamel Low-Sheen, 95-8901/95-819 Series. Applied Dry Film Thickness: 2.0 mils min. 
4.	Topcoat: Gloss Level 3 and 4:
a.	Pittsburgh Paints: Pitthane Ultra LS Low Sheen Urethane Enamel, 95-8901/95-899 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	PPG Paints: PSX 805 Polysiloxane, Satin, PX8053 Series. Applied Dry Film Thickness: 3.0 mils min.
5.	Topcoat: Gloss Level 6 and 7:
a.	Pittsburgh Paints: Durethane DTM Urethane Mastic, 95-3300/95-339 Series. Applied Dry Film Thickness: 3.0 mils min.
b.	Pittsburgh Paints: Pitthane Ultra Gloss Urethane Enamel, 95-812/95-819 Series. Applied Dry Film Thickness: 2.0 mils min.
c.	PPG Paints: Amershield VOC Low VOC Gloss Polyester Acrylic Polyurethane, AMV-3 Series. Applied Dry Film Thickness: 3.0 mils min.
d.	PPG Paints: PSX 700 Polysiloxane, Gloss, PX7003 Series. Applied Dry Film Thickness: 3.0 mils min.
D.	Acrylic Finish over Epoxy Primer:
1.	Substrate:
a.	Exterior wood surfaces:
2.	Primer:
a.	Pittsburgh Paints: Seal Grip Gripper Interior/Exterior Universal Acrylic Primer, 17-921XI Series. Applied Dry Film Thickness: 1.6 mils min.
b.	Pittsburgh Paints: Seal Grip Interior/Exterior Alkyd Primer, 17-941NF. Applied Dry Film Thickness: 2.2 mils min.
3.	Intermediate Coat:
a.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Satin, 90-1710 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Semi-Gloss, 90-1610 Series. Applied Dry Film Thickness:  2.0 mils min.
c.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Gloss, 90-1510 Series. Applied Dry Film Thickness:   2.0 mils min.
4.	Topcoat Gloss Level 3:
a.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Satin, 90-1710 Series. Applied Dry Film Thickness:   2.0 mils min.
5.	Topcoat Gloss Level 5:
a.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Semi-Gloss, 90-1610 Series. Applied Dry Film Thickness:   2.0 mils min.
6.	Topcoat Gloss Level 6 and 7:
a.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Gloss, 90-1510 Series. Applied Dry Film Thickness: 2.0 mils min.
E.	Fluoropolymer System: One finish coat applied over an epoxy primer.
1.	Substrate:
a.	Ferrous Metal.
b.	Nonferrous Metal.
2.	Primer:
a.	Pittsburgh Paints: Coraflon ADS Epoxy Primer, ADS 573/ADS574. Applied Dry Film Thickness: 3.0 mils min.
3.	Finish:
a.	Pittsburgh Paints: Coraflon ADS Fluoropolymer. Apply per instructions on the technical data bulletin. Metallic finishes may require an additional clear coat of Coraflon ADS.
2.8	INTERIOR HIGH PERFORMANCE COATING SYSTEMS
A.	Epoxy, Urethane or Siloxane Finish over Epoxy Primer:
1.	Substrate:
a.	Concrete and Masonry other than concrete masonry units:
b.	Ferrous metal.
c.	Nonferrous metal.
2.	Primer:
a.	Pittsburgh Paints: Aquapon WB EP Two-Component Waterborne Epoxy Primer, 98E-46/98E-99 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	PPG Paints: Amerlock Sealer Penetrating Epoxy Primer/Sealer, AK-0A Series. Applied Dry Film Thickness: 1.0 mils min.
c.	PPG Paints: Amerlock 2 VOC Fast Dry High Solids Epoxy Semi-Gloss, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
d.	PPG Paints: Amerlock 600 High Build Epoxy Semi-Gloss, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
e.	PPG Paints: Amerlock 2/400 High Solids Epoxy Semi-Gloss, AK2-T3 Series. Applied Dry Film Thickness: 4.0 mils min.
3.	Intermediate Coat: For use with Acrylic, Urethane or Siloxane Topcoats.
a.	Pittsburgh Paints: Aquapon WB EP Two-Component Waterborne Epoxy Semi-Gloss, 98E-1/98E-100 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	PPG Paints: Amerlock 2 VOC Fast Dry High Solids Epoxy Semi-Gloss, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
c.	PPG Paints: Amerlock 600 High Build Epoxy Semi-Gloss, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
d.	PPG Paints: Amerlock 2/400 High Solids Epoxy Semi-Gloss, AK2-T3 Series. Applied Dry Film Thickness: 4.0 mils min.
e.	PPG Paints: Aquapon WB EP Two-Component Waterborne Epoxy Gloss, 98E-1/98E-98 Series. Applied Dry Film Thickness: 2.0 mils min.
4.	Topcoat: Gloss Level 3 and 4:
a.	Pittsburgh Paints: Pitthane Ultra LS Urethane Enamel Low Sheen, 95-8901/95-899 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	PPG Paints: PSX 805 Polysiloxane Satin, PX8053 Series. Applied Dry Film Thickness: 3.0 mils min.
5.	Topcoat Gloss Level 5:
a.	Pittsburgh Paints: Aquapon WB EP Two-Component Waterborne Epoxy Semi-Gloss, 98E-1/98E-100 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	PPG Paints: Amerlock 2 VOC Fast Dry High Solids Epoxy Semi-Gloss, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
c.	PPG Paints: Amerlock 600 High Build Epoxy Semi-Gloss, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
d.	PPG Paints: Amerlock 2/400 High Solids Epoxy Semi-Gloss, AK2-T3 Series. Applied Dry Film Thickness: 4.0 mils min.
6.	Topcoat Gloss Level 6 and 7:
a.	Pittsburgh Paints: Aquapon WB EP Two-Component Waterborne Epoxy Gloss, 98E-1/98E-98 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	Pittsburgh Paints: Durethane DTM Urethane Mastic Gloss, 95-3300/95-339 Series. Applied Dry Film Thickness: 3.0 mils min.
c.	Pittsburgh Paints: Pitthane Ultra Urethane Enamel Gloss, 95-812/95-819 Series. Applied Dry Film Thickness: 2.0 mils min.
d.	PPG Paints: Amershield VOC Low VOC Polyester Acrylic Polyurethane Gloss, AMV-3 Series. Applied Dry Film Thickness: 3.0 mils min.
e.	PPG Paints: PSX 700 Polysiloxane Gloss, PX7003 Series. Applied Dry Film Thickness: 3.0 mils min.
B.	Epoxy, Urethane or Siloxane Finish over Epoxy Block Filler:
1.	Substrate:
a.	Concrete masonry units:
2.	Block Filler:
a.	PPG Paints: Amerlock 400BF Epoxy Block Filler, AK400B-30/AK400B-B. Applied Dry Film Thickness: 4.0 mils min.
3.	Intermediate Coat: For use with Acrylic, Urethane or Siloxane Topcoats.
a.	Pittsburgh Paints: Aquapon WB EP Two-Component Waterborne Epoxy Semi-Gloss, 98E-1/98E-100 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	PPG Paints: Amerlock 2 VOC Fast Dry High Solids Epoxy Semi-Gloss, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
c.	PPG Paints: Amerlock 600 High Build Epoxy Semi-Gloss, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
d.	PPG Paints: Amerlock 2/400 High Solids Epoxy Semi-Gloss, AK2-T3 Series. Applied Dry Film Thickness: 4.0 mils min.
e.	Pittsburgh Paints: Aquapon WB EP Two-Component Waterborne Epoxy Gloss, 98E-1/98E-98 Series. Applied Dry Film Thickness: 2.0 mils min.
4.	Topcoat: Gloss Level 3 and 4:
a.	Pittsburgh Paints: Pitthane Ultra LS Urethane Enamel Low Sheen, 95-8901/95-899 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	PPG Paints: PSX 805 Polysiloxane Satin, PX8053 Series. Applied Dry Film Thickness: 3.0 mils min.
5.	Topcoat Gloss Level 5:
a.	Pittsburgh Paints: Aquapon WB EP Two-Component Waterborne Epoxy Semi-Gloss, 98E-1/98E-100 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	PPG Paints: Amerlock 2 VOC Fast Dry High Solids Epoxy Semi-Gloss, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
c.	PPG Paints: Amerlock 600 High Build Epoxy Semi-Gloss, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
d.	PPG Paints: Amerlock 2/400 High Solids Epoxy Semi-Gloss, AK2-T3 Series. Applied Dry Film Thickness: 4.0 mils min.
6.	Topcoat Gloss Level 6 and 7:
a.	Pittsburgh Paints: Aquapon WB EP Two-Component Waterborne Epoxy Gloss, 98E-1/98E-98 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	Pittsburgh Paints: Durethane DTM Urethane Mastic Gloss, 95-3300/95-339 Series. Applied Dry Film Thickness: 3.0 mils min.
c.	Pittsburgh Paints: Pitthane Ultra Urethane Enamel Gloss , 95-812/95-819 Series. Applied Dry Film Thickness: 2.0 mils min.
d.	PPG Paints: Amershield VOC Low VOC Polyester Acrylic Polyurethane Gloss , AMV-3 Series. Applied Dry Film Thickness: 3.0 mils min.
e.	PPG Paints: PSX 700 Polysiloxane Gloss, PX7003 Series. Applied Dry Film Thickness: 3.0 mils min.
C.	Acrylic Finish over Primer:
1.	Substrates:
a.	Wood:
b.	Interior wood surfaces:
2.	Primer:
a.	Pittsburgh Paints: Seal Grip Gripper Interior/Exterior Universal Acrylic Primer, 17-921XI Series. Applied Dry Film Thickness: 1.6 mils min.
b.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Primer, 90-1912 Series. Applied Dry Film Thickness: 2.0 mils min.
3.	Intermediate Coat:
a.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Satin, 90-1710 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Semi-Gloss, 90-1610 Series. Applied Dry Film Thickness: 2.0 mils min.
c.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Gloss, 90-1510 Series. Applied Dry Film Thickness: 2.0 mils min.
4.	Topcoat Gloss Level 3:
a.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Satin, 90-1710 Series. Applied Dry Film Thickness: 2.0 mils min.
5.	Topcoat Gloss Level 5:
a.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Semi-Gloss, 90-1610 Series. Applied Dry Film Thickness: 2.0 mils min.
6.	Topcoat Gloss Level 6 and 7:
a.	Pittsburgh Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Industrial Enamel Gloss, 90-1510 Series. Applied Dry Film Thickness: 2.0 mils min.
D.	Fluoropolymer System: One finish coat applied over an epoxy primer.
1.	Substrate:
a.	Ferrous metal.
b.	Nonferrous metal.
2.	Primer:
a.	Pittsburgh Paints: Coraflon ADS Epoxy Primer, ADS 573/ADS574. Applied Dry Film Thickness: 3.0 mils min.
3.	Finish: 
a.	Pittsburgh Paints: Coraflon ADS Fluoropolymer. Apply per instructions on the technical data bulletin. Metallic finishes may require an additional clear coat of Coraflon ADS.
PART 3    EXECUTION
3.1	EXAMINATION
A.	Do not begin installation until substrates have been properly prepared.
B.	If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.
C.	Coordination of Work: Review other Sections in which primers are provided to ensure compatibility of the total system for various substrates. On request, furnish information on characteristics of finish materials to ensure use of compatible primers.
1.	Notify Architect about anticipated problems when using the materials specified over substrates primed by others.
2.	If a potential incompatibility of primers applied by others exists, obtain the following from the primer Applicator before proceeding:
a.	Confirmation of primer's suitability for expected service conditions.
b.	Confirmation of primer's ability to be top coated with materials specified.
3.2	PREPARATION
A.	General: Remove hardware and hardware accessories, plates, machined surfaces, lighting fixtures, and similar items already installed that are not to be painted. If removal is impractical or impossible because of size or weight of the item, provide surface-applied protection before surface preparation and painting.
1.	After completing painting operations in each space or area, reinstall items removed using workers skilled in the trades involved.
B.	Cleaning: Before applying paint or other surface treatments, clean substrates of substances that could impair bond of the various coatings. Remove oil and grease before cleaning.
1.	Schedule cleaning and painting so dust and other contaminants from the cleaning process will not fall on wet, newly painted surfaces.
C.	Surface Preparation: Clean and prepare surfaces to be painted according to manufacturer's written instructions for each particular substrate condition and as specified.
1.	Provide barrier coats over incompatible primers or remove and reprime.
2.	Provide barrier coats over incompatible primers or remove primers and reprime substrate.
3.	Cementitious Substrates: Prepare concrete, brick, concrete masonry block, and cement plaster surfaces to be coated. Remove efflorescence, chalk, dust, dirt, grease, oils, and release agents. Roughen as required to remove glaze. If hardeners or sealers have been used to improve curing, use mechanical methods to prepare surfaces.
a.	Use abrasive blast-cleaning methods if recommended by coating manufacturer.
b.	Determine alkalinity and moisture content of surfaces by performing appropriate tests. If surfaces are sufficiently alkaline to cause the finish paint to blister and burn, correct this condition before application. Do not coat surfaces if moisture content exceeds that permitted in manufacturer's written instructions.
4.	Wood Substrates: Clean surfaces of dirt, oil, and other foreign substances with scrapers, mineral spirits, and sandpaper, as required. Smoothly sand surfaces exposed to view and dust off.
a.	Scrape and clean small, dry, seasoned knots, and apply a thin coat of white shellac or other recommended knot sealer, before applying primer.
b.	Immediately on delivery, prime edges, ends, faces, undersides, and backsides of wood to be coated.
c.	After priming, fill holes and imperfections in the finish surfaces with putty or plastic wood filler. Sand smooth when dried.
5.	Ferrous Metal Substrates: Clean ungalvanized ferrous-metal surfaces that have not been shop coated: remove oil, grease, dirt, loose mill scale, and other foreign substances. Use solvent or mechanical cleaning methods that comply with SSPC recommendations.
a.	Blast-clean steel surfaces as recommended by coating manufacturer and according to SSPC-SP 10.
b.	Treat bare and sandblasted or pickled clean metal with a metal treatment wash coat before priming.
c.	Touch up bare areas and shop-applied prime coats that have been damaged. Wire brush, solvent clean, and touch up with same primer as the shop coat.
6.	Nonferrous-Metal Substrates: Clean nonferrous and galvanized surfaces according to manufacturer's written instructions for the type of service, metal substrate, and application required.
a.	Remove pretreatment from galvanized sheet metal fabricated from coil stock by mechanical methods.
D.	Material Preparation: Carefully mix and prepare coating materials according to manufacturer's written instructions.
1.	Maintain containers used in mixing and applying coatings in a clean condition, free of foreign materials and residue.
2.	Stir materials before applying to produce a mixture of uniform density. Stir as required during application. Do not stir surface film into the material. Remove film and, if necessary, strain coating material before using.
3.	Use only the type of thinners approved by manufacturer and only within recommended limits.
4.	Tinting: Tint each undercoat a lighter shade to simplify identification of each coat when multiple coats of same material are applied. Tint undercoats to match the color of the finish coat but provide sufficient differences in shade of undercoats to distinguish each separate coat.
3.3	APPLICATION
A.	General: Apply paint according to manufacturer's written instructions. Use applicators and techniques best suited for substrate and type of material being applied.
B.	General: Apply high-performance coatings according to manufacturer's written instructions.
1.	Use applicators and techniques best suited for the material being applied.
2.	Do not apply high-performance coatings over dirt, rust, scale, grease, moisture, scuffed surfaces, or conditions detrimental to forming a durable coating film.
3.	Coating surface treatments, and finishes are indicated in the coating system descriptions.
4.	Provide finish coats compatible with primers used.
5.	The term "exposed surfaces" includes areas visible when permanent or built-in fixtures, convector covers, grilles, covers for finned-tube radiation, and similar components are in place. Extend coatings in these areas, as required, to maintain system integrity and provide desired protection.
C.	Application Procedures: Apply coatings by brush, roller, spray, or other applicators according to manufacturer's written instructions.
1.	The number of coats and film thickness required is the same regardless of application method.
2.	Completed Work: Match approved Samples for color, texture, and coverage. Remove, refinish, or recoat work that does not comply with specified requirements.
3.4	FIELD QUALITY CONTROL
A.	Owner reserves the right to invoke the following test procedure at any time and as often as Owner deems necessary during the period when paint is being applied:
1.	Owner will engage a qualified independent testing agency to sample paint material being used. Samples of material delivered to Project will be taken, identified, sealed, and certified in the presence of Contractor.
2.	Owner may direct Contractor to stop painting if test results show material being used does not comply with specified requirements. Contractor shall remove noncomplying paint from Project site, pay for testing, and repaint surfaces previously coated with the noncomplying paint. If necessary, Contractor may be required to remove noncomplying paint from previously painted surfaces if, on repainting with specified paint, the two coatings are incompatible.
3.5	CLEANING
A.	After completing painting, clean glass and paint spattered surfaces. Remove spattered paint by washing and scraping without scratching or damaging adjacent finished surfaces.
3.6	PROTECTION
A.	Protect work of other trades, whether being painted or not, against damage from painting. Correct damage by cleaning, repairing, or replacing, and repainting, as approved by Architect.
B.	Provide "Wet Paint" signs to protect newly painted finishes. After completing painting operations, remove temporary protective wrappings provided by others to protect their work.
C.	After work of other trades is complete, touch up and restore damaged or defaced painted surfaces.

END OF SECTION