SECTION 06 60 00

CELLULAR PVC FABRICATIONS

Display hidden notes to specifier. (Don't know how? Click Here)

Copyright 2019 - 2026 ARCAT, Inc. - All rights reserved

** NOTE TO SPECIFIER ** Wolf Home Products; PVC Fabrications.
This section is based on the products of Wolf Home Products, which is located at:
20 W. Market St.
York, PA 17401
Toll Free Tel: 800-388-9653
Email: request info (JDFoura@wolfhomeproducts.com)
Web: https://www.wolfhomeproducts.com  
 [ Click Here ] for additional information.
Wolf Home Products was founded in 1843 as a single store selling dry goods and lumber on the banks of Pennsylvania's Susquehanna River. During the first half of the 1900s, the company expanded into a mid-Atlantic wholesale and retail lumber operation with 30 locations.
By the early 2000s, Wolf transitioned its successful lumber operation into a sourcing organization, offering kitchen, bath, and building products exclusively to independent building materials dealers.
Wolf Home Products continued its growth with the introduction of Wolf-branded product lines in 2010. Today, the company is committed to product and geographic expansion, servicing 3,500+ dealers nationally and in Canada.

- GENERAL

  - SECTION INCLUDES

    - Cellular PVC Fabrications of the following types:

      - Decking. (Perspective Decking, Serenity Decking)

      - Porch flooring. (Serenity Porch)

      - Railings. (Distinction Railings, Wolf Railings)

      - Siding. (Portrait Siding)

      - Trim.

      - Outdoor lighting.

  - RELATED SECTIONS

** NOTE TO SPECIFIER ** Delete any sections below not relevant to this project; add others as required.

    - Section 06 10 00 - Rough Carpentry.

    - Section 06 20 00 - Finish Carpentry.

    - Section 07 27 00 - Air Barriers.

    - Section 07 90 00 - Joint Protection.

    - Section 09 90 00 - Painting and Coating.

  - REFERENCES

** NOTE TO SPECIFIER ** Delete references from the list below that are not actually required by the text of the edited section.

    - ASTM International (ASTM):

      - ASTM B429 - Standard Specification for Aluminum Alloy Extruded Structural Pipe and Tube.

      - ASTM C177 - Standard Test Method for Steady-State Heat Flux Measurements and Thermal Transmission Properties by Means of the Guarded-Hot-Plate Apparatus.

      - ASTM C1363 - Standard Test Method for Thermal Performance of Building Materials and Envelope Assemblies by Means of a Hot Box Apparatus.

      - ASTM D256 - Standard Test Methods for Determining the Izod Pendulum Impact Resistance of Plastics.

      - ASTM D570 - Standard Test Method for Water Absorption of Plastics.

      - ASTM D635 - Standard Test Method for Rate of Burning and/or Extent and Time of Burning of Plastics in a Horizontal Position; 2018.

      - ASTM D648 - Standard Test Method for Deflection Temperature of Plastics Under Flexural Load in the Edgewise Position.

      - ASTM D696 - Test Method for Coefficient of Linear Expansion of Plastics.

      - ASTM D790 - Standard Test Methods for Flexural Properties of Unreinforced and Reinforced Plastics and Electrical Insulating Materials.

      - ASTM D792 - Standard Test Methods for Density and Specific Gravity (Relative Density) of Plastics by Displacement.

      - ASTM D1435 - Practice for Outdoor Weathering of Plastics.

      - ASTM D1761 - Standard Test Methods for Mechanical Fasteners in Wood.

      - ASTM D1784 - Standard Specification for Rigid Poly(Vinyl Chloride) (PVC) Compounds and Chlorinated Poly(Vinyl Chloride) (CPVC) Compounds.

      - ASTM D2244 - Practice for Calculation of Color Tolerances and Color Differences from Instrumentally Measured Color Coordinates.

      - ASTM D3345 - Standard Test Method for Laboratory Evaluation of Solid Wood for Resistance to Termites.

      - ASTM D3679 - Standard Specification for Rigid Poly(Vinyl Chloride) (PVC) Siding; 2017.

      - ASTM D4226 - Test Methods for Impact Resistance of Rigid Poly Vinyl Chloride (PVC) Building Products.

      - ASTM D5206 - Standard Test Method for Windload Resistance of Rigid Plastic Siding; 2013.

      - ASTM D5420 - Standard Test Method for Impact Resistance of Flat, Rigid Plastic Specimen by Means of a Striker Impacted by a Falling Weight (Gardner Impact).

      - ASTM D6662 - Standard Specification for Polyolefin-Based Plastic Lumber Decking Boards.

      - ASTM E84 - Standard Test Method for Surface Burning Characteristics of Building Materials.

      - ASTM E330 - Standard Test Method for Structural Performance of Exterior Windows, Doors, Skylights and Curtain Walls by Uniform Static Air Pressure Difference.

      - ASTM G147 - Practice for Conditioning and handling of Nonmetallic Materials for Natural and Artificial Weathering Tests.

    - American Association of Textile Chemists and Colorists (AATCC):

      - AATCC 127 - Water Resistance: Hydrostatic Pressure Test.

    - American Wood Protection Association (AWPA):

      - AWPA E12 - Standard Method of Determining Corrosion of Metal in Contact with Treated Wood.

    - International Code Council (ICC):

      - ICC AC227 - Rigid Cellular PVC Non-Load Bearing Exterior Trim.

  - SUBMITTALS

    - Submit under provisions of Section 01 30 00 - Administrative Requirements.

    - Product Data:

      - Manufacturer's data sheets on each product to be used.

      - Preparation instructions and recommendations.

      - Storage and handling requirements and recommendations.

      - Typical installation methods.

** NOTE TO SPECIFIER ** Delete if not applicable to product type.

    - Verification Samples: Two representative units of each type, size, pattern and color.

    - Shop Drawings: Include details of materials, construction and finish. Include relationship with adjacent construction.

  - QUALITY ASSURANCE

    - Manufacturer Qualifications: Company specializing in manufacturing products specified in this section with a minimum five years documented experience.

    - Installer Qualifications: Company specializing in performing Work of this section with minimum two years documented experience with projects of similar scope and complexity.

    - Source Limitations: Provide each type of product from a single manufacturing source to ensure uniformity.

** NOTE TO SPECIFIER ** Include mock-up if the project size or quality warrant the expense. The following is one example of how a mock-up on might be specified. When deciding on the extent of the mock-up, consider all the major different types of work on the project.

    - Mock-Up: Construct a mock-up with actual materials in sufficient time for Architect's review and to not delay construction progress. Locate mock-up as acceptable to Architect and provide temporary foundations and support.

      - Intent of mock-up is to demonstrate quality of workmanship and visual appearance.

      - If mock-up is not acceptable, rebuild mock-up until satisfactory results are achieved.

      - Retain mock-up during construction as a standard for comparison with completed work.

      - Do not alter or remove mock-up until work is completed or removal is authorized.

  - PRE-INSTALLATION CONFERENCE

    - Convene a conference approximately two weeks before scheduled commencement of the Work. Attendees shall include Architect, Contractor and trades involved. Agenda shall include schedule, responsibilities, critical path items and approvals.

  - DELIVERY, STORAGE, AND HANDLING

    - Store and handle in strict compliance with manufacturer's written instructions and recommendations.

    - Protect from damage due to weather, excessive temperature, and construction operations.

  - PROJECT CONDITIONS

    - Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's recommended limits.

  - WARRANTY

    - Manufacturer's Warranty: Provide manufacturer's standard limited warranty.

** NOTE TO SPECIFIER ** Delete warranty duration options not required.

      - Warranty Duration, Perspective Decking: Twenty-five (25) years.

      - Warranty Duration, Serenity Decking:

        - Residential: Lifetime.

        - Non-residential: Twenty (20) years.

      - Warranty Duration, Serenity Porch:

        - Residential: Lifetime.

        - Non-residential: Twenty (20) years.

      - Warranty Duration, Distinction Railings: Lifetime.

      - Warranty Duration, Wolf Railings:

        - Residential: Lifetime.

        - Non-residential: Thirty (30) years.

      - Warranty Duration, Siding:

        - Residential: Lifetime.

        - Non-residential: Twenty (20) years.

      - Warranty Duration, Trim:

        - Residential: Lifetime.

        - Non-residential: Twenty-five (25) years.

      - Warranty Duration, Outdoor Lighting: Five (5) years.

- PRODUCTS

  - MANUFACTURERS

    - Acceptable Supplier: Wolf Home Products, which is located at: 20 West Market Street; York, PA 17401; ASD Toll Free: 800-388-9653; Email: JDFoura@wolfhomeproducts.com; Web: www.wolfhomeproducts.com.

** NOTE TO SPECIFIER ** Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

    - Substitutions: Not permitted.

    - Requests for substitutions will be considered in accordance with provisions of Section 01 60 00 - Product Requirements.

** NOTE TO SPECIFIER ** Delete Article if not required.

  - CELLULAR PVC DECKING

** NOTE TO SPECIFIER ** Delete basis of design options not required.

    - Basis of Design: Wolf Perspective Decking; as manufactured by Wolf Home Products.

      - Performance Requirements:

        - Meets or exceeds ICC standards.

        - Resists rot, delamination, splitting, and cracking.

        - Moisture, mold, and mildew resistant.

        - Made from up to 94 percent recycled content.

        - Suitable for commercial or residential applications.

      - Material: Solid cellular PVC.

      - Dimensions: 7/8 x 5-1/2 inches (22 x 140 mm).

      - Rimboards: 3/4 x 11-1/4 inches (19 x 286 mm) x 12 feet (3658 mm) long.

      - Profile: Grooved, to accept hidden fasteners.

      - Texture: Wood grain.

** NOTE TO SPECIFIER ** Optional. Delete if not required.

      - Seal: Dexerdry, acts like gutters to create dry space below the deck.

** NOTE TO SPECIFIER ** Delete board length options not required.

      - Board Length: 12 feet (3658 mm).

      - Board Length: 16 feet (4877 mm).

      - Board Length: 20 feet (6096 mm).

** NOTE TO SPECIFIER ** Delete color options not required.

      - Color: Acacia.

      - Color: Cedar Ridge.

      - Color: Potomac Grey.

      - Color: Redwood.

      - Color: Dune.

      - Color: To be selected by Architect.

** NOTE TO SPECIFIER ** Delete fastener system options not required.

      - Fastener System: Universal hidden fastener.

      - Fastener System: Phantom GT hidden fastener.

    - Basis of Design: Wolf Serenity Decking; as manufactured by Wolf Home Products.

      - Performance Requirements:

        - Meets or exceeds ICC standards.

        - Resists rot, delamination, splitting, and cracking.

        - Moisture, mold, and mildew resistant.

      - Material: Solid cellular PVC.

      - Dimensions: 1 x 5-1/2 inches (25 x 140 mm).

      - Rimboards: 1/2 x 11-3/4 inches (12 x 298 mm) x 12 feet (3658 mm) long.

      - Texture: Wood grain, reversible.

** NOTE TO SPECIFIER ** Delete board length options not required.

      - Board Length: 12 feet (3658 mm).

      - Board Length: 16 feet (4877 mm).

      - Board Length: 20 feet (6096 mm).

** NOTE TO SPECIFIER ** Delete color options not required.

      - Color: Amber Wood

      - Color: Black Walnut.

      - Color: Golden Cypress.

      - Color: Driftwood Grey.

      - Color: Rosewood.

      - Color: Silver Teak

      - Color: Teakwood.

      - Color: Weathered Ipe.

      - Color: Harbor Grey.

      - Color: Sand Castle.

      - Color: To be selected by Architect.

** NOTE TO SPECIFIER ** Delete fastener system options not required.

      - Fasteners: Hidden.

      - Fasteners: Traditional.

** NOTE TO SPECIFIER ** Delete Article if not required.

  - CELLULAR PVC PORCH FLOORING

    - Basis of Design: Wolf Serenity Porch; as manufactured by Wolf Home Products.

      - Performance Requirements:

        - Meets or exceeds ICC standards.

        - Resists rot, delamination, splitting, and cracking.

        - Mold and mildew resistant.

        - Resistant to staining and fading.

        - Recycled Content: 95 percent.

        - Surface Burning Characteristics per ASTM E84: Flame spread index maximum 200, smoke developed maximum 285.

        - Load Capacity: 100 psf (4.79 kPa) with deflection limited to 1/360 of span.

      - Material: Capped cellular PVC.

** NOTE TO SPECIFIER ** Pewter color size is 3/4 x 3-1/8 (19 x 79 mm), all other colors are 1 x 3-1/8 inch (25 x 79 mm). Delete dimension option not required.

      - Dimensions: 1 x 3-1/8 inches (25 x 79 mm).

      - Dimensions: 3/4 x 3-1/8 inches (19 x 79 mm).

      - Texture: Wood grain, reversible.

      - Profile: Tongue and groove.

** NOTE TO SPECIFIER ** Delete board length options not required.

      - Board Length: 10 feet (3048 mm).

      - Board Length: 12 feet (3658 mm).

      - Board Length: 16 feet (4877 mm).

** NOTE TO SPECIFIER ** Delete color options not required.

      - Color: Amber Wood

      - Color: Golden Cypress.

      - Color: Silver Teak

      - Color: Weathered Ipe.

      - Color: Harbor Grey.

      - Color: Sand Castle.

      - Color: Pewter.

      - Color: To be selected by Architect.

** NOTE TO SPECIFIER ** Use Type 316 for coastal applications. Delete fastener options not required.

      - Fasteners: Stainless steel, Type 316.

      - Fasteners: Stainless steel, Type 305.

      - Minimum Screw Size: No. 7 screw.

      - Minimum Fastener Length: 2 inches (51 mm).

      - Adhesive: Manufacturer's recommended waterproof, air cure type.

** NOTE TO SPECIFIER ** Delete Article if not required.

  - CELLULAR PVC RAILINGS

** NOTE TO SPECIFIER ** Delete basis of design options not required.

    - Basis of Design: Wolf Distinction Railing; as manufactured by Wolf Home Products.

      - Performance Requirements:

        - Meets or exceeds ICC standards.

        - Suitable for commercial or residential applications.

      - Material: Solid cellular PVC.

** NOTE TO SPECIFIER ** Delete length options not required.

      - Rail Section Length: 6 feet (1829 mm).

      - Rail Section Length: 8 feet (2438 mm).

** NOTE TO SPECIFIER ** Delete configuration options not required.

      - Configuration: Flat.

      - Configuration: Stair.

      - Configuration: Flat and stair.

      - Components:

** NOTE TO SPECIFIER ** Delete component options not required.

        - Top and bottom rails. Top rail features elegant cures and flat top for a beverage friendly surface.

        - Channel: Structural grade aluminum H-channel.

        - Baluster: Solid core baluster.

        - Post Sleeves: Allow for quick and easy installation.

        - Brackets: Optibracket attaches straight or at 22.5, 45, or 90 degree angles.

        - Hardware.

        - Post caps.

        - Trim rings.

      - Color: White.

    - Basis of Design: Wolf Railing; as manufactured by Wolf Home Products.

      - Performance and Design Requirements:

        - Distributed Loads: Design railing assembly, wall rails, and attachments to resist distributed force of 50 lbs per linear foot (730 N per m) applied to the top of the assembly and in any direction.

        - Concentrated Loads: Design railing assembly, wall rails, and attachments to resist a concentrated force of 200 lbs (89 N) applied at any point on the top of the assembly and in any direction.

        - Allow for expansion and contraction of members and building movement without damage to connections or members.

        - Provide anchors and other components as required to attach to structure; where exposed fasteners are unavoidable provide flush countersunk fasteners.

        - Poly Vinyl Chloride (PVC) per ASTM D1784: lmpact-resistant and ultraviolet (UV) stable extruded product.

        - Surface Burning Characteristics per ASTM E84: Flame spread index of 200, maximum.

        - Aluminum Reinforcement for Rails: Aluminum extrusions; alloy and temper 6063-T5 or 6063-T6 complying with ASTM B429.

      - Material: Solid cellular PVC.

** NOTE TO SPECIFIER ** Delete configuration options not required.

      - Configuration: Flat.

      - Configuration: Stair.

      - Configuration: Flat and stair.

** NOTE TO SPECIFIER ** Delete baluster style options not required.

      - Baluster Style: Value Series, Colonial.

      - Baluster Style: Value Series, Square.

      - Baluster Style: Classic Series, Round.

** NOTE TO SPECIFIER ** Delete color options not required.

        - Color: White.

        - Color: Black Bronze.

        - Color: Matte Black.

        - Color: Copper.

        - Color: Rust.

      - Baluster Style: Deluxe Series, Scenic Clear View Glass.

      - Baluster Style: Deluxe Series, Deckorators Classic.

      - Baluster Style: Deluxe Series, Deckorators Baroque.

      - Baluster Style: Deluxe Series, Deckorators Arc.

      - Structural Posts: Colonial structural post.

      - Post Sleeve Size: As required to fit wood posts.

      - Post Trim: One piece post trim.

** NOTE TO SPECIFIER ** Delete post cap options not required.

      - Post Cap: As specified in Outdoor Lighting Article.

      - Post Cap: New England Classic Cap.

      - Post Cap: Federation Cap.

      - Post Cap: External Pyramid Cap.

      - Rail Brackets and Mounting Hardware: Manufacturer's mounting brackets to match railing configuration. Complete with cover plates and fasteners.

      - Exposed Fasteners: No exposed bolts or screws one trim has been installed.

** NOTE TO SPECIFIER ** Delete color options not required.

      - Color: White.

      - Color: Almond.

      - Color: Khaki.

      - Color: Mocha Walnut.

      - Color: Earl Gray.

      - Color: Green Teak.

      - Color: To be selected by Architect.

      - Adhesive: Manufacturer's recommended waterproof, air cure type.

** NOTE TO SPECIFIER ** Delete Article if not required.

  - CELLULAR PVC SIDING

    - Performance Requirements:

      - Comply with ASTM D3679.

      - Coefficient of Linear Expansion per ASTM D696: Exceeds requirements.

      - Weathering per ASTM D1435 and ASTM G147: Passes; Uniform of color; no peeling, chipping, cracking, flaking and pitting.

      - Uniformity of Color per ASTM D2244: Passed.

      - Horizontal Flammability per ASTM D635:

        - Extent of Burn: 0 mm.

        - Average Time of Burn: Less than 1 seconds.

    - Basis of Design: Wolf Portrait Siding; as manufactured by Wolf Home Products.

      - Material: Solid cellular PVC.

** NOTE TO SPECIFIER ** Delete profile option not required.

      - Profile: Silhouette, Single 7 inch (178 mm) exposure, 8-1/4 inch (210 mm) total face dimension.

        - Wind Resistance per ASTM D5206: Capable of withstanding 95 psf (4.55 kPa) negative pressure.

        - Impact Resistance per ASTM D4226: 169 in.lbf (19.1 Nm).

        - Thermal Resistance Value per ASTM C1363: 0.37 hr sq ft F/btu (256.54 cm K per W).

      - Profile: Vignette, Double 4 inch (102 mm) exposure, 9-1/4 inch (235 mm) total face dimension.

        - Wind Resistance per ASTM D5206: Capable of withstanding 185 psf (8.86 kPa) negative pressure.

        - Impact Resistance per ASTM D4226: 71 in.lbf (8 Nm).

        - Thermal Resistance Value per ASTM C1363: 0.36 hr. sq.ft. F/btu (249.6 cm K per W).

** NOTE TO SPECIFIER ** Delete color options not required.

      - Color: Morning Mist.

      - Color: Oyster White.

      - Color: Graphite.

      - Color: Riverstone.

      - Color: Sandstone.

      - Color: Hemlock.

      - Color: Chestnut.

      - Color: Vintage Taupe.

      - Color: To be selected by Architect.

      - Nailing Flange: Single layer with pre-slotted nail holes and smooth finish.

    - Accessory Materials

** NOTE TO SPECIFIER ** Delete accessory options not required.

      - Drainage House Wrap: Non-woven vapor permeable water resistant barrier.

        - Basis of Design: BLOCK-IT House Wrap as manufactured by Kimberly-Clark and supplied by Wolf Home Products.

      - Starter Strips: Wolf Portrait Siding starter strips.

      - Trim and Accessories: Coordinating accessories made of same material as required for complete installation.

** NOTE TO SPECIFIER ** Delete color option not required.

        - Color: Match adjacent siding.

        - Color: _____.

        - Size: 5/4 cellular PVC trim.

        - Types: As indicated on Drawings.

      - Seam Plates: Infinity Seam Plates designed and sized to match siding profile.

        - Adhesive: Approved by siding manufacturer.

      - Fasteners: Stainless steel or hot-dipped galvanized steel, 6 penny nails.

        - Long enough to penetrate through substrate a minimum of 3/4 inch (19 mm).

        - Do not use brads, staples, wire nails, or fine-threaded wood screws.

        - Trim Fasteners: Cortex hidden fastening system for trim.

** NOTE TO SPECIFIER ** Delete Article if not required.

  - CELLULAR PVC TRIM

    - Performance Requirements:

      - Density (ASTM D792): 0.022 lbs per cu inch (0.60 g per cu cm).

      - Water Absorption, 24 hours (ASTM D570): Less than 0.3 percent.

      - Water Resistance (ASTM D570 and AATCC 127): No penetration, passes ICC AC227.

      - Surface Burning (ASTM E84): Flame spread index of 25.

      - Burning Rate (ASTM D635): No burn when flame removed.

      - Gardener Impact Resistance (ASTM D5420): 629 in-lbf (71.1 Nm) for 3/4 inch (19 mm) thick trim.

      - Coefficient of Linear Thermal Expansion (ASTM D 696): .000035 inch/inch/degree F (.000063 mm/mm/C).

      - Strength (ASTM D790):

        - MOR (Flexural Strength): 3,600.0 psi (24,821 kPa).

        - MOR (Flexural Modulus): 144,000.0 psi (992,845 kPa).

      - Weathering (ASTM G155 and ASTM D790):

        - MOR Change: Plus 2.4 percent, Pass ICC AC 227.

        - MOE Change: Plus 0.7 percent.

      - Weathering (ASTM D6662 and ASTM D790):

        - MOR Change: Plus 0.1 percent, Pass ICC AC 227.

        - MOE Change: Plus 0.9 percent.

      - Termite Resistance (ASTM D3345): 9.2, Pass ICC AC 227.

      - Mechanical Fastener, Allowable Load (ASTM D1761): 151 lbf (671.7 N) with 8d nail and 1 inch (25 mm) thick trim.

      - Negative Transverse Wind Load (ASTM E330): 72 psf (3.45 kPa).

      - Heat Deflection Temperature (ASTM D648): 146 degrees F (63 degrees C) at 264 psi (1820 kPa).

      - Corrosion by Preservative Treated Wood (AWAP E12): No weight loss, Pass ICC AC 227.

      - Izod Impact, Notched (ASTM D648): 0.37 ft-lb/in (0.02 N-m/mm).

      - Heat Conductivity (ASTM C177): 0.50 btu-in/hr-ft2-degrees F (0.00072 W/cm C).

    - Basis of Design: Wolf PVC Trim; as manufactured by Wolf Home Products.

      - Material: Solid cellular PVC.

      - Allowable Tolerances:

        - Variation in component length: Minus 0.00 and plus 7/8 inch (22 mm).

        - Variation in component Width: Minus 0.00 and plus 1/16 inch (1.6 mm).

        - Variation in component thickness: Plus or minus 5 percent.

        - Variation in component edge: Plus or minus 2 degrees.

        - Density range: 0.58 - 0.62.

        - Shore-D hardness: 45.

** NOTE TO SPECIFIER ** Delete color options not required.

      - Color: Morning Mist.

      - Color: Oyster White.

      - Color: Graphite.

      - Color: Riverstone.

      - Color: Sandstone.

      - Color: Hemlock.

      - Color: Chestnut.

      - Color: Vintage Taupe.

      - Color: To be selected by Architect.

    - Accessory Materials

** NOTE TO SPECIFIER ** Delete accessory options not required.

      - Fasteners: Stainless steel or hot-dipped galvanized steel, 6 penny nails.

        - Long enough to penetrate through substrate a minimum of 3/4 inch (19 mm).

        - Do not use brads, staples, wire nails, or fine-threaded wood screws.

      - Adhesives: Extreme Adhesives or as recommended by trim manufacturer.

      - Sealants: Fill n Flex or as recommended by trim manufacturer.

      - Paints: See Section 09 90 00 - Painting and Coating:

        - Light Colors with LRV or 55 or higher: Use a 100 percent acrylic latex paint.

        - Dark Colors with LRV or 54 or lower: Use paints specifically formulated for use on vinyl or PVC products. Acrylic or urethane based latex exterior paints are recommended.

** NOTE TO SPECIFIER ** Used for seaming, splicing of insulation sheets, house wraps, wall boards, splicing around window frames, and as a waterproofing tape on outdoor deck's rafter. Delete article if not required.

  - SELF-ADHERING FLASHING TAPE:

    - Product: Nichigo G-Tape No. 3040BK. For installation of exterior wall fenestration products. Maintains performance after exposure to prolonged sunlight and precipitation.

    - Composition:

      - LDPE laminating layer.

      - HDPE cloth layer.

      - LDPE Laminated layer.

      - Acrylic adhesive.

      - Paper liner.

    - Performance Requirements: Meets AAMA 711-13; Type A, without primer, Level 3 exposure up to 176 degreesF, and AC 148.

    - Physical Properties:

      - Thickness per PSTC 13: 9.4 mils (0.24 mm).

      - Peel Adhesion per PSTC 101: 136 oz per inch (15 N per cm).

      - Shear Adhesion per PSTC 107: 39 mils (1.0 mm).

      - Breaking Strength per PSTC 131: 44.5 lbf per inch (78 N per cm).

      - Elongation PSTC 131: 17 percent.

      - Temperature Use Range per MCC Method: Minus 40 to 200 degrees F (4 to 93 degrees C).

    - Characteristics:

      - Waterproof.

      - High dimension stability.

      - Extremely High weather resistance.

      - Firm fixing on rough surfaces.

      - High initial stickiness.

      - No black speck or stain.

      - Tear by hands. No cutting tool is required.

      - Scrapless: Face to face contact of adhesive separates without damaging the adhesive.

      - Light Weight: 50 to 70 percent lighter than conventional window flashing tape.

** NOTE TO SPECIFIER ** Delete Article if not required.

  - OUTDOOR LIGHTING

    - Basis of Design: Wolf Outdoor Lighting; as manufactured by Wolf Home Products.

      - Performance Requirements:

        - Energy efficient and weather resistant.

        - Bluetooth compatible.

        - Durable and UV stable.

        - Rated Life: 50,000 hours.

** NOTE TO SPECIFIER ** Delete transformer option not required.

      - Transformer: Standard.

      - Transformer: Dimmable.

      - Low voltage DC power.

** NOTE TO SPECIFIER ** Delete style options not required.

      - Style: Ornamental downward low-voltage post cap light.

** NOTE TO SPECIFIER ** Delete size options not required.

        - Size: 2 inches (51 mm).

        - Size: 2-1/2 inches (64 mm).

        - Size: 4 inches (102 mm).

        - Size: 4-1/4 inches (108 mm).

** NOTE TO SPECIFIER ** Delete color options not required.

        - Color: White.

        - Color: Black.

        - Color: Textured Black.

      - Style: Ornamental low-voltage post cap light.

** NOTE TO SPECIFIER ** Delete size options not required.

        - Size: 2 inches (51 mm).

        - Size: 2-1/2 inches (64 mm).

        - Size: 4 inches (102 mm).

        - Size: 4-1/4 inches (108 mm).

** NOTE TO SPECIFIER ** Delete color options not required.

        - Color: White.

        - Color: Black.

        - Color: Textured Black.

      - Style: Ornamental low-voltage combo post cap light.

** NOTE TO SPECIFIER ** Delete size options not required.

        - Size: 2 inches (51 mm).

        - Size: 2-1/2 inches (64 mm).

        - Size: 4 inches (102 mm).

        - Size: 4-1/4 inches (108 mm).

** NOTE TO SPECIFIER ** Delete color options not required.

        - Color: White.

        - Color: Black.

        - Color: Textured Black.

      - Style: Dome side light scalloped lens.

** NOTE TO SPECIFIER ** Delete color option not required.

        - Color: White.

        - Color: Black.

      - Style: Dome side light.

** NOTE TO SPECIFIER ** Delete color option not required.

        - Color: White.

        - Color: Black.

      - Style: Side stair light with 2 covers.

** NOTE TO SPECIFIER ** Delete color option not required.

        - Color: White.

        - Color: Black.

      - Style: LED strip light.

** NOTE TO SPECIFIER ** Delete length option not required.

        - Length: 68 inches (1727 mm).

        - Length: 92 inches (2337 mm).

      - Style: Ornamental side light.

** NOTE TO SPECIFIER ** Delete options not required.

        - Color: White.

        - Color: Black.

      - Style: 3 inch (76 mm) under-rail light.

** NOTE TO SPECIFIER ** Delete options not required.

        - Color: White.

        - Color: Black.

      - Style: Flush deck light.

    - Accessories:

** NOTE TO SPECIFIER ** Delete accessory options not required.

      - Power supply, 12 watt.

      - Power supply, 50 watt.

      - Dimmer for 12 watt.

      - Wire harness, 2 foot (610 mm).

      - Wire harness, 5 foot (1524 mm).

      - Wire harness, 7 foot (2134 mm).

      - Wire harness, 9 foot (2743 mm).

      - Splitter, 2 output.

      - Splitter, 5 output.

      - U-channel for LED strip light, white, 68 inch (1727 mm).

      - U-channel for LED strip light, white, 92 inch (2337 mm).

      - U-channel for LED strip light, black, 72 inch (1829 mm).

      - U-channel for LED strip light, black, 96 inch (2438 mm).

- EXECUTION

  - EXAMINATION

    - Do not begin installation until substrates have been properly constructed and prepared.

    - Verify that substrate and adjacent materials are dry and ready to receive vapor retarder.

    - For decking and porch flooring installations, ensure surfaces are suitable for installation of decking and that adequate structural support has been provided.

    - If substrate preparation is the responsibility of another installer, notify Architect in writing of unsatisfactory preparation before proceeding.

  - PREPARATION

    - Clean surfaces thoroughly prior to installation.

    - Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

  - INSTALLATION

    - Install in accordance with manufacturer's instructions, approved submittals, and in proper relationship with adjacent construction.

    - Cutting: Use saw capable of miter cuts with a fine-toothed carbide tipped finish trim blade with tooth count as recommended by manufacturer.

    - Follow manufacturer's recommendations for fastener placement and spacing.

    - Decking and Porch Flooring:

      - Install a 1/4 inch (6 mm) bead of adhesive on each joist to minimize expansion and contraction.

      - Install with embossed or grain side up. Install rim boards with embossed or grain side out.

      - Fasten tight to joists. Provide shims if there are variations in framing.

      - Countersink fasteners. Provide necessary clearance when installing the next board.

      - Cut final boards as required and install as soon as possible after cutting.

      - Expansion and Contraction: Refer to manufacturers board spacing chart based on temperature at the time of installation.

      - Install decking with ends staggered over firm bearing. On sloped surfaces, lay decking with tongue upward.

      - Secure with manufacturer's recommended fastener system.

      - Install end butts and miters tight.

    - Railings:

      - Install in accordance with manufacturer's instructions.

      - Install all flat railing wood posts to a height of 36 inches (914 mm) above finished floor or deck and check for level and plumb.

      - Install stair wood posts a minimum of 48 inches (1219 mm) above the tread and check for level and plumb.

    - Siding:

      - Install the manufacturer's siding starter strip straight and level line, nailing every 8 to 12 inches (203 to 305 mm) fastening to wall studs as often as possible.

      - Install siding, and trim in accordance with manufacturer's printed installation instructions.

      - Provide a minimum of 1/2 inch (13 mm) clearance between siding and any surface that may collect water.

      - Cut siding face down.

    - Trim:

      - Glue all joints between trim pieces to prevent joint separation.

  - FIELD QUALITY CONTROL

    - Field Inspection: Coordinate field inspection in accordance with appropriate sections in Division 01.

  - CLEANING AND PROTECTION

    - Clean products in accordance with the manufacturer's recommendations.

    - Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION